## Slide 1: Hybrid Magnets: Design and Status
(with contributions from the CBETA team)

## Slide 2: Outline
Lattice and Magnet Requirements
General Concept
Prototype Magnet
Tolerances
Correctors
Path to Prototype Girder

## Slide 3: Cell
Qf/Qd: identical gradient / aperture (different length)
Beam excursion: +/- 31mm
Design: tracking with 3D field maps

## Slide 4: Requirements
Magnet to magnet variation
  Permanent magnet tolerances (harmonics / gradient strength)
  Temperature variation (harmonics, gradient strength)
  Geometric tolerances (harmonics)
  (Vibration – prefer no water cooling)
Correctors
  Risk sheet: all risks can be reduced with sufficient corrector strength
  In practice: corrector strength limited
  Avoid using correctors for errors which can be addressed by magnet design
Systematic effects: not that critical
Need magnet design which can satisfy this

## Slide 5: Magnet Concept: Hybrid
Demonstrated to work (Fermilab recycler)
Advantages
  (Largely) conventional approach
  Field quality determined by pole
  Can only drive harmonics which are allowed by geometry
Tolerances
  Laminations: shuffle
    Small magnet to magnet variation
  Permanent magnets: reduced to 1D problem
    easy to deal with remaining tolerance
  Passive scheme for temperature compensation

## Slide 6: 2D Geometry Qf/Qd
80% PM (N49M)
M
M
Size of magnets: driven by beam pipe requirements

## Slide 7: Higher Order Harmonics
Can be corrected with pole chamfer 30° reduces 12-pole to 6 units…
… but would trigger lattice re-design
Systematic effect – no problem for CBETA
R=36mm

## Slide 8: Prototype Magnet
Fast track: SiFe poles
  Reduced gradient to avoid saturation
Concept:
  Use precision Al-spacers (red arrows)
  Laminations rest on precision spacers
  Design tolerance on spacers: +/-20um
After assembly
  Tolerance spacers: 300um
  Poles misaligned
Fix: use set screws to align poles
  Calipers
  Optical level
  (not perfect!)

## Slide 9: Comparison with Simulation
Real | Simulation | Run 8
b1 | --- | ---
b2 | 10000 | -10000
b3 | 0 | 0.07
b4 | 0 | -1.46
b5 | 0 | 0.06
b6 | -14.866 | 14.29
b7 | 0 | 0.09
b8 | 0 | 0.03
b9 | 0 | 0.01
b10 | -0.14323 | -0.65
b11 | 0 | -0.01
b12 | 0 | 0
b13 | 0 | 0
b14 | -0.0811 | 0.03
b15 | 0 | 0
Skew | Simulation | Run 8
a1 | --- | ---
a2 | 0 | ---
a3 | 0 | 0.13
a4 | 0 | -0.4
a5 | 0 | 0.13
a6 | 0 | 0.18
a7 | 0 | -0.11
a8 | 0 | 0.04
a9 | 0 | 0
a10 | 0 | -0.01
a11 | 0 | 0
a12 | 0 | 0
a13 | 0 | 0
a14 | 0 | 0
a15 | 0 | 0
R=25mm
No geometry
change

## Slide 10: Tolerances: Permanent Magnets
Largest tolerance: PMs
  dx, dy, dz
  Br,x, Br,y, Br,z
Permanent Magnets
  (from industry)
  Magnetization 3-5%
  Magnetization angle 1-3º
Hybrid magnet design
  Important only flux through surface perpendicular to pole piece (Br,y)
  Reduced all tolerances of PMs to one
  Can be measured and corrected if necessary
Yoke
Pole
Br
Br,x
Br,y
d

## Slide 11: Tolerances: Permanent Magnets
Statistics
  128 permanent magnets per quadrupole
  Random drawing: flux difference between poles <0.05%
Measure blocks and sort
  Can reduce error to 10-6 level
  (cost associated with this)
Correcting errors: magnetic shunts
  Thin iron strip next to PMs
  Locally short-circuits some of the flux
PM

## Slide 12: Block Measurements
Blue: Qf
Green: Qd
Qd: +/-0.5%
Qf: +/-1%
Much smaller spread than expected
Br smaller than expected (but within +/-5% spec)
Matching (iterative): error < 1x10-5

## Slide 13: Angle of Magnetization
Qf
Qd
M
x
y
z
Angle: γ
Angle of magnetization not important for hybrid magnet

## Slide 14: Pole Tolerance
Required pole accuracy?
  Start with ideal pole and add error function
  Amplitude +/-50um
  (easily achievable with stamping)
Benchmarking
  3D tracking
  Look at orbit distortion
  Result: no issue
Choose worst error function
  Increase amplitude to 150um
  Orbit distortion < 0.3mm
Pole shape very robust

## Slide 15: Geometry / Field Quality
Pole area
  Pole shape
  Distances / tilt
  Identical to other quadrupoles
Distance pole to back yoke
  NdFeB: µr~1
  Adds to air gap

## Slide 16: Shunting
Flux imbalance: ‘bad dipole’
  (Dipole and sextupole)
  difference in PMs
  gap difference back-leg steel
Correction: magnetic shunts
  thin strip of soft-iron next to PM
  Shorts small fraction of the flux
  1mm shunt: flux change about 1%
Prototype magnet
  Gap changed due to inadequate precision spacers
  6 units of sextupole
  Corrected with shunts
  Perfect agreement with simulations

## Slide 17: Elimination of Sextupole
Real | Sim. | Run 1 | Run 8
b1 | --- | --- | ---
b2 | 10000 | -10000 | -10000
b3 | 0 | 6.25 | 0.07
b4 | 0 | -1.48 | -1.46
b5 | 0 | 0.46 | 0.06
b6 | -14.866 | 14.31 | 14.29
b7 | 0 | 0.01 | 0.09
b8 | 0 | 0.02 | 0.03
b9 | 0 | -0.01 | 0.01
b10 | -0.14323 | -0.65 | -0.65
b11 | 0 | 0.01 | -0.01
b12 | 0 | 0 | 0
b13 | 0 | 0 | 0
b14 | -0.0811 | 0.03 | 0.03
b15 | 0 | 0.00 | 0
Skew | Sim. | Run 1 | Run 8
a1 | --- | --- | ---
a2 | 0 | 0 | ---
a3 | 0 | -5.97 | 0.13
a4 | 0 | -0.22 | -0.4
a5 | 0 | 0.52 | 0.13
a6 | 0 | 0.18 | 0.18
a7 | 0 | -0.01 | -0.11
a8 | 0 | 0.04 | 0.04
a9 | 0 | -0.02 | 0
a10 | 0 | -0.01 | -0.01
a11 | 0 | 0 | 0
a12 | 0 | 0 | 0
a13 | 0 | 0 | 0
a14 | 0 | 0 | 0
a15 | 0 | 0 | 0
R=25mm
Run 8:
158mm length
shim to pole 4

## Slide 18: Octupole Error (b4/a4)
A
B
a
b
c
d
a=c
b=d
a≠b
Very likely – wouldn’t show up in optical survey (optical level)
CMM survey underway to confirm
Jack Tanabe, Iron Dominated Electromagnets Design, Fabrication, Assembly and Measurements, SLAC 2005.

## Slide 19: Temperature Compensation
NdFeB: (∆B/B)/∆T≈-1.1x10-3/K
  (have two vendors which guarantee this value)
Compensation scheme: 30-32% Ni-Fe
  Pioneered by Fermilab
  Curie temperature of 60°C
  Bsat=0.3-0.1 T (20-45°C)
Required Ni-Fe: about 20% of PM
NdFeB
NiFe
Top
Side
Chart: Temperature in °C
| 0 | 10 | 20 | 30 | 40 | 50 | 60
3A/cm | 193 | 182 | 161 | 120 | 72 | 34 | 12
10A/cm | 359 | 301 | 236 | 166 | 101 | 52 | 22
50A/cm | 391 | 328 | 261 | 192 | 127 | 73 | 37
80A/cm | 396 | 335 | 269 | 202 | 137 | 82 | 44
200A/cm | 407 | 350 | 289 | 225 | 163 | 108 | 65
 | 269 | 202 | 135 | 68 | 1 | -66
Thermoflux TX65/100

## Slide 20: 3D NiFe Temperature Compensation
Not shown: same for Qd / individual magnets
Qf, field at outermost aperture
20ºC
30ºC
0.368T
0.3681T
z (m)
NiFe
Demonstrated (exp.) temperature coefficient (%/K):
  uncompensated: -0.103
  Compensated: <-0.003

## Slide 21: Variation of Br
Magnets designed for Br of 1.37T
  But Br could also be 1.42T
CBETA: easier to deal with higher gradient
  Can reduce gradient, but not increase (easily)
  Systematic change
Temperature compensation?
  Fill horizontal slots during assembly
  Longitudinal space required (width)
    Nominal: 8.25mm
    Br =1.42T: 8.5mm
Also: μr of PMs not guaranteed property
Blue: NiFe
Available hor. gap: 12mm
Can correct for 3% gradient difference

## Slide 22: Magnet Manufacturing
Vendor A
Assembly
Vendor C
Permanent
Magnets
Vendor D
Raw Material Iron
Vendor B
Laminations
Rotating Coil Measurement
Shunt to cancel unwanted harmonics
Shunting to get gradient identical
Girder
Temperature compensation:
PM properties and NiFe specs guaranteed
Can calculate required amount of NiFe
In addition: take samples and verify with c-core magnet (1 PM + NiFe per pole)

## Slide 23: Correctors
Dipole correctors
  Normal: 347.26 Gauss.cm (B/B~5x10-3)
  Skew: 590 G.cm (B/B~8x10-3)
Quad corrector: +/- 4%
  Gradient quality unaffected by quad corrector
All air cooled
With engineering at the moment
  Manpower limited

## Slide 24: Crosstalk
Distance between magnets comparable to aperture
  Flux leakage, drives neighbouring magnet
  10% effect
Predicted accurately?
  Yes, by FEA
  Need enough elements
  Check solver tolerance
Worst case scenario
  Systematic change
  Can correct for this by offsetting magnets
Benchmarking: Opera vs Comsol
Will measure this with prototype magnets
D
D
D
F
F
Opera Model
Iron only

## Slide 25: Difference Map
Remaining difference caused by coarse mesh
Turnaround times
Opera 2.5d
Comsol: 4h
Not a concern

## Slide 26: eRHIC
Solution scales easily
General: eRHIC magnets are easier
  CBETA: stretch in terms of gradient / aperture
  This are long magnets
  No crosstalk
Block sorting quite possibly not required
  Larger number of PMs per magnet
  Shunting works well
  Much easier logistics
  Cost savings
Company (SBIR): down-select of different magnet types (incl. Halbach)
This is cost-efficient structure

## Slide 27: Schedule
Surveying of fast-track prototype magnet
Upgrade to full prototype Qd
  Good quality iron
  Full strength
  Temperature compensation
Prototype Girder options
  A: start procurement after full prototype
  B: start procurement immediately, prototype in parallel
Option A
Option B

## Slide 28: Preferred Route: Option B
Gain: 2.5 months
Confidence in magnet design
  No surprises
  Prototype shows good agreement with simulation
  Octupole due to pole misalignment, should disappear
  Shunting works, fast and efficient process
  Temperature compensation shown to work in tests at BNL
Minor design modifications can be made after prototype girder

## Slide 29: Conclusion
CBETA
  Prototyping of essential technology for eRHIC
  Chosen design: Iron dominated magnets
Essential: small magnet to magnet variation
  Need to keep tolerances under control
Permanent magnets
  Large tolerances on magnetic moment / angle
Hybrid magnets: designed to cope with that
Prototype magnet
  ~2 units out of 10000 (R=25mm, up to 20-pole)
  2 units octupole: likely caused by pole misalignment (conformation underway)
Correctors
  Normal/skew dipole, quadrupole

## Slide 30: Additional Slides

## Slide 31: Fast Track Qd Magnet

## Slide 32: Hysteresis Effects
Assembly error
  One quadrant: assembled with wrong polarity
Can be studied with Jiles-Atherton material model
Small effect on gradient
Cure: cycle quad corrector (Step 3)

## Slide 33: Quad Corrector
Coil: 8x10mm2
J = 1A/mm2
+/-4%
Gradient quality unaffected by quad corrector
Can be air-cooled
G/G0,nominal
1.04
1.0
0.96
x (m)

## Slide 34: Materials
Iron
  Low carbon steel
  JFE-EFE: procured recently for large magnetic shielding project
  BH curves for as delivered, machined, machined+annealed
  (SiFe no change in gradient or quality)
Permanent Magnet
  Grade: N49

## Slide 35: Magnetization
200 MeV
150 MeV
1.8T
1.4T
Less stringent requirements on iron

## Slide 36: Helmholtz Coil
Thanks to Toshiya Tanabe & Chris Eng (BNL Insertion Devices Group)
Mike Anerella, Jesse, Ray + Mike
Variation in permanent magnets: Match PMs to deliver same amount of flux to each pole

## Slide 37: Geometry Errors
Back-yoke
  Introduces sextupole
  Same as imbalanced poles
Pole (100um)
  Changes:
 | Bn | An | Bn | An
1 | 0 | 0 | 0 | 0
2 | 0 | 0 | 0 | 0
3 | -1.6 | 1.6 | -1.7 | 0.8
4 | 0 | 0.5 | 0.5 | 0.4
5 | -0.6 | -0.6 | -0.5 | -0.4
6 | 0.5 | 0 | 0.4 | 0
Poles will be aligned to 25um
Shifted Shifted+rotation

## Slide 38: Assembly
PM: 35x37.3x28.5 mm3
Holding force: >30kg
Adjacent PMs repel….
… unless they have iron on both sides
Grid
Courtesy of George Mahler
53/58 laminations (2mm thick)
8mm end lamination

## Slide 39: Variation of Temperature Coefficient
NdFeB: (∆B/B)/∆T≈-1.1x10-3/K
  Not guaranteed property
So far: Thermoflux 65/100G
Alternative: 45/100S?
Advantage:
  Bsat larger slope
  Smaller saturation field
  Need less material for same effect
Example: c-core magnet
  5.5 mm vs 8 mm
Disadvantage: smaller temperature range
  15-30°C (vs. >10-40°C)

## Slide 40: Opera DFDFD Model
N: DOF
E: Estimated error
W: Scaling factor (1)

## Slide 41: Gradient quality (2D)
Beam excursion: 31mm
Hump: orbit compression
Requested: 1%
ΔG/G0

## Slide 42: 3D Integrated Gradient Quality
Caused by end effects of magnets
(N.b. This works!)

## Slide 43: Grid Concept
PM sizes
  Qd: 35x37.3x31.2 mm3
  Qf: 35x37.3x28.5 mm3
Small PMs vs. big PMs
  Matching (statistics)
  Holding force (60 lbs)
Space in between PMs
  Temperature compensation
  Shunting
NiFe

## Slide 44: Bench Test
Material: VAC 745TP
Temperature coefficient (%/K)
  uncompensated: -0.103
  Compensated: <-0.003
Chart: 
| Point 1 Field (T) | Point 2 | Point 3 | Point 4 | Point 5 | Point 6 | Point 7 | Point 8
0 T_Room | -0.2155 | -0.215 | -0.2152 | -0.2152 | -0.219 | -0.2192 | -0.219 | -0.2187
0 T_Fridge | -0.2177 | -0.2172 | -0.2173 | -0.2177 | -0.2217 | -0.2215 | -0.2218 | -0.2216
24 T_Room | -0.2032 | -0.2029 | -0.203 | -0.2032 | -0.2065 | -0.2067 | -0.2067 | -0.2067
24 T_Fridge | -0.2032 | -0.2029 | -0.203 | -0.2032 | -0.2067 | -0.2069 | -0.2067 | -0.2068
NiFe

## Slide 45: Discrepancy in Quad Strength
Quad strength within 2%
  Good, but not great
  (Demonstrator was closer)
Likely reason: set screws
  Ferro-magnetic
  Will act as shunt
Number of options
  Wait for ‘full’ prototype
Worst case: systematic error