## Slide 1
Electron beam generation and cathode R&D at the HERACLES facility
Matthew Andorf, CLASSE

## Slide 2
HERACLES TEAM
In collaboration with
Jai Kwan Bae (Former student)
Luca Cultrera (now @ BNL)
Jared Maxson
Ivan Bazarov
Adam Bartnik
Alice Galdi (now @U. of Salerno)
Sam Levenson (Graduate student)

## Slide 3
Photocathodes for High Current applications
For high current operation, we require a relatively high Quantum Efficiency
  For visible light photons, a 1% QE cathode yields ~4 mA per 1 W of laser power
  Metal cathodes provide QE’s several orders of magnitude too small. Must use semiconductor-based cathodes!
ERL-FEL based UV lithography~ 10 mA average current
Electron based, strong hadron cooling with an ERL needs 100 mA!
Cornell has a long history of high current photocathode development. Current record holder for highest average current from a photoinjector, 65 ma!
For high brightness, photocathodes are ideal. They provide low transverse and longitudinal energy spreads
  Low emittance beams enable the FEL-lasing process
  SHC requires, a high charge bright beam with low energy spread
Alkali-antimonides are great for these applications

## Slide 4
Photocathodes for High Current Spin-Polarized electrons
PEPPo
Many future facilities want spin-polarized electrons at high average currents
Only candidate cathode for the job: GaAs!
Charge lifetime: The amount of current extracted before the QE degrades by 1/e
  1000 C is state of the art6 hours at 50 ma!

## Slide 5
GaAs photocathodes for spin-polarized electron beams
0.34 eV spin-orbit splitting in the valance band:
  4-fold degeneracy in p3/2
  2-fold degeneracy in p1/2
Optical selection rules require Δm=+/-1 for right/left-handed circularly polarized light
Max polarization occurs with excitation at the bandgap where emission from p3/2 >> emission from p1/2
  Theoretical max value of 50% for Bulk GaAs
  Straining GaAs breaks the p3/2 degeneracy theoretically allowing 100% polarization
Pierce et al, The GaAs Spin Polarized Electron Source (1980)
Bae et al, Rugged Spin Polarized Electron Source Based on Negative Electron Affinity GaAs photocathode with Robust Cs2Te coating (2018)

## Slide 6
Negative Electron Affinity activation
For the highest QE, GaAs are “activated” to Negative Electron Affinity (NEA)
  NEA means the bulk conduction band minimum is larger than the vacuum level
NEA is typically achieved by depositing a monolayer of Cs-Oxidant onto the GaAs surface can be done by:
  Co-deposition: Cs is deposited until QE peaks, at which point an oxidant is leaked while Cs source remains on
  Yo-yo method: the cathode is over cesiated at which point the cesium source turns off. It is then exposed to an oxidant until the QE peaks, the oxidant is then turned off and cesium source back on. The cycle is repeated numerous times.
Either O2 and NF3 can be used for an oxidant
Problem: A monolayer is a fragile thing!
  Chemical poisoning: Interaction with residual gas
  Ion back bombardment: residual gas is ionized and accelerated towards the cathode

## Slide 7
The Mother Chamber
“Mom, your love is a mystery: How can you do it all? You’re always there with the perfect fix For my problems, big and small…..”

## Slide 8
The growth chamber
Cs,Sb,Te,Rb sources+O2 leak valve, thermally regulated with pneumatic valve control
Quartz microbalance (QMB) for deposition monitoring
Substrate heater

## Slide 9
The Auger chamber
Auger Electron Spectroscopy-To characterize surface chemistry
Low Energy Electron Diffraction-Chararacterize surface crystallinity
Cs, O2 leak valve.
Insulated, bias-able cathode holder

## Slide 10
The TE meter
10 kV electron gun
Microchannel plate for beam imaging
Measure Mean Transverse Energy (MTE)

## Slide 11
Mott polarimeter
20 keV gun + einzel lens beamline
Tungsten scattering target
Measure spin-polarization

## Slide 12
GaAs with Cs3Sb as a robust NEA activation layer
NEA GaAs can be generated by forming a heterojunction at the surface with another semiconductor (activation layer) subject to two criteria:
  In the activation layer, the gap from the fermi level to vacuum should be smaller than GaAs’s bandgap (~1.4 eV).
  So that photoemission does not occur from activation layer, its bandgap should be larger than GaAs’s.
    This criteria can be violated if the activation layer is sufficiently thin
The above suggest using p-doped GaAs with an intrinsic semiconductor with a small electron affinity for the activation layer
Cs3Sb fits this description
  Known to be less sensitive to chemical poisoning
  As a photoemitter, it can sustain 10’s of mA beam current for weeks (alkali-antimonide!)
  This indicates Cs3Sb may be a very robust activation layer!
p-type
intrinsic?

## Slide 13
GaAs with Cs3Sb as a robust NEA activation layer (recipes)
Various activation recipes were tried and compared with Cs-O2 activation:
All methods achieved NEA
  Overall, Cs-O2 produced the highest QE while Cs-Sb had the worse
  Including O2 in the activation improved QE of Sb containing recipes
The QE was monitored over time to determine robustness
  All Sb activations outperformed pure Cs-O2 and pure Cs-Sb had the longest lifetime.
Co-deposition of Cs-Sb-O finds a happy middle ground
  10x Improved lifetime over Cs-O activation.
  10x improved QE over Cs-Sb activation
Bae et al, “Improved lifetime of a high spin polarization superlattice photocathode (2020)”

## Slide 14
GaAs with Cs3Sb as a robust NEA activation layer—Trade offs
Cs-O-Sb co-deposition recipe was further refined through scanning the Sb layer thickness:
  QE and electron spin-polarization decrease with Sb layer thickness
  0.12 nm layer results in only a small QE decrease while preserving max spin-polarization!
Cultrera et al, “Long lifetime polarized electron beam production from negative electron affinity GaAs activated with Sb-Cs-O: Trade-offs between efficiency, spin polarization, and lifetime (2020)”

## Slide 15
Ion back bombardment
An electron beam can ionize residual gas which will be positively charged
Ions will be accelerated towards the cathode and cause damage
So far, results have been in growth chamber
  Low current (1-100 nA)
  Low voltage (-18 V)
  Main source of degradation comes from vacuum poisoning
In a high voltage DC gun, induced damage from ion back bombardment is more severe
  Lower energy ions can sputter off activation layer
  High energy ions damage GaAs crystal structure
Operation at high voltage and current is critical to testing efficacy of alternative activation layers!

## Slide 16
Reducing beamline ions
Although ionization cross-section at high energy (>100 keV) is small, a significant number of ions are generated outside the gun:
  Vacuum tends to be poorer in the beamlines
    Out gassing from beam loss
  Beamline is much longer than cathode/anode gap
Ions can migrate from beamline into cathode/anode gap and be accelerated
Biased anode can reduce migration
  JLAB, 2 kV bias, 22% increase in charge lifetime for GaAs
Cornell developed clearing electrodes for high current running
  Required voltage predicted by electron beam size
  No reported lifetime changes but substantial reduction in beam trips

## Slide 17
Off centered cathode
Transverse electric field inside the gun provides focusing towards the electrostatic center (EC)
If the cathode active area is positioned off axis, away from the EC, the total number of ions striking the cathode is reduced, increasing operational lifetime.
Can not eliminate ion back bombardment completely
  Ions generated near the cathode will still strike the active area.
Smaller active reduces stray beam, further increasing lifetime.
Grames et al. “Charge and fluence lifetime measurements of a dc high voltage GaAs photogun at high average current(2011)”
Puck used in HERACLES for GaAs running

## Slide 18
The HERACLES beamline
A beamline dedicated to the study of high current beam running:
Former CU-ERL gun 200kV @ 10 mA
Ion clearing electrodes
75 kW beam dump
EPICS based control system
Attached storage system: QE mapping, Cs-O activation

## Slide 19
Beamline and Diagnostic details
Beamline
2 Solenoids, 3 corrector pairs (hor/vert)
2 clearing electrodes
3 screens, 1 quad detector
1 Faraday cup
EMS system not implemented
3 Beam screens ensure clean beam transport from cathode to dump
Solenoid scan characterizes cathode MTE
Thermal couples register beam induced temperature rise at the dump

## Slide 20
Laser Setup
The Ar ion laser has been refurbished and now can operated with tunable wavelength in the visible and UV.
5 W in the visible (ML)
2 W in the UV (ML)

## Slide 21
HERACLES commissioning low current
July 17th, 2020
First beam in the summer of 2020
Gun processed up to 200 keV
Beam-based alignment of
  Electrostatic center to solenoid 1
Clean transport of beam from cathode to final view screen
  Mu metal, degaussing…
Magnet calibrations
  Angular kick vs current
  Larmor rotation

## Slide 22
HERACLES high current demonstration
Cs3Sb cathode on stainless steel puck
10 mA max current, limited by radiation trips
8 mA constant current for 3 + hours with no significant change in cathode QE
Ready for cathode lifetime studies!

## Slide 23
Cs-Sb-O activated GaAs cathode in HERACLES
Goal
Compare the charge lifetimes of Cs-Sb-O vs Cs-O activated GaAs.
Sample Preparation:
Cs-O:GaAs
  activated with co-deposition in a chamber attached to the rear of HERACLES.
  Lifetime measurements performed within hours of activation
Cs-O-Sb:GaAs
  Activated in Mother chamber and transported via a vacuum suitcase to HERACLES
  ~24 hours between activation and lifetime measurement
Run Conditions
  1 mA beam current held constant for 2-3 hours
  488 nm drive laser. QE map at 532 and 780 nm
  Typical vacuum pressure in the low e-10’s during run

## Slide 24
Cs-Sb-O activated GaAs cathode in HERACLES (results)
Cs-O
Cs-Sb-O
We did not see an improvement in the charge lifetime at 488 nm
Pre/post run comparisons of QE indicate lifetime at 780 nm may have improved.
  Relative QE change smaller for Cs-Sb-O samples
Cs-Sb-O had lower QE’s
  We observed roughly a factor of 3 reduction in the QE between activation in the Mother chamber and beginning the run.
  Required laser power a factor of 4-10 higher
The story is not over!
  New growth chamber on HERACLES to support Cs-Sb-O activation
  780 nm drive laser

## Slide 25
Summary
GaAs is currently the only viable candidate for high current spin polarized production
NEA activation is fragile, making the charge lifetime low compared to alkali-antimonides
Cs-Sb-O activation improves GaAs lifetime in growth chambers
No improvement of lifetime was observed with operation at 488 nm
  Some indirect evidence for improved lifetime at 780 nm
Future work
  Lifetime studies performed at the 780 nm
  Upgraded growth chamber on HERACLES to allow for Cs-Sb-O testing with transporting

## Slide 26
BACKUP SLIDES

## Slide 27
Analysis of QE degradation at high current
Damage is caused by ion back bombardment, but how exactly? The ions can either:
  Sputter off the NEA activation layer
  Damage the bulk crystal structure
Multiple GaAs samples ran in the CEBAF and IR-VUV FEL guns (JLAB) were studied after operation1
On two bulk GaAs samples:
  Rutherford Backscattering Spectrometry (RBS) showed no evidence of crystal damage.
  Secondary Ion Mass Spectrometry (SIMS) did not indicate hydrogen ion implantation
On SL samples:
  SIMS did show ion implantation that correlated with use AND location on the sample
1V. Shutthanandan et al. PRAB 15, 063501 (2012)

## Slide 28
Analysis of QE degradation at high current
Damage is caused by ion back bombardment, but how exactly? The ions can either:
  Sputter off the NEA activation layer
  Damage the bulk crystal structure
Multiple GaAs samples ran in the CEBAF and IR-VUV FEL guns (JLAB) were studied after operation1
On two bulk GaAs samples:
  Rutherford Backscattering Spectrometry (RBS) showed no evidence of crystal damage.
  Secondary Ion Mass Spectrometry (SIMS) did not indicate hydrogen ion implantation
On SL samples:
  SIMS did show ion implantation that correlated with use AND location on the sample
1V. Shutthanandan et al. PRAB 15, 063501 (2012)

## Slide 29
Analysis of QE degradation at high current
Damage is caused by ion back bombardment, but how exactly? The ions can either:
  Sputter off the NEA activation layer
  Damage the bulk crystal structure
Multiple GaAs samples ran in the CEBAF and IR-VUV FEL guns (JLAB) were studied after operation1
On two bulk GaAs samples:
  Rutherford Backscattering Spectrometry (RBS) showed no evidence of crystal damage.
  Secondary Ion Mass Spectrometry (SIMS) did not indicate hydrogen ion implantation
On SL samples:
  SIMS did show ion implantation that correlated with use AND location on the sample
1V. Shutthanandan et al. PRAB 15, 063501 (2012)

## Slide 30
Ion Implantation into GaAs
W. Liu et al, PRAB 19, 103402 (2016)
Hydrogen ions implanted at 100 and 10000 eV for 3 different cleave planes
Hypothesized 110’s smaller atomic density would support the most channeling and thus, be less damaged.
QE measured as a function of heat cycles
Low energy implantation resulted in QE loss that was recoverable
  Interstitial defects
High energy resulted in some permanent loss
  Knock out vacancy

## Slide 31
Ion Back Bombardment in RF guns
1 J.W. Lewellen “Ion tracking in photocathode RF guns”
2 Ji Qiang “Particle in Cell Monte Carlo simulation of ion back bombardment in a high average current RF photo-gun”
Ions are heavy enough such that over one period of acceleration, they do not travel the length of a cavity cell
The ponderomotive effect causes the ions to move from strong field regions to weaker field regions In general away from the cathode
Eliminates high energy bombardment (<9 keV for 700 keV gun)

## Slide 32
Ion bombardment reduction with an off-set anode