## Slide 1: Elastic Finite Element Modeling of X-ray Measured Microstructures
Sarah Bonestell
Dalton Shadle

## Slide 2: Overview of Project
Motivation:
  Developing a better understanding of fatigue failure on the microscopic level
Overall goal:
  Analyze elastic stress/strain on the microstructure of a metal superalloy (Inconel-718) by using Finite Element Modeling (FEM) and measurements captured through X-rays
Process:
  Experiment/Measurements
  Meshing
  Modeling
  Analysis

## Slide 3: Background
400 MPa
700 MPa
Far-Field Detector
Near-Field Detector
Sample
Optics
Figure 1. Forming and Shaping Technology (FAST) Beamline at CHESS
Figure 2. Stress/Strain curve for Inconel-718

## Slide 4: Experiment/Measurements
HEDM- High energy X-ray diffraction
Near-Field and Far-Field measurements
  Obtain map, orientation, elastic strain, and centroid of grains
Figure 1. Near-Field and Far-Field data collection

## Slide 5: Meshing
Grain map
Tessellation
Mesh
Python script converts NF and FF data into tessellation file of microstructure grains
Neper creates a mesh on the microstructure
Neper output transformed into files readable by MechMet

## Slide 6: Modeling
Run MechMet.m script
  Performs FEA
    Software that mathematically predicts stress/strain on a structure by using stiffness matrix, boundaries and forces as input
  Outputs
    vtk file for visual analysis in ParaView
    Files for further data analysis (stress, strain, stiffness, strength-to-stiffness)
Figure 2. MechMet MATLAB script
Figure 3. Microstructure visualized in Paraview

## Slide 7: Analysis
400 MPa Stress:
700 MPa Stress:

## Slide 8: Future Work
SXM Optimization
  MATLAB script finds optimal C11, C12, C44 values
Use optimal values to find grains experiencing high stress
  Need good model agreement, reliable SXM
  Will give better understanding of fatigue/crack initiation
Generalized Hooke’s Law:
Figure 4. Microstructure depicting grains with highest Von Mises stress

## Slide 9: Questions?