Comparison of Electronic Cloud Abatement Techniques Under Same Beam Conditions
and
Constraining Photoelectron Energy Distributions Using Bunch-Current Scans
Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
CesrTA Electron Cloud Meeting
16 March 2011

---
Witness Bunch Study Data Sets
2010
The December data sets were designed to study the dependence of the witness bunch studies on bunch current.
They provide an opportunity to address Mark's request for vacuum chamber comparisons
for the same beam energy, species, bunch current and spacing, and reflected photon contribution (15E/W).
For TiN and Carbon we can increase the sample of comparisons at 2 GeV in the 2011 data-taking periods.
We have not yet submitted the Task Overview sheets for these measurements.

---
Vacuum Chamber Comparison Under Same Beam Conditions
5.3 GeV Positron Beam
Witness bunch with 28-ns spacing
15W
15E
5 mA/bunch
The carbon coating
suppresses high-energy
photoelectrons compared
 to the TiN coating.
The results for the second
carbon-coated chamber
corroborate the
high-energy photoelectron
suppression relative
to TiN observed with the
first carbon chamber.
The q.e. for reflected
photons and the SEY
are both much smaller
for TiN compared to Al.
The 3-mA TiN witness
signal is a factor of 5
smaller than
for 5 mA/bunch.
(see slide 5)
3 mA/bunch
The second
carbon-coated chamber
shows conditioning effects
between 5/17 and 12/24,
primarily for the
quantum efficiency.

---
Vacuum Chamber Comparison Under Same Beam Conditions
5.3 GeV Electron Beam
Witness bunch with 28-ns spacing
15W
15E
5 mA/bunch
The carbon coating
suppresses photoelectron
production relative to
the TiN coating, but
the SEY may be higher.
Similar conclusions as
for the first carbon-coated
vacuum chamber.
The measurements with
the electron beam
confirm the much
smaller q.e. for reflected
photons and SEY
for TiN compared to Al
found with the positron
beam.
3 mA/bunch
The electron beam
measurements confirm
the processing effect for
the second carbon
vacuum chamber observed
with the positron beam.

---
Bunch Current Scans in September (TiN, Carbon 2)
5.3 GeV Positron Beam
Witness bunch with 14-ns spacing
The bunch current scan of 9/21
confirms the nonlinearity in the
TiN signal peak height observed
in the vacuum chamber comparisons.
Remark from MAP: The AREAS of the
signals are linear with bunch current at
To better than 15%, as would be expected
if primary photoelectrons dominated the
signal, in which case the SEY curve will
not affect it much. Simulations will tell.

---
ECLOUD Simulations for the Bunch Current Scan
5.3 GeV Positron Beam
Witness bunch with 14-ns spacing
1 -10 mA / bunch
1 mA / bunch
The bunch current scans provide a much more stringent test of the photoelectron energy distributions used in the simulation.
This example shows that the function used for the 3-mA witness bunch studies is a poor match for the 1-mA single-bunch signal, because the beam kick is not strong enough.

---
ECLOUD Simulations for the Bunch Current Scan:
Tuning the Photoelectron Energy Distribution
1 -10 mA / bunch
1 mA / bunch
After MUCH tuning work, the optimal p.e. energy distribution has changed a LOT.
These examples show why: the energy acceptance at 1 mA and 10 mA is very different.
The 10-mA signal requires a low energy peak to which the 1-mA signal is entirely insensitive.

---
Present Status
Still work to do. Dip is wrong.

---
Relative Contribution of Primaries
10 mA / bunch
1 mA / bunch
All signal macroparticles
All signal macroparticles
Primary macroparticles only
Primary macroparticles only
Witness at 14 ns mostly secondaries for 1 and 10-mA bunch currents.