Using Time-Resolved Retarding Field Analyzer Measurements
to Determine the SEY Mitigation Effectiveness of Grooves
-- Bonus: first look at last night's data --
Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
 Electron Cloud Meeting
17 April 2013

---
Progress in modeling the TR RFA Data
Status on 10 April
Present Status
Removed bug in RC time constant convolution. RC unchanged at 25 ns.
Tuned photoelectron energy distribution, photon rate, RFA acceptance function.
Canonical Al secondary yield model unchanged: δts= 1.8, δred= 0.2, δel= 0.4

---
Sensitivity to the secondary emission model
In contrast to the modeling studies for the shielded pickup data with SEY-mitigating coatings, the photoelectron production model is unchanged in the time-resolved RFA experiments, since the photoelectron production is predominantly at the primary photon impact point on the outside of the vacuum chamber.
This example comparison shows the sensitivity to the peak secondary yield to be better than 10%. Is this plot a candidate for our IPAC'13 paper?
This determination of the effective SEY value for grooves should instruct our upcoming publication on the electron cloud buildup analysis for the ILC damping ring. However, in that design we recommend TiN-coated grooves.

---
Effectiveness of TiN-coated grooves
Is it worthwhile going to the effort of using grooves in a TiN-coated vacuum chamber?
JPS reports that when the chicane magnetic field is set to 800 G, these already-small signals disappear entirely.

---
First look at yesterday's measurements by JPS
Some apparent reduction in SEY.
There is an opportunity today to remedy the saturation problem. The shift starts half an hour from now.

---
SPU and time-resolved RFA collector geometries
Shielded pickups	Time-resolved RFAs
Number of holes	169	261
Hole diameter	0.76 mm	1.7 mm
Transparency	29.8%	15.4%
Hole depth	1.8 - 2.4 mm	5.0 - 7.5 mm
Tan Θmax	0.32 - 0.42	0.23 - 0.34
Θmax	18-23 degrees	13-19 degrees
Number of collectors	3	9
Collector pitch	14 mm	5.8 mm
Collector width	18 mm	(round)	5.8 mm