Shielded Button Measurement/ECLOUD Simulation Comparison
for the Cloud Lifetime Study Using Witness Bunch Data
 All material for this talk may be obtained at www.lepp.cornell.edu/~critten/cesrta/ecloud/1oct10
 The measurements of 3/27/2010 are described here: https ://webdb.lepp.cornell.edu/elog/CTA+MS/551
The measurements of 5/17/2010 are described here: https ://webdb.lepp.cornell.edu/elog/CTA+MS/629
See also previous talks in the electron cloud meetings on simulations for the shielded button data on 4/21, 4/28, 5/12, 7/7, 7/14, 8/4, 9/2010
 Context
A primary purpose of the shielded pickup project (time-resolved measurements vs RFA) is to measure the cloud lifetime.
This lifetime is sensitive to the secondary yield for low-energy cloud particles hitting the vacuum chamber wall.
This presentation shows the first results on the sensitivity to the parameter d0 using witness bunch data.
Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
CesrTA General Meeting
1 October 2010

---
 John Sikora's cloud lifetime study on 3/27
using 5 mA/bunch e+ data at 15E (TiN)
https://cesrweb.lepp.cornell.edu/instr/data/shbut/2010/20100327_summary.html

---
 ECLOUD simulation for the cloud lifetime study
using 5 mA/bunch e+ data at 15E (TiN)
Secondary Yield Model
True secondary yield: 0.9
True secondary peak energy: 400 eV
Rediffused yield: 0.1
Elastic yield d0: 0.55
Two 5-mA bunch spaced by 14, 28, 42, 56, 70, 84 ns.
ECLOUD statistical errors are shown.
The measured button signals are shown as smooth dotted lines.
The measured signals are scaled by an arbitrary factor of 7.
Simulated cloud lifetime too long: reduce elastic yield?

---
 ECLOUD cloud lifetime sensitivity to elastic yield d0
d0 =0.15
d0 =0.35
d0 =0.55
d0 =0.75
d0 =0.95
d0 =1.05
The optimal value for d0 (0.15) is lower than has been generally assumed (0.5-0.7).
Note that not only the simulated peak signal value for witness bunch signals is better, but also the width.
Could such a low elastic yield be a characteristic of TiN coating?
Our tune shift simulations gave reasonable cloud decay times with a value of 0.5 for uncoated aluminum chambers.

---
 Next project
Bare aluminum chamber with 4 ns spacing
5/17/2010
NB: nonmonotonic! The narrower spacing gives sensitivity to the cloud buildup and motion.
Will we find the higher value for d0 (about 0.5) which was found to be compatible with our tune shift simulations?

---
 YES
d0 is much higher for aluminum than for TiN
d0 =0.05
d0 =0.15
d0 =0.35
d0 =0.55
d0 =0.75
d0 =0.95
Many systematic checks remain before a value for d0 can be precisely given, but the sensitivity is obvious.
This study was difficult because an unexpected extreme sensitivity to the photoelectron energy distribution had to be discovered.
The simulation for the 4- and 8-ns spaced bunches still needs work.