First Results on the Diamond-like Carbon Mitigation Technique
From Shielded-Pickup Measurements
– Measurements recorded 4/7 and 4/16 --
Jim Crittenden & John Sikora
Cornell Laboratory for Accelerator-Based Sciences and Education
Electron Cloud Meeting
20 April 2011

---
How the Witness-bunch Method Works
Example: 15W, Al v.c., 2.1 GeV, 3 mA/bunch e+ beam, 4-ns spacing
Superposition of 15 such traces
illustrating the sensitivity to cloud lifetime
Shielded pickup scope trace for two bunches
44 ns apart
The witness bunch signal includes the single-bunch signal as well as the the signal
produced by cloud electrons accelerated into the shielded pickup by the kick from the witness bunch.

---
 Model Sensitivity to Secondary Electron Yield Parameters
3/27/10: 15E, TiN, 5.3 GeV, 5 mA/bunch e+ beam, 14-ns spacing
This example of ECLOUD simulations shows a preferred value for the elastic yield in a TiN-coated v.c. of d0=0.05.
A similar value was found for amorphous carbon coating (two different v.c.), while the value found for bare Al was 0.75.

---
 First Results for Diamond-like Carbon Coating
4/7/11: 15E, DLC, 5.3 GeV, 5 mA/bunch e+ beam, 14-ns spacing
Compare to the model used for TiN at 15E in order to have the same sync rad conditions
The diamond-like carbon coating exhibits significantly lower values for the quantum efficiency for producing
photoelectrons as well as lower secondary yield, both for the true secondary process and the elastic process.

---
 2.1 GeV Witness Bunch Study
We DO have such a study for carbon at 15E, but with 4-ns spacing
5/9/11: 15E, Carbon, 2.1 GeV, 3 mA/bunch e+ beam
At 3 mA/bunch the carbon signals are very small and the data quality suffers from some oscillation background.
Very good model using power-law energy distribution with 50% 5 eV Gaussian for photoelectron energy spectrum.
The modeled true secondary yield may be low. Note that the elastic yield affects the early signals as well.

---
 2.1 GeV Witness Bunch Study
5/9/11: 15E, Carbon, 2.1 GeV, 3 mA/bunch e+ beam, 14-ns spacing
We DO have such a study for carbon at 15E, but with 4-ns spacing
Full scan of elastic yield values for the 9 May 2010 carbon data.
The data quality reduces the discriminating power for the elastic yield. Values greater than 0.25 are excluded.

---
 Compare new DLC measurements to successful carbon model
4/16/11: 15E, DLC, 2.1 GeV, 3 mA/bunch e+ beam, 14-ns spacing
Result shows lower quantum efficiency and secondary yield relative to the carbon chamber
just as the 5.3 GeV witness bunch study found lower values relative to TiN.

---
 Witness studies with bunch current scan to improve sensitivity
4/16/11: 15E, DLC, 2.1 GeV, 5 and 8 mA/bunch e+ beam, 14-ns spacing
Model photoelectron energy distribution may require re-tuning because the accepted energy range depends on bunch current.