First Look at Today's SPU Measurements
Complete program of pre-conditioned Al and TiN witness bunch data achieved 3 am – 7 am.
Jim Crittenden & John Sikora
Cornell Laboratory for Accelerator-Based Sciences and Education
 CESRTA Collaboration Meeting
22 August 2012

---
Witness Bunch Study for TiN-coated Aluminum
Compare today's measurements to those of 6/18/2011
15W 5.3 GeV 5 mA/bunch e+ 14-ns spacing
Present best model for 6/18/11
Same model with today's measurements
on unconditioned TiN
Initial indication is the the quantum efficiency is similar, but there is much more cloud due to SEY.