Shielded Pickup Measurements in June, 2011
Ryan Badman, Jim Crittenden, John Sikora
The TiN-coated vacuum chamber at 15W was installed in September, 2010.
The diamond-like carbon-coated (DLC) chamber at 15E was installed in January, 2011.
Therefore, our standard data sets (solenoidal-field, witness-bunch, and bunch-current scans)
at 2.1 and 5.3 GeV in June provided primarily information on conditioning (the first such info for DLC).
We also took the first standard data sets at 4.0 GeV, as well as bias voltage scan data.
Preliminary assessment of conditioning effects in the diamond-like carbon-coated chamber
based on modeling experience
The quantum efficiency for photoelectrons produced by reflected s.r. photons has increased slightly, and the photoelectron energy spectrum has a higher energy tail.
The secondary yield has decreased slightly.

---
Vacuum Chamber Comparisons Under Same Beam Conditions
5.3 GeV Positron Beam
Electron Cloud Modeling Results for Time-Resolved Shielded Pickup Measurements at CesrTA, WEP142, PAC'11, 3/28-4/1/2011, New York City, NY
15W
15E
5 mA/bunch
The carbon coating
suppresses high-energy
photoelectrons compared
 to the TiN coating.
The results for the second
carbon-coated chamber
corroborate the
high-energy photoelectron
suppression relative
to TiN observed with the
first carbon chamber.
The q.e. for reflected
photons and the SEY
are both much smaller
for TiN compared to
relatively unprocessed
Al.
3 mA/bunch
The second
carbon-coated chamber
shows conditioning effects
between 5/17 and 12/24,
primarily for the
quantum efficiency.
Conversation with
Pedro Costa-Pinto at PAC'11

---
ECLOUD Modeling for the Conditioning Effects in the DLC Coating
Recent Developments in Modeling for Time-Resolved Measurements of Electron Cloud Buildup at CesrTA, WEPC135, IPAC'11, 9/26-30/2011, San Sebastian, Spain
Optimization of the modeled photoelectron energy distribution and quantum efficiencies for direct and reflected photons, secondary yield components, and the energy distribution of secondary electrons provides a good description of the measured shielded-pickup signals.
The SPU signal from the leading positron bunch is dominated by photoelectrons produced on the bottom of the vacuum chamber. Its modeled size and shape result from the photoelectron production kinetic energies and the attractive beam kick, which combine to determine the arrival times of cloud particles contributing to the signal.
The SPU signal from the witness bunch includes in addition the cloud electrons accelerated by the beam into the detector. Many of these are secondaries, and thus sensitive to the secondary yield and production kinematics.
Consequently, the ratio of the leading and witness-bunch signals discriminates between photoelectron production and secondary electron production. In this case of the DLC coating conditioning effect, the measured signals are consistent with a change in quantum efficiency and inconsistent with a change in secondary yield.

---
Ryan's Study of How the Witness Bunch Measurements Can Constrain Parameters of the Secondary Electron Production Kinematics
Original ECLOUD Model vs. New Optimized Model
f(Esec) ~ Esec exp (-Esec/SEMAX )
SEMAX=0.8 eV
f(Esec) ~ exp( -ln(Esec/SEMAX)2/2 )
SEMAX=1.8 eV

---
        peak
        not in
        data
Sensitivity to SEMAX Parameter using exponential function
(Note the late simulation peak at SEMAX>0.8 eV that is not present in the data)

---
Lower bound on SEMAX obtained from 14-ns witness bunch signal shape

---
New for this meeting:
The witness bunch measurements at 2.1 GeV provide constraints
very similar to those obtained with the 5.3 GeV data.

---
The 2.1 GeV measurements also provide an upper bound on the SEMAX parameter
similar to the one found with the 5.3 GeV data.