Parameter Correlations in the ECLOUD Simulation for the Cloud Lifetime Study Using SPU Witness Bunch Data, First Results for Carbon-coated Vacuum Chambers
and
First Results Using SYNRAD3D Azimuthal Photoelectron Distributions
 All material for this talk may be obtained at www.lepp.cornell.edu/~critten/cesrta/ecloud/24nov10
 See also previous talks on simulations for the shielded pickup data on 4/21, 4/28, 5/12, 7/7, 7/14, 8/4, 9/8, 9/22, and 11/3/2010
A primary purpose of the shielded pickup project (time-resolved measurements) is to measure the cloud lifetime.
This lifetime is sensitive to the secondary yield for low-energy cloud particles hitting the vacuum chamber wall.
First results on the sensitivity to the parameter d0 using witness bunch data were shown on 9/22/2010 and at ECLOUD10.
In the meantime, the ECLOUD SPU acceptance model has been improved and hole secondaries introduced (3 Nov).
Today we address the systematic sensitivity of the d0 determination to other model parameters.
Motivated by Joe Calvey's RFA studies of model parameters shown last week, we use the data for carbon-coated vacuum chambers for this purpose. We also show the first use of the SYNRAD3D fits for photoelectron azimuthal distributions.
Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
Electron Cloud Meeting
24 November 2010

---
Status as of ECLOUD10 for the cloud lifetime study
using 3/27 5 mA/bunch e+ data at 15E (TiN)
Secondary Yield Model
True secondary yield: 0.9
True secondary peak energy: 400 eV
Rediffused yield: 0.1
Elastic yield d0: 0.55
Simulated Population of SEY Curve
Red: True secondaries
Blue: Rediffused
Green: Elastics
Rediffused plotted on top of the elastics
Two 5-mA bunches spaced by 14, 28, 42, 56, 70, 84 ns.
ECLOUD statistical errors are shown.
The measured button signals are shown as smooth dotted lines.
The measured signals are scaled by an arbitrary factor of 7.
True Secondaries
Elastic
Simulated cloud lifetime found to be sensitive to d0
TiN (3/27 15E 14-ns) : d0 = 0.05 Al(5/17 15W 4-ns): d0= 0.75
Rediffused
 d0 = 0.55 clearly too high !

---
 ECLOUD cloud lifetime sensitivity to elastic yield d0
-- Present status for 3/27 5 mA/bunch data for 15W carbon-coated v.c. --
Baseline parameters: 0.9 g /m/s, q.e. 5%, reflectivity 20%, dts = 0.7, Epk = 400 eV, dred = 0.1.
SPU signal scaled by factor 1.7. Elastic yield parameter d0 = 0.05 is the best match.

---
 Sensitivity to Reflectivity: 20% --> 30%
SYNRAD3D value is 27% (dipole method, GD 14 July 2010, JAC 8 Sep 2010)
The source of the rising edge of the first-bunch signal is photoelectrons from the bottom of the beampipe,
so the SPU scale factor must be raised from 1.7 to 2.5. No value for d0 reproduces the measured witness bunch signals.

---
 Sensitivity to Reflectivity: 20% --> 10%
For this comparison, the SPU scale factor has been left unchanged at 1.7, rather than reducing it to 0.85. The simulated ratio of the
14-ns-bunch signal to that of the first-bunch is clearly wrong. If this were corrected, again, no value for d0 would reproduce
the measured witness bunch signals, because the direct signal contributes a substantial fraction of the 84-ns-bunch signal.

---
 Sensitivity to True secondary yield: 0.7 --> 0.5
Can the elastic yield compensate the true secondary yield?
Nope. The elastic component does not contribute enough to the 4-ns-bunch signal to compensate a deficit in the true secondary yield.
Also investigated Epk=250, 400 eV, dts = 0.9 , dred = 0.1, 0.3 and dts , dred correlation. The elastic yield did not budge.
Also, none of these parameters could explain the narrowness of the observed signals. Needs more study.

---
 ECLOUD cloud lifetime study for the 15E carbon-coated v.c.
-- 3 mA/bunch 5/17 data 4-ns spacing --
Baseline parameters: 0.4 g /m/s, q.e. 5%, reflectivity 40%, dts = 0.7, Epk = 400 eV, dred = 0.1.
SPU signal scaled by factor 1.4. Elastic yield parameter d0 = 0.35 is the best match, but work needed.

---
 SYNRAD3D photoelectron azimuthal distribution
RFA_tab_fits_Lorentz_chess_20090225_positron.csv RFA: SP15W2
3/27 15W 5 mA
14-ns spacing
q.e. 10%
spu scale 1.7
unchanged
NB: Synrad3D
calculations
were done
for a
centered beam.
These data
were taken
with the
pretzel orbit.
No photon
energy
information
from
SYNRAD3D
was used.
A custom p.e.
energy
distribution
was derived
from the
single-bunch
signal shape.
SYNRAD3D provides absolute photon rates as a function of scaled v.c. perimeter in the form of two Lorentzian fits plus a 6th order polynomial.
https: //wiki.lepp.cornell.edu/ilc/pub/Public/CesrTA/EcloudParams/Synrad3d_RFA_fits.pdf
ECLOUD reads the csv file and generates the azimuthal distribution using Miguel's ellipse functions and my Monte Carlo utilities.

---
 SYNRAD3D photoelectron azimuthal distribution
RFA_tab_fits_Lorentz_chess_20090225_positron.csv RFA: SP15E2
3/17 15E 3 mA
4-ns spacing
q.e. 10%
spu scale 1.4
unchanged
Remarkable
agreement
again!
Lowering the
true
secondary
yield
below 0.7
may help.
SYNRAD3D reproduces the WIDTH of the SPU signals better than the assumption of uniform azimuthal distribution of reflected photons.
Note that in each of these measurements, the positron beam was displaced 12 mm toward the outside of the vacuum chamber.
I continue to work on the excess early peak for closely spaced witness bunches, which is so bad that I omitted the 4-ns and 8-ns bunches here.

---
Compare uniform and SYNRAD3D
photoelectron azimuthal distributions
Uniform
SYNRAD3D
The SYNRAD3D azimuthal distribution is a remarkable improvement, both for the shape of the single-bunch signal and
for the shapes and relative sizes of the witness bunches at 4 and 32 ns.
This explains why my weeks-long attempt to fix the 4-ns bunch with the photoelectron energy distribution alone has been so fruitless.
The accuracy of the normalization must be fortuitous, since the assumption of 10% quantum efficiency for SYNRAD3D was arbitrary.

---
Compare azimuthal origins of
SPU signal particles
Uniform
SYNRAD3D
Single Bunch
0 < t < 30 ns
4-ns Bunch
10 < t < 30 ns
32-ns Bunch
32 < t < 52 ns
Particles contributing to the signal by
producing secondaries in the port holes
are shown in blue
There are many fewer signal particles in SYNRAD3D for the first bunch and the witness bunch at 4-ns.
That is, SYNRAD3D produces many more particles at azimuthal positions where they cannot contribute to these signals.
Particles produced at the opposite side of the vacuum chamber from the primary source point are important for the
signal from the witness bunch at 32-ns. These are absent in the uniform azimuthal distribution.