## Slide 1: Electron Cloud Growth & Mitigation: In-Situ SEY Measurements Retarding Field Analyzer Studies
W. Hartung, J. Calvey, C. Dennett, J. Makita, V. Omanovic for the CESRTA Collaboration
CesrTA Advisory Committee Meeting ● 11 September 2012

## Slide 2
In-Situ Secondary Electron Yield Measurements
W. Hartung, C. Dennett, V. Omanovic for the CESRTA Collaboration

## Slide 3: Review: SEY Studies
Secondary emission is important for models of electron cloud build-up
SEY depends on energy and angle of incident electron
Secondary electrons have a distribution in energy and angle
Inc. energy = 300 eV Inc. angle = normal
Inc. angle = normal

## Slide 4: Review: SEY Studies
Secondary Electron Yield (SEY) Studies
  Measure SEY of surfaces under realistic conditions
  Measure effect of beam conditioning
  Compare different materials and mitigation coatings
SEY apparatus based on technology developed at SLAC for measurements in PEP-II
SEY measurements being done at CERN and KEK also

## Slide 5: Review: SEY Studies
Unique aspects of CesrTA SEY program
  In-situ: see beam conditioning vs time, not just before and after; change samples rapidly
  Observe deconditioning in a realistic environment
  Compare effect of direct SR photons to scattered photons + electrons
Collaborative aspects of CesrTA SEY program
  Samples and coatings from SLAC, CERN, KEK
  Duplicate systems delivered to Fermilab for future studies in Main Injector
  Funding in place for surface texturing R&D with PNNL

## Slide 6: In-Situ Measurements
In-Situ SEY Station (ISSS)
  Horizontal sample: direct photons in middle
  45° sample: scattered photons and cloud electrons
  SEY measurements while samples remain under vacuum
  Typically measure SEY during weekly tunnel access

## Slide 7: SEY Samples
20°
25°
30°
TiN- coated
TiN- coated
Bare Al
Use DC electron gun and picoammeter for indirect SEY measurement

## Slide 8: In-Situ Apparatus
Expose samples to beam environment
Measure SEY
e-Gun
Sample
Beam Pipe
Sample
e-Gun
CESR Beam

## Slide 9: In-Situ Apparatus

## Slide 10: SEY Samples
Material | Dates | Comments
TiN | Jan 2010- Aug 2010 | Samples from SLAC
Al | Aug 2010- Nov 2010 | 6061-T6
Amorphous C | Nov 2010- Jan 2011 | Coating by CERN
Diamond-like C | Sep 2011- Nov 2011 | Coating by KEK
TiN | Nov 2011- Mar 2012 | Samples from SLAC
Cu | Mar 2012- Jul 2012 | OFC 101
Stainless steel | Aug 2012- | 316-series

## Slide 11: SEY Techniques
Material | Dates | Modifications
TiN | Jan 2010- Aug 2010 | Commission systems
Al | Aug 2010- Nov 2010 | Remove vacuum gauges
Amorphous C | Nov 2010- Jan 2011 | 
 |  | Mitigate leakage current and charging
Diamond-like C | Sep 2011- Nov 2011 | Improve spatial resolution Ensure exposure of samples to direct SR
TiN | Nov 2011- Mar 2012 | More resolution at low energy More height resolution and range
Cu | Mar 2012- Jul 2012 | More angle resolution and range
Stainless steel | Aug 2012- | Reduce cross-talk, improve record-keeping

## Slide 12: SEY vs Energy: Example
Beam conditioning of horizontal TiN sample (2011-2012)
SEY at center of sample: Inc. angle = 25°
Note:
100 Amp·hr
= 3·1023 photons/meter

## Slide 13: Peak SEY vs Beam Dose
Horiz.
45°
Beam conditioning of SEY samples (center, inc. angle = 25°)

## Slide 14: SEY Findings
Direct SR (horizontal sample) vs electrons and scattered photons (45° sample)
  Did not observe clear difference with initial samples
  Now observing some differences after improvements in techniques
Preliminary Findings
  Differences limited to early conditioning for stainless steel and copper
  Differences endure longer for TiN

## Slide 15: Example: SEY along beam pipe
Beam conditioning of stainless steel (at 405 eV)
Horiz.
45°
Direct SR
Inc. angle
≈ 25°

## Slide 16: SEY Work in Progress
SEY dependence on incident angle
  More extensive measurements on recent samples
  Need to compare with SEY models
SEY at low incident energy
  More extensive measurements on recent samples
  Need to better quantify systematic errors
Deconditioning
  Observe SEY increase with samples in vacuum
  Quantified effect for Cu samples during down
  Observe SEY increase with exposure to air
    More systematic measurements needed

## Slide 17: Connection to SEY Models
SEY models for EC build-up
  SEY depends on energy and angle of incident e-
  “True” secondaries: low energy
  “Elastic” secondaries: same energy as incident e-
  “Rediffused” secondaries: energy ≤ incident e-
Work in progress/future interests
  What parameters of SEY models are constrained by the measurements?
  How does the measured SEY differ from the actual SEY?
  What can we learn about the energy distribution of secondaries?

## Slide 18: Conclusion
CesrTA SEY studies
  Measurements on samples of 6 materials/coatings so far
  Improvements in techniques have been made
  Measured rate of beam conditioning
  Measured direct SR vs indirect conditioning
  Connecting SEY measurements to SEY models: in progress
  Ultimate goals: constrain SEY model parameters as much as possible; use results in EC models

## Slide 19
Retarding Field Analyzer Studies
J. Calvey, W. Hartung, J. Makita for the CESRTA Collaboration

## Slide 20: Review: Retarding Field Analyzers
Retarding Field Analyzers (RFAs)
  Measure flux of electrons from cloud
  Average over many turns (basic version)
  Modes of operation:
    Dedicated measurements with energy resolution
    Passive measurements without energy resolution
Use of RFAs for electron cloud studies was pioneered at Argonne/APS
CesrTA RFA program collaborators: APS (K. Harkay et al.), LANL, SLAC, KEK, CERN

## Slide 21: Review: Retarding Field Analyzers
CesrTA RFA program: unique features
  RFA designs with transverse resolution
  RFA designs for insertion in confined spaces
  Many RFAs (~30) deployed in a single ring
  RFAs in different environments: drift, dipole, quadrupole, wiggler
  Dedicated RFA measurements
    Under different beam conditions
    In vacuum chambers with different mitigations
    Over time, to observe beam conditioning
    In combination with other EC diagnostics
  Large data set already, ~4 years of measurements

## Slide 22: Review: Retarding Field Analyzers
e- cloud
Beam pipe
Grid (metal mesh)
Collector(s)
+100 V
Vgrid
Ideal RFA: measure electrons with energy > −Vgrid

## Slide 23: CesrTA thin segmented RFA design
Beam pipe
Beam pipe holes
Retarding grids
Collectors

## Slide 24: RFA Measurement Examples
RFA results for segmented collectors in different environments
  Show distinctive “fingerprints” depending on local field (type of magnet and location of RFA)
  Show good qualitative agreement with predictions of models for electron cloud build-up
  Show good quantitative agreement with EC model predictions in drift regions

## Slide 25: RFA Measurements: Drifts
  Broad distribution of electron flux
  Peak flux generally aligned with transverse position of passing bunches
  High flux of low-energy electrons
  Some electrons with KE > 250 eV
Collector current density vs transverse position
vs retarding voltage (Cu chamber, Ibeam ~ 56 mA)

## Slide 26: RFA Measurements: Dipoles
  Dipole field pins cloud electrons into trajectories that are vertically aligned with passing bunches
  Segmented RFAs show sharper peak aligned with transverse position of beam
Collector current density vs transverse position vs retarding voltage (Al chamber, Ibeam ~ 56 mA)

## Slide 27: RFA Measurements: Dipoles
  Dipole RFA’s show “bifurcation” at high beam current
  Cloud electrons receive bigger kicks from passing bunches as the beam current increases; impacting electron energies match peak in SEY curve (~300 eV) at larger transverse distances
Collector current density vs transverse position
vs beam current
(Al chamber)

## Slide 28: RFA Measurements: Quadrupoles
  Quadrupole field guides electrons along field lines
  Segmented RFAs show sharp peak in a single collector with high electron flux
  Electrons can remain trapped long after the bunch has passed
Collector current density
vs transverse position vs retarding voltage (Ibeam ~ 56 mA)

## Slide 29: Mitigations
RFA provide quantitative measure of effects of surface coatings for mitigation of electron cloud
Coated chambers
  TiN
  Amorphous C
  Diamond-like C
  NEG
Uncoated Al chambers have much higher flux
Drift RFA in 15E with
different
chambers

## Slide 30: Mitigations: Findings
Drifts
  Effective mitigation via coatings: TiN (SLAC), amorphous C (CERN), diamond-like C (KEK), or NEG (SAES)
Dipoles and quadrupoles
  Effective mitigation via coatings: TiN
  Even more effective if grooves + coatings
Wigglers
  Most effective mitigation: clearing electrode

## Slide 31: Quantitative Analysis of RFA Data
  RFA measurements provide data for validation of models for electron cloud build-up
  Models require parameters describing surface phenomena: photon reflectivity, electron photo-emission, electron secondary emission
  This is a major aspect of the CesrTA RFA program. More info in Phase I Report and papers

## Slide 32: Quantitative Analysis of RFA Data
Model for SEY vs energy and angle of incident electron
Inc. angle = normal
δts
δred
δ0
Ets
Selected electron cloud model parameters
QE = quantum efficiency
(electron photo-emission)

## Slide 33: Quantitative Analysis: Example
  Beam conditions used for one round of fitting
  EC model parameters which are sensitive to conditions are shown

## Slide 34: Quantitative Analysis: Example
Best fit parameters: TiN-coated chamber in 15W
EC model parameters are adjusted for best fit to RFA measurements, using large data set with different beam conditions
Uncertainty estimates do not take into account correlations within the model

## Slide 35: Quantitative Analysis of RFA Data
Ideal RFAs would provide electron flux as a function of energy
Real RFAs have complications
  They drain electrons from beam environment
  Secondaries are produced in beam pipe holes
  When retarding voltage is close to electron energy, the electrons are focussed
Work in progress
  Modelling of electron transport into RFAs
  Bench measurements with RFAs
Goal: proper interpretation of RFA data

## Slide 36: RFA Bench Measurements: Example
Beam from DC electron gun (135 mm away): 200 eV, 100 nA
RFA for bench measurements
3D RFA model

## Slide 37: Conclusion
CesrTA RFA program
  Large-scale deployment of RFAs and extensive measurements
  Providing quantitative information
    from different environments
    on the effect of mitigations
    for validation of electron cloud build up models
  Ultimate goals: help in the development of electron cloud models with predictive capability