Status and Plans for
Time-Resolved Measurements of Electron Cloud Buildup
What have we learned?
What questions remain?
What is the plan to address these questions?
-- Instrumentation -- Measurements -- Analysis
Jim Crittenden, with John Sikora and Yulin Li
CESRTA General Meeting
28 March 2014

---
What have we learned from
time-resolved measurements of cloud buildup?
Shielded Button Detectors
Witness-bunch studies with positrons provide sensitivity to the individual physical parameters governing cloud buildup
Photoelectron yield and energy distributions can be analyzed by varying bunch current
Differentiate between secondary emission processes. Sensitivity to cloud kinetic energy.
Cloud lifetimes for various mitigation techniques. Al, TiN, aC (2), DLC.
Dependence of photoelectron production and secondary emission on beam conditioning
Measurements with solenoidal magnetic field are very sensitive to the azimuthal dependence of photoelectron production rate and energy distribution.
Time-resolved Retarding Field Analyzers
Ten-bunch positron trains with 8 mA/bunch provide comparisons of secondary emission properties
Grounding/noise problems solved
Effective time resolution of 25 ns
Comparison of cloud buildup with uncoated Al, TiN-coated Al, with and without grooves.
Measurement of the SEY mitigation provided by grooves in storage ring operation
Shielded Stripline Detectors in Q48W
Comparison of signals from ten- and twenty-bunch trains provide good sensitivity to cloud trapping
First measurement of cloud trapping in a positron storage ring
Intermediate trains and bunches provide a clearing effect
Signals are dominated by secondary emission properties of stainless steel

---
What questions remain?
Shielded Button Detectors
Need to understand measurements with an electron beam.
Model predicts a large prompt signal which is not observed
Essential for present and future light sources
Need improved modeling for buildup in solenoid field, PEY, 2.1 GeV, 4 GeV
More detailed cross calibration with other measurement techniques, such as TE-wave and RFAs
Time-resolved Retarding Field Analyzers
Measure PEY properties of the Al, TiN and grooved surfaces at lower bunch current
Use two-bunch studies to differentiate SEY properties such as cloud lifetime
How does the dipole magnetic field influence the cloud buildup and mitigation?
Measure resonant effects by varying bunch spacing and scanning B field in small steps
Characterize cloud kinetic energy using the retarding field
Shielded Stripline Detectors in Q48W
Measure dependence of cloud trapping on train length and bunch spacing (April 2014)
Use bunch current dependence to further constrain SEY properties
Characterize cloud in fringe field
Is there trapping with an electron beam?
Use validated model to estimate trapping effects in the ILC positron damping ring (PRL)

---
-- Instrumentation and Measurements --
Phase III Proposal
Move the chicane assembly to a region of the CESR ring with higher photon rates
The chicane is 2.54 m long. Between BPMs 13W and 14W, 5.1m are occupied by 4 RFAs. Between BPMs 14E and 13E, 5.9m are occupied by 4 RFAs and doglegs.
In L3, the photon rate [Ecritical] for e+(e-) is 0.07-0.12 (0.034-0.044) g/m/e [2.3 (2.3) keV]
At 15E, the photon rate [Ecritical] for e+(e-) is 0.45 (1.0) g/m/e [3.7 (5.6) keV]
At 15W, the photon rate [Ecritical] for e+(e-)is 0.8 (0.6) g/m/e [5.6 (3.7) keV]
By increasing the photon rate by a factor of 10 to 30, witness bunch studies at lower bunch current would be made possible, giving differential sensitivity to PEY and the SEY processes
Other v.c. materials could also be tested in these variable dipole fields
Stainless steel for comparison and systematic check of cloud trapping model
Amorphous carbon (different!). Cu (common). Any newly proposed mitigation techniques
Design and install a shielded stripline in an arc quadrupole. Vary field strength. e- beam.
Second-generation designs for time-resolved RFAs and shielded striplines
This may take the form of developing filtering techniques (hardware/software)

---
-- Instrumentation and Measurements --
Additional Ideas
Intentional design of TE-wave resonators and detectors in chicane region for cross-calibration with the time-resolved RFAs, as opposed to serendipity/opportunism
Install shielded button detectors in round flanges at 45 and 180 degrees
If dedicated, tunable X-ray beam: shielded pickups and solenoids for PEY, slotted antechamber with floating stripline. Is E-line available?

---
-- Analysis --
Two Examples of Many ...
The measurements of shielded button signals with solenoidal magnetic field have been understood to depend on the detailed 2D distribution of photoelectron production energy and azimuth (Jared G.)
The present model is crude and inflexible: energy distributions can be defined only for direct and reflected photons separately.
The necessary flexibility is easy to code.
The optimal 2D distribution can be obtained from a single ECLOUD run by using weights which match the modeled to the measured signal in each time bin.
The potential payoff is enormous.
Quantitative validation of Synrad3D models
Information more detailed than XPS (1981 Nobel for Kai Siegbahn's work in the 1960's)
Make use of two recent major advances in the analysis of the TR_RFA measurements
Quantitative understanding of the shielding hole transmission for an axial magnetic field
Corrected L3 vacuum chamber model with major change in Synrad3D result
Only presentation of results at present is IPAC13. Restricted to SEY of uncoated grooves.
Phase II served to demonstrate many novel methodological concepts.
They have yet to be exploited.