First Results on the Diamond-like Carbon Mitigation Technique
From Shielded-Pickup Measurements
– Measurements recorded yesterday evening --
Jim Crittenden & John Sikora
Cornell Laboratory for Accelerator-Based Sciences and Education
CesrTA General Meeting
8 April 2011

---
How the Witness-bunch Method Works
Example: 15W, Al v.c., 2.1 GeV, 3 mA/bunch e+ beam, 4-ns spacing
Superposition of 15 such traces
illustrating the sensitivity to cloud lifetime
Shielded pickup scope trace for two bunches
44 ns apart
The witness bunch signal includes the single-bunch signal as well as the the signal
produced by cloud electrons accelerated into the shielded pickup by the kick from the witness bunch.

---
 Model Sensitivity to Secondary Electron Yield Parameters
3/27/10: 15E, TiN, 5.3 GeV, 5 mA/bunch e+ beam, 14-ns spacing
This example of ECLOUD simulations shows a preferred value for the elastic yield in a TiN-coated v.c. of d0=0.05.
A similar value was found for amorphous carbon coating (two different custom v.c.), while the value for bare Al was 0.75.

---
 First Results for Diamond-like Carbon Coating
4/7/11: 15E, DLC, 5.3 GeV, 5 mA/bunch e+ beam, 14-ns spacing
The diamond-like carbon coating exhibits significantly lower values for the quantum efficiency for producing
photoelectrons as well as lower secondary yield, both for the true secondary process and the elastic process.