Detailed Characterization of Vacuum Chamber Surface Properties
Using Measurements of the Time Dependence of Electron Cloud Development
Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
 CESRTA Advisory Committee
29 August 2012

---
EC Buildup Detectors at CESRTA
L3 Electron cloud experimental region
PEP-II EC Hardware:
Chicane, SEY station
Four time-resolved RFA's
Drift and quadrupole diagnostic chambers
New electron cloud experimental regions in arcs
(after 6 wigglers moved to L0 straight)
Locations for collaborator experimental
vacuum chambers
Custom vacuum chambers with shielded pickup detectors
Uncoated aluminum, and TiN, amorphous carbon, diamond-like carbon coatings
30 RFA's in drift regions, dipoles, quadrupoles, and wigglers

---
Shielded Pickup Design and Readout
10 kW
Bias +50 V
0.76 mm
diameter
8-bit
digitizing
oscilloscope
2 mm
X 100
0.1 µF
50 W
Detail
The pickup electrodes are shielded by the vacuum chamber hole pattern against the beam-induced signal.
The positive bias ensures that secondaries produced on the electrode do not escape.

---
Witness Bunch Method for Constraining Model Parameters
Example : 5/9/2010 2.1 GeV e+ 3 mA/bunch Al v.c. 15W
Shielded pickup scope trace
for two bunches 44 ns apart
Superposition of 15 such traces
illustrating the sensitivity to cloud lifetime
Leading bunch signal
from photoelectrons
produced on the bottom
of the vacuum chamber
Witness bunch signal
includes in addition cloud
electrons, mostly secondaries,
accelerated into the detector
by the beam.
The single bunch signal arises from photoelectrons produced on the bottom of the vacuum chamber.
Its shape is closely related to the photoelectron kinetic energy distribution and the beam kick.
The witness bunch signal includes the single-bunch signal as well as the that produced by cloud particles accelerated into the shielded pickup by the kick from the witness bunch. The witness signal is therefore sensitive to SEY.

---
Electron cloud buildup modeling code
ECLOUD
* Originated at CERN in the late 1990's
* Widespread application for PS, SPS, LHC, KEK, RHIC, ILC ...
* Under active development at Cornell since 2008
* Successful modeling of CESRTA tune shift measurements
* Interactive shielded pickup model implemented in 2010
* Full POSINST SEY functions added as option 2010-2012
* Flexible photoelectron energy distributions added 2011
* Synrad3D photon absorption distribution added 2011
Cloud snapshot after 14 ns
Generation of photoelectrons
Production energy, angle
Azimuthal distribution (v.c. reflectivity)
Time-sliced cloud dynamics
Cloud space charge force
Beam kick
Magnetic fields
Secondary yield model
True secondaries (yields > 1!)
Rediffused secondaries (high energy)
Elastic reflection (dominates at low energy)
Shielded pickup model
Acceptance vs incident angle, energy
Signal charge removed from cloud
Non-signal charge creates secondaries

---
Modeled photelectron
kinetic energy distribution
Two Power-Law Contributions
F(E) = E P1 / ( 1 + E/E0 ) P2
E0 = Epeak (P2-P1)/P1
This level of modeling accuracy was achieved with the photoelectron energy distribution shown below, using a sum of two power law distributions.
Epeak= 80 eV P1= 4 P2= 8.4
The high-energy component (22%) has a peak energy of 80 eV and an asymptotic power of 4.4. Its contribution to the signal is shown as yellow circles in the lower left plot.
Epeak= 4 eV P1= 4 P2= 6
The low-energy component (78%) has a peak energy of 4 eV and an asymptotic power of 2. It's contribution to the signal is shown as pink triangles.
Electron Cloud Buildup Models and Plans at CESRTA
JAC et al, LCWS11
Recent Developments in Modeling Time-resolved Shielded-pickup Measurements
of Electron Cloud Buildup at CESRTA
JAC et al, IPAC11

---
Modeled secondary electron
kinetic energy distributions
Probabilistic Model for the Simulation of Secondary Electron Emission
M.A.Furman and M.F.F.Pivi, Phys. Rev. ST-AB 5, 124404 (2002)
Can Low-Energy electrons Affect High-Energy Particle Accelerators?
R.Cimino, et al, Physical Review Letters, Vol. 93, Nr. 1, 014801 (2004)
The time development of the cloud is directly dependent on secondary kinetic energies and therefore on the relative probabilities of the three secondary production processes.

---
Constraints on kinetic energy distribution of secondary electrons
f(Esec) ~ Esec exp (-Esec/ESEY )
Recent Developments in Modeling Time-resolved Shielded-pickup Measurements
of Electron Cloud Buildup at CESRTA
JAC et al, IPAC11
The CESRTA Test Accelerator Electron Cloud Research Program Phase 1 Report
M.A.Palmer et al, August, 2012
Electron Cloud Buildup Models and Plans at CESRTA
JAC et al, LCWS11
The pulse shape for the 14-ns witness bunch signal sets a lower bound on the model parameter ESEY.

---
Evolution of cloud profile prior to each bunch passage
Prior to 14-ns bunch
Prior to 28-ns bunch
Prior to 84-ns bunch
Determines the shielded-pickup signal shape and size.

---
Beam conditioning effects on
an amorphous carbon coating
Recent Developments in Modeling Time-resolved Shielded-pickup Measurements
of Electron Cloud Buildup at CESRTA
JAC et al, IPAC11
Time-resolved Shielded-pickup Measurements and Modeling of
Beam Conditioning Effects on Electron Cloud Buildup at CESRTA
JAC et al, IPAC12
The beam conditioning effect for an amorphous carbon coating is primarily in quantum efficiency in both the
early and late conditioning process.

---
Vacuum Chamber Comparison Under Same Beam Conditions
5.3 GeV Positron Beam
Witness bunch with 14-ns spacing
Both the quantum efficiency and secondary yield for the TiN coating is remarkably stable over this range of beam conditioning.
The reproducibility of the measurement is at the level of a few percent after two months.

---
Witness Bunch Study for Uncoated Aluminum 5/17/2010
15W 5.3 GeV 3 mA/bunch e+ 4-ns spacing
2010 model now updated to use Synrad3D results and
vacuum chamber profile with vertical side walls
Sensitivity to value for elastic yield.

---
Discriminating between the true and rediffused
secondary yield processes
The rediffused secondary yield process determines the trailing edge of the signal from a single bunch.
This trailing edge is insensitive to d0 .
The late witness bunch signal used to determine d0 is also sensitive to the rediffused yield process.
The witness bunch method provides discriminating power between the true and rediffused processes.

---
Witness Bunch Study for TiN-coated Aluminum
Compare today's measurements to those of 6/18/2011
15W 5.3 GeV 5 mA/bunch e+ 14-ns spacing
Present best model for 6/18/11
Same model with 8/22/12 measurements
on unconditioned TiN
Initial indication is the the quantum efficiency is similar, but there is much more cloud due to SEY.

---
Witness Bunch Study for TiN-coated Aluminum
Compare recent measurements to those of 6/18/2011
15W 5.3 GeV 5 mA/bunch e+ 28-ns spacing

---
Shielded-pickup Witness Bunch Measurement Program
2010 - present
2.1, 4.0, and 5.3 GeV
Electron and positron beams
1-10 mA/bunch
Uncoated aluminum
TiN-coated aluminum
Two amorphous-carbon coatings
Diamond-like carbon coating
Unconditioned uncoated aluminum
Unconditioned TiN coating
Unconditioned a-carbon coating
4-ns, 14-ns bunch spacings up to 140 ns

---
Vacuum Chamber Comparison Under Same Beam Conditions
5.3 GeV Positron Beam
Witness bunch with 28-ns spacing
15W
15E
5 mA/bunch
The a-carbon coating
suppresses high-energy
photoelectrons compared to the TiN coating.
The results for the second
a-carbon-coated chamber
corroborate the high-energy photoelectron
suppression relative
to TiN observed with the
first a-carbon-coated chamber.
The quantum efficiency for reflected photons and the SEY are both much smaller for the TiN coating compared to uncoated aluminum.
3 mA/bunch
The second
carbon-coated chamber
shows conditioning effects between 5/17/10 and 12/24/10 , primarily for the quantum efficiency.