Time-Resolved Retarding Field Analyzer Measurements & Modeling:
-- SEY Mitigation Effectiveness of Grooves in Uncoated Aluminum --
-- Recent Measurements of Cloud Buildup with Dipole Field
John Sikora and Jim Crittenden
Cornell Laboratory for Accelerator-Based Sciences and Education
 CESRTA General Meeting
26 April 2013

---
Updated figure for effectiveness of grooves
5.3 GeV e+ 10 bunch train 8 mA/bunch
In contrast to the modeling studies for the shielded pickup data with SEY-mitigating coatings, the photoelectron production model is unchanged in the time-resolved RFA experiments, since the photoelectron production is predominantly at the primary photon impact point on the outside of the vacuum chamber.
This example comparison shows the sensitivity to the peak secondary yield to be better than 10%.
This determination of the effective SEY value for grooves should instruct our upcoming publication on the electron cloud buildup analysis for the ILC damping ring. However, in that design we recommend TiN-coated grooves.

---
More cloud buildup information
Before RC time constant
Cloud density
Dramatic signal fluctuations are smoothed out by the TR-RFA time resolution
Cloud increases and decreases between bunch passages. Saturates at 3e12 e/m3.

---
Compare Al and TiN
with and without grooves
0 Gauss
810 Gauss
In spite of beam noise and ringing, the reduction of cloud with TiN grooves is clear.