# A  DATABASE  OF

ELECTRON-SOLID INTERACTIONS

Compiled by

David C Joy

EM Facility, University of Tennessee, and

Oak Ridge National Laboratory

Revision # 04-02

## For comments, errata, and suggestions please contact me at djoy@utk.edu

# This compilation is  © David C Joy  April  2004

A DATA BASE ON ELECTRON-SOLID INTERACTIONS

David C Joy

EM Facility, University of Tennessee,

Knoxville, TN 37996-0810

and

Oak Ridge National Laboratory,

Oak Ridge, TN 37831-6064

Abstract

A  collection  of data comprising  secondary  and    backscattered  electron    yields,   measurements of  electron  stopping powers, and X-ray ionization cross-sections,     has been assembled from published sources. Values are provided for both elements and many compounds although the quality and quantity of the  available data varies widely  from one material to another. These compilations  provide the basic framework for understanding and interpreting electron beam images in a quantitative way -  as is required  for example in semiconductor device metrology - and also form a comprehensive source of experimental data for testing analytical and Monte Carlo models of electron beam interactions.

Introduction

1997 marks the one hundredth anniversary of the discovery of the electron. Within a year of that event  Starke (1898)  in Germany, and  Campbell-Swinton (1899) in England, independently showed that electrons were backscattered from solid specimens and  so made  the  first  quantitative  measurements  of  the  interaction  of  electrons with material. Over the  century since then many dozens of papers have been published that contain information on  various   aspects  of  electron-solid    interactions. Unfortunately no  systematic collections of the results of  such  investigations appear to be available for any part of the field of electron microscopy and  microanalysis.  As a  result,  anyone requiring   a specific piece of data  - such as the backscattering yield of molybdenum at 15keV, or the secondary electron  yield from  gallium arsenide at  3keV  to  take two  random examples -  has no option but to search the literature in the hope of finding a value which must then, in the absence of  any other comparable evidence, be taken as correct. What is required is a source which collects and collates all the values available so as to provide the user with not only a value, but some indication as to its likely reliability

Structure of the data base

The  database  presented  here  is  an  attempt  to present  as complete a survey as possible  of  the  published  results  on   backscattering yields, secondary electron  yields,  stopping  powers,  X-ray ionization cross-sections, and  fluorescent yields. Computer-aided  literature searches  have been conducted to try and  find  all   published references   in this general area for the period from 1898 to the present day. Clearly no claim can be made as the completeness of any such search, and   it is perhaps to be hoped that some major body  of work has been overlooked  because, as discussed below, there   are otherwise major omissions in the materials available.

The rules for the data  included in this collection are simple:

(a)  only experimental  results  are included.  Values that  are  not  specifically   indicated   by  the   author(s)   as  being   experimental,  or  values  that  are   clearly  the  result  of

interpolation,  extrapolation,  or  curve  fitting,  have  been    expunged.

(b)  no  attempt  has   been  made  to  critically  assess   the  accuracy  or  precision of the data, nor to remove any results on the basis of their presumed quality.

(c)  values  have  been  tabulated  primarily  for  the   energy  range up to 30keV, although data points  for incident energies  up to 100keV have been included where they are available.

The decision not  to engage in any  judgment of the quality  of  any of the sets of results may seem to be a significant drawback to the utility of the database. However, until so much data has been collated for each element or compound that  rogue values can infallibly  be distinguished and eliminated, there  is no criterion on  which to reject any particular result. Further it is conceivable that two  tabulated  values  of a  given  parameter  may  differ  substantially and yet still both be of value. This is because of  an inherent contradiction in the nature of the measurements that are being made. A measurement made in a UHV electron scattering  machine with in situ sample cleaning and baking facilities will  naturally be more 'reliable'  than a measurement  made inside a  typical scanning electron microscope. But the values recorded in  the microscope are more  'representative' of the conditions  usually employed on a day to  day basis  in an e-beam tool than those obtained  in the  environment of  a specialist  instrument. All  types of  results are, therefore, reported so  that users of the database  can  make  their  own  judgment  as  to  the  suitability,  or   otherwise,  of any given piece of information.

The  database  currently  contains  several thousand  individual   values collected  from  more than one hundred  published  papers  and reports  spanning the period from 1898 to the present day. Since this is a 'work  in  progress'   the  compilation   is  constantly  being   extended as  additional  values  become  available.  As  far as   possible a consistent style of presentation is used so that data  for different  elements and compounds may  readily  be compared. All of the available data sets are grouped by element or compound name for each of the major information groups (SE yields, BSE yields, Stopping Powers, X-ray ionization cross-sections). The data is presented in a simple two column format with the origin of  each of the data sets (numbered #1 to #n) indicated by a number  in parenthesis referring back to the bibliography.

Backscattered Electrons

The  data on the backscattered electron  (BSE) yield as a function of the atomic number of the target and of the incident beam energy is of particular importance in Monte Carlo computations because it  provides the best  test of the  scattering models that are used in the simulation. This data is  therefore both the starting point for the construction of a Monte Carlo model,  and  the  source  of  values  against  which  the  simulation can  be tested.  The backscattered  electron section  contains data for  forty or more elements  spread across  the periodic  table, as well as for a selection of compounds. If  Castaing’s rule can be assumed to be correct then the backscattering yield of a compound can be found if the backscattering coefficients and the atomic fraction of the elements that form it  are known. Hence a desirable long term goal is to obtain a complete set of BSE yield curves for elements. At present the  BSE section  contains information  on more  than  45 elements which is  barely  half  of  the  solid  elements in the periodic table, and of this number perhaps only  25%  of the data sets are   of the highest quality,  so much experimental work remains to be done especially at the lower energies.

Secondary Yields

With  the increasing  interest  in the  simulation of  secondary  electron (SE) line profiles and images  there is a need to have   detailed information on secondary electron yields as a function   of atomic number  and incident  beam energy.  Secondary electron   emission was the  subject of  intense experimental  study for a   period of twenty years or more from the early 1930s, resulting in  the publication of  no less than  six full length  books on the  topic. This effort did not, however, produce as much experimental  data as would have been expected because the aim of much of the  work that was done was to  demonstrate that the SE yield versus  energy curve followed a  "universal law" (Seiler  1984), and to  find the parameters describing  this curve. As  a result the data   actually published was usually given in a normalized format that makes it  difficult  to derive  absolute  values.  The database  currently contains yields for about 40 or elements, and a collection of  inorganic compounds  and  polymers.

The clear  discrepancies that often exist between  the  comparable sets of  original yield  figures for the same material may  be the  result  of surface  contamination,  or the   result of a different assumption  about the appropriate emitted  energy range for secondary electrons (usually now taken to be 0  to 50eV, although in some early work 0 to 70 or even 0 to 100eV  was used). In  addition, since many of the  materials  documented are poorly conducting the effects of charging must also  be considered.  For example,  in  studies of  the  oxides (e.g.  Whetten and  Laponsky  1957)  maximum SE  yields  of  >10 were  measured using  pulsed  electron-beam  techniques.  Clearly  no   non-conducting material can sustain this  level of emission for   any significant period of time, since it will become positively   charged and recollect its own  secondaries. Similarly at higher  energies, where the SE yield  <1 and negative charging occurs,  the incident  beam energy  must  be corrected  for  any negative surface  potential acquired  by  the  sample  to give  a  correct result (although there is no little evidence in the original papers that  this has  been  done).  Consequently all  SE  yield  results for   insulators must be treated with caution unless the provenance of the original data is well documented.

Since there is no sum rule for secondary yields, data must be acquired for every compound of interest over the energy range required, a task which will be a lengthy one unless suitably automated procedures can be developed and applied. In addition it will be necessary to repeat many  of the   measurements  reported here using  better techniques  before any level of precision and accuracy can be obtained. In summary  the SE  data is  in an even  less  satisfactory state  than that for the BS electrons, even though a wider range of materials is covered, because the quality of much of the data is poor..

Stopping Powers

The stopping power of  an electron in a  solid, i.e. the rate  at which the electron transfers its energy to the material through  which it is passing, is a quantity of the highest importance for  all studies of electron-solid  interactions since it determines  among other parameters the electron range (Bethe 1930), the rate of secondary  electron  production  (Bethe  1941),  the lateral  distribution and the distribution in depth of X-ray production,

and the  generation  and distribution  of  electron-hole pairs.   Despite  its  importance  there  is  no  body  of  experimental   measurements of stopping power at those energies of interest to  electron microscopy and microanalysis. Instead stopping powers,   and the quantities which  depend on them,  have been deduced by   analyzing measurements of  the transmission  energy spectrum of  MeV-energy -particles to yield a value for the mean ionization  potential I of the specimen  (ICRU 1983), and then Bethe's  (1930) analytical expression for the stopping power has been invoked to compute the stopping power at the  energy of interest.  While this  procedure is of   acceptable accuracy at high energies  (>10keV) it is not reliable at lower energies because some of the interactions included in the value of  I (e.g. inner shell  ionizations)  no longer   contribute.

The   database  contains   experimentally  determined   stopping    power curves for a collection of elements and compounds. The method for  obtaining this information from electron energy loss spectra has been described elsewhere (Luo et al 1991). The data is plotted in units of eV/Å  as a  function of the incident  energy in keV. At  the high energy end of the profiles the data corresponds closely to values deduced from Bethe's (1930) law and using the I-values from the ICRU  tables. At lower  energies, however, significant  deviations  occur  as   the  Bethe   model  becomes  physically    unrealistic although good agreement has  been found with values   computed from a  dielectric model of  the solids  (Ashley et al  1979).

The stopping power of a compound is the weighted sum of the stopping power of its constituents, thus a key priority  for future work should be to complete the set of stopping power profiles for elements   rather than to acquire more data on compounds.

X-ray Ionization Cross-Sections

Measured  values  of  the  X-ray  ionization cross-sections  for   various elements and emission  lines as a  function of incident  beam energy  are  also of  great  importance  in microanalysis.  Unfortunately, as a brief study of the graphs included here will  show, the amount of data available  is small for K-shells, negligible for the L-shells, and all but non-existent for the M- and higher shells.  This  is  the result  of  pervasive  experimental  difficulties, in  particular the fact that any   measurement   couples together  the ionization  cross-section and the  fluorescent yield . Since, as can be seen from the plots in section 5 of the data-base,  the  value  of the fluorescent yield    is poorly known for the L- and M-shells  this causes a significant degree in uncertainty in the cross-section deduced from this data.  A more practically useful approach is, instead, to quote an ‘X-ray generation’ cross-section which is the product of the ionization cross-section and the fluorescent yield  term. Because the fluorescent term is never required separately in X-ray microanalysis this result looses nothing of its generality but is much more robust. Future updates of this database will include results in this format. For completeness section 5 tabulates all the available fluorescent yield data for K,L, and M-shells.

Conclusions

This database is  a first  step towards the  goal of providing a comprehensive collection of the parameters which describe electron-solid interactions.  In  addition to  meeting the  needs  of those  working in  Monte Carlo modeling, it is  hoped that a systematic collection  of data such as  this may also  be of value   in experimental electron microscopy. The  quality and quantity of  the data that  has been amassed varies  widely from one material , and  from one topic, to another so that while a few elements can be considered as well characterized  the overall  situation is  poor  especially for materials used  in such  areas  as integrated  circuit device fabrication .

Acknowledgments

The original version of the database was  supported by the Semiconductor Research Corporation (SRC) under contract 96-LJ-413.001, contract monitor is Dr. D Herr, and by a grant from International SEMATECH.

References

Ashley J C, Tung C J, and Ritchie R H, (1979), Surf.Sci.81, 409

Bethe H A, (1930), Ann.Phys.5, 325

Bethe H A, (1941), Phys. Rev., 59, 940

Bishop H, (1966)), Ph.D Thesis University of Cambridge

Campbell-Swinton A A,  (1899), Proc.Roy.Soc., 64, 377

I.C.R.U., (1983),  "Stopping powers  of electrons  and positrons",   Report #37 to

International Committee on Radiation Units, (ICRU:Bethesda, MD)

Luo S, Zhang X, and Joy D C, (1991), Rad.Effects and Defects in  Solids, 117, 235

Seiler H, (1984), J.appl.Phys., 54, R1

Starke H, (1898), Ann.Phys., 66, 49

Whetten N R, and Laponsky  A B, (1957), J. appl. Phys., 28, 515

INDEX

Introduction									2

Index										9

Master reference list								10

Section 1 Secondary electron yields - 	(a) for elements		16

(b) for compounds		92

Section 2 Backscattered electron yields-	(a) for elements		131

(b) for compounds		208

Section 3 Electron stopping powers            (a) for elements		219

(b) for compounds		236

Section 4 X-ray ionization cross-sections					252

Section 5 X-ray fluorescent yields						299

Reference List

1. Hunger H-J Kuchler L, (1979), phys.stat.sol., (a) 56  , K45

2. Reimer L, Tolkamp C, (1980), Scanning 3, 35.

3. Moncrieff D A, Barker P R (1976), Scanning 1, 195

4. Bongeler R, Golla U, Kussens M, Reimer L, Schendler B, Senkel

R, Spranck M, (1993), Scanning  15, 1

5. Shimizu R, (1974), J. appl. Phys  45, 2107

6. Bishop H E, (1963),   Ph D Thesis, Cambridge

7. Philibert J and Weinryb E, (1963), Proc. 3rd Conf on X-ray Optics and Microanalysis

p163;  also E.Weinryb and J Philibert, (1964), C.R.Acad.Sci., 256, 4535

8. Heinrich K F J, (1966), Proc. 4th Conf. on X-ray Optics and Microanalysis, ed R

Castaing et  al , (Hermann:Paris), p159

9. Kanaya  K, Ono S, (1984), in "Electron Beam Interactions with Solids", ed D Kyser,

(SEM  Inc.:Chicago),  69-98

10. Dione G F, (1973), J. appl. Phys  44, 5361

11. Knoll, M (1935), Z. Tech. Phys. 16, 467

12. Bruining H (1942), "Die Sekundt-Elektronen Emission Fester Korper", Springer-

Verlag, Berlin

13. Neubert G and Rogaschewski S, (1980), phys. stat. sol. (a) 59, 35

14. Kanter M, (1961), Phys. Rev. 121, 1677

15. Drescher H, Reimer L and Seidel M, (1970), Z. angew. Physik  29, 331

16. Sommerkamp P, (1970), Z. angew Physik. 4, 202

17. Czaja W, (1966), J. appl. Phys  37, 4236

18. Whetten N R and Laponsky A B, (1957), J. appl. Phys  28, 515

19. Whetten N R, (1964), J. appl. Phys  35, 3279

20. Dawson P H (1966), J. appl. Phys 37, 3644. (Note that this SE  data  was taken for

energy  cutoffs varying from 30eV to 100eV).

21. Bruining H, and De Boer J M, (1938), Physica V, 17

22. Cosslett V E and Thomas R N (1965), Brit. J. Appl. Phys: J. Phys D 16, 774

23. Koshikawa T and Shimizu R, (1973), J. Phy. D. Appl. Phys. 6, 1369

24. Johnson J B and McKay K G (1954), Phys Rev. 93, 668

25. Dionne G F (1975), J. appl. Phys  46, 3347

26. Kanaya K and Kawakatsu M, (1972), J. Phys. D. Appl. Phys. 5, 1727

27. Hazelton R C, Yadlowsky E J, Churchill R J, and Parker L W, (1981), IEEE Trans.

on   Nucl.Sci., NS-28, 4541

28. Gross B, von Seggern H, Berraissoui A, (1983), IEEE Trans. on Electrical

Insulation,  EI-22, 23

29. Kishimoto Y, Ohshima T, Hashimoto H, Hayashi T, (1990), J .appl.Polymer Sci.,

39, 2055

30. Matskevich T L, (1959), Fiz. Tvend. Tela. Acad.Nauk. SSSR., 1, 227

31. Kazantsev A P, Matskevich T L, (1965), Sov.Phys.Sol.State, 6,  1898

32. Willis R F, and Skinner R F, (1973), Solid State Comm., 13,  685

33. Gair S, quoted in Burke EA, (1980), IEEE Trans. on Nucl.Sci., NS-27, 1760

34. Sternglass E.J., (1954), Phys.Rev., 95, 345

35. Palluel P, (1947), Compt. Rendu  224, 1492

36. Clark E, (1935), Phys.Rev., 48, 30

37. Tawara H, Harison KG, and De Heer FJ, (1973), Physica 63, 351

38. Hink W, and Pashke H, (1971), Phys.Rev., A4, 507; also Hink W

and Pashke H, (1971), Z.Phys., 244, 140

39.  Isaacson M, (1972), J.Chem.Phys., 56, 1813

40. Colliex P C, and Jouffrey B,(1972), Phil.Mag. 25, 491

41. Egerton R F, (1975), Phil.Mag., 31, 199

- Glupe G and Melhorne W, (1971), J.Physique Suppl.32 C4 - 40;  also Glupe G and

Melhorne  W, (1967), Phys.Lett. 25A, 274

43. Shima K, Nakagawa T, Umetani K, and Fikumo T, (1981), Phys.Rev., A24, 72

44. Davis D V, Mistry VD, Quarles C A, (1972), Phys.Lett., 38A, 169

45. Platton H, Schiwietz G, and Nolte G, (1985), Phys,Lett  107A, 83

46. Fitting H-J, (1974), Phys.Stat.Sol., (a)26, 525

47. Luo S, Zhang X, and Joy DC, (1991), Rad.Eff. and Defects in  Solids, 117, 235

48. Sorenson H, (1977), J.appl.Phys., 48, 2244

49. Kurrelmeyer B, and Hayner L J, (1937), Phys.Rev.,52, 952

50. Kamiya M, Kuwako A, Ishii K, Morita S, and Oyamada M, (1980),  Phys.Rev.,

A22, 413

51. McDonald S C, and Spicer B M, (1988), Phys.Rev. A37, 985

52. Hoffman D H H, Brendel C., Genz H, Low W, Muller S, and Richter A, (1979),

Z.Phys.,  A293, 187; also -Hoffman D H H, Genz H, Low W, and  Richter   A,

(1978), Phys.Lett.,  65A, 304

53. Hink W, and Ziegler A, (1969), Z.Phys. 226, 222

54.  Luo S, Dunlap J R, and Joy D C, (1993), Proc.51st Ann.Meeting MSA,  ed G W

Bailey and  C L Rieder, (San  Francisco Press:San Francisco), 1188

55. Meyer F and Vrakking J J, (1973), Phys. Lett., 44A, 511; see  also Vrakking J J and

Meyer F, (1974), Phys.Rev. A 9, 1932

56. Hippler R, Sneed K, McGregor I, and Kleinpoppen H, (1982),  Z.Phys., A307, 83

57. Quarles C, and Semaan M, (1982), Phys.Rev., A26, 3147

58. Jessenberger J, and Hink W, (1975), Z.Phys., A275, 331

59. Shima K, (1980), Phys.Lett.,  , 237

60. Pockman LT, Webster DL, Kirkpatrick P, and Harworth K,  (1947), Phys.Rev.,

71, 330

61. Myers H P, (1952), Proc.Roy.Soc., 215,  329

62. Hubner H, Ilgen K, and Hoffman K-W, (1972), Z.Phys. 255, 269

63. Kiss K, Kalman G, Palinkas J, and Schlank B, (1981), Acta Phys.Hung., 50, 97

64. Salem S I, and Moreland L D, (1971), Phys.Lett., 37A, 161

65. Green M, (1964), Proc.Roy.Soc., 83, 435

66. Hansen H, and Flammersfeld A, (1966), Nucl.Phys. 79, 134

67. Smick A E, and Kirkpatrick P, (1945), Phys.Rev., 67, 153

68. Wittry D B, (1966), Proc. 4th Conf. on X-ray Optics and  Microanalysis, ed R

Castaing et  al , (Hermann:Paris), p168

69. Rothwell T.E., and Russell P.E., (1988), in "Microbeam Analysis -1988", ed

D.E.Newbury,  (San Francisco Press:San Francisco), 149

70. Whetten N.R., (1962), in "Methods in Experimental Physics",  (Academic

Press:NY),  IV

71. Green M, and Cosslett V.E., (1968), Brit.J.appl.Phys. (J.Phys.D), 1, 425

72. Sudarshan T S, (1976), IEEE Trans. on Electrical Insulation, EI-11, 32

73.  LaVerne J A, and Mozumder A, (1985), J.Phys.Chem. 89, 4219

74. Al-Ahmad K O. and Watt D E, (1983), J.Phys.D:Appl.Phys., 16,   2257

75.  Ishigure N, Mori C, and Watanabe T, (1978), J.Phys.Soc. Japan., 44, 973

76. Garber F W, Nakai M Y, Harter J A, and Birkhoff R D, (1971),  J.appl.Phys., 42,

1149

77. Luo S, (1994), Ph.D Thesis University of Tennessee

78. Kalil F, Stone W G, Hubell H H, and Birkhoff R D, (1959), ORNL Report 2731

79. Arifov U A, Khadzhimukhamedov Kh. Kh. and Makhmudov, (1971),  in "Secondary

Emission and Structural Properties of Solids", ed U A Arifov, (Consultants

Bureau:NY), 30

80. Arifov U A and Kasymov A Kh., (1971),, in "Secondary  Emission and Structural

Properties of Solids", ed U A Arifov, (Consultants   Bureau:NY), 78

81. Septier A and Belgarovi M, (1985), IEEE Trans. on Electrical Insulators, EI-20, 725

82. Ahearn A J, (1931), Phys.Rev., 38, 1858

83. Flinn E A and Salehi M, (1980), J.appl.Phys., 51, 3441

84. Flinn E A and Salehi M, (1979), J.appl.Phys., 50, 3674

85. Dunn B, Ooka K, and Mackenzie J D, (1973), J.Am.Cer.Soc., 56, 9

86. Joy D C, Joy C S,  SEMATECH Report  TT# 96063130A-TR, August 1996

87. Kaneff  W, (1960), Annalen der Physik, 7, 84

88. Petzel B, (1960), Annalen der Physik, 6, 55

89. Hovington P, Joy D C, Gauvin R, and Evans N, (1995),  unpublished data. For a

summary see Joy D C, Luo S, Gauvin R, Hovington P, and Evans N, (1996),

Scanning Microscopy  10, 653-666

90. Buhl. R, (1959), Zeit.f.Phys., 155; see also Keller, M,  (1961), Zeit.f.Phys.,

164, 274

91. Miyake S, (1938), Proc.Phys.Math.Soc. Japan  20, 280

92. Lashkarev V E, and Chaban A S, (1935), Phys.Z.Soviet  8, 240

93  Westbrook G L, and Quarles C A, (1987), Nucl.Instrum. and  Methods in Phys.Res.,

B24-25, 196

94. Motz J W and Placious R C, (1964), Phys.Rev.,  136,   662

95. Broyles C, Thomas D, and Haynes S, (1953), Phys. Rev. 89, 715

96. Lay H, (1934), Z.Physik 91, 533

97. Frey W F,  Johnston R E, Hopkins J I, (1958), Phys.Rev., 113, 1057

98.  Konstantinov A A, Sazonova T E, and Perepelkin V V, (1960), Izv. Akad.Nauk

SSSR, Ser.Fiz. 24, 1480; also from Konstantinov et al, (1961), Izv. Akad. Nauk

SSSR, Ser. Fiz. 25, 219;  Konstantinov et al, (1964), Izv. Akad. Nauk SSSR,

Ser. Fiz. 28, 107;  Konstantinov et al, (1965), Izv. Akad. Nauk SSSR, Ser. Fiz.

29, 302

99. Gray P R, (1956), Phys.Rev., 101, 1306

100. Data taken from miscellaneous references in Fink R W, Jopson R C, Mark H, and

Swift C D, (1966), Rev. Mod. Phys., 38, 513

101. Data taken from miscellaneous references in  Bambynek W, Crasemann B, Fink R

W, Freund H-U, Mark H, Swift C D, Price R E, and Rao P V, (1972),

Rev.Mod.Phys., 44, 716

102. Jopson R C, Mark H, Swift C D, (1962), Phys.Rev., 128, 2671

103. Sidhu N P S, Grewal B S, and Sahota H S, (1988), Xray Spectrometry  17, 29

104. Fischer B, and Hoffmann K-W, (1967), Z. fur Physik, 204, 122

105. Henrich V E, and Fan J C C, (1974), J. app. Phys., 45, 5484

106. Bronstein I M, and Fraiman B S, (1969), in “Vtorichnaya Elektronnaya Emissiya”,

(Nauka: Moskva), p340

107. El Gomati M M, and Assad A M D, (1997), Proc. 5th European Workshop on

Microbeam Analysis, (in press)

108. Rossouw C J, and Whelan M J, (1979), J.Phys.D. Appl.Phys., 12, 797

109. Allawadhi K L, Sood B S, Raj Mittal, Singh N, and Sharma J K, (1996), X-ray

Spectr. 25, 233

110. Horakeri L D, Hanumaiah B, and Thontadarya S R, (1997), X-ray Spectr. 26, 69

111. Mearini G T, Krainsky I L, Dayton J A, Wang X, Zorman C A, Angus J C,

Hoffman D F, and Anderson D F, (1995), Appl.Phys.Lett.,66, 242

112. Thomas S, and Pattinson E B, (1969), Brit.J.Appl.Phys., II-2, 1539

113. He F Q, Long X, Peng X, Luo Z, and An Z, (1997), in press Acta Physica Sinica

114. He F Q, Long X G, Peng X F, Luo Z M, and An Z, (1997) in press

115. Suszcynsky D M, Borovsky J E, and Goertz C K, (1992), J. Geophysical Res., 97,

2611

116.  Horakeri LD, Hanumaiah, and Thontadarya S R, (1998), X-ray Spectrometry 27,

344

117. An Z, Li  T H, Wang L M, Xia X Y, and Luo Z M, (1996), Phys.Rev.54, 3067

118. Luo Z, An Z, Li T, Wang  LM, Zhu Q, and Xia X, (1997),  J.Phys.B:

At.Mol.Opt.Phys. 30, 2681

119. Luo Z, An Z, He F, Li T, Long X, and Peng X, (1996), J.Phys.B: At.Mol.Opt.Phys.,

29, 4001

120. He F Q,   Peng X F, Long X G, Luo ZM, An Z,  (1997), Nucl. Instrum. and

Methods in Physical Research  B129, 445

121. Peng X, He F, Long X G, Luo ZM, An Z, (1998), Phys.Rev.A58, 2034

122. Thiel B, (1999), Personal communication. To be published in Microscopy and

Microanalysis

123. Llovet X, Merlet C, and salvat F, (2000), J.Phys.B:At.Mol.Opt.Phys. 33, 3761-3772

124. Schneider H, Tobehn I, Ebel F, and Hippler R, (1993), Phys.Rev.Lett. 71, 2707-

22709

125. An Z, Tang C H, Zhou C G, and Luo Z M, (2000), J.Phys.B:At.Mol.Opt.Phys. 33,

3677-3684

126. Llovet X, Merlet C, and Salvat F, J.Phys.B:At.Mol.Opt.Phys, 35,  973-982, (2001)

127. Hilleret N, Bojko J, Grobner O, Henrist B, Scheuerlein C, and Taborelli M, (2000),

"The secondary electron yield of technical materials and its Variation with surface

treatments" in Proc.7th European Particle Accelerator Conference, Vienna.

128.Campos CS, Vasconcellos M A Z, Llovet  X, and Salvat F, (2002), “Measurements

of L-shell X-ray production cross-sections of W, Pt, and Au by 10-30keV

electrons”, Phys. Rev. A, 66

129. Prasad M S, (2002), personal communication

130. Ushio Y, Banno T, Matuda N, Baba S, Kinbara A, (1988), Thin Solid Films 167,

299

131.  Ling Y, (2003), personal communication

132. Sim K-S, and Kamel N, (2003), “A new setup and measurement technique for

SNR”, Phys.Lett.A (in press)

SECTION ONE

Secondary Electron Yield Data

- for elements, arranged in ascending atomic number

- for compounds, sorted in alpha-numeric order

Hydrogen (solid) Z=1

Reference  (48)

E(keV)  	 SE yield

0.5000    	0.2640

0.8000   	 0.2080

1.0000    	0.1720

1.2000    	0.1560

1.5000    	0.1200

2.0500    	0.0960

2.9500    	0.0720

Data Set #2	Reference (127)     Sample is 75 monolayers of condensed H2 on copper

E(keV)		SE yield

  - 0.89

  - 0.93

  - 0.95

  - 0.89

  - 0.86

  - 0.79

  - 0.75

  - 0.73

  - 0.66

  - 0.61

  - 0.55

  - 0.52

  - 0.51

0.887		0.50

0.993		0.48

1.099		0.46

1.205		0.46

1.364		0.43

1.444		0.43

1.550		0.43

1.655		0.43

1.709		0.41

1.801		0.41

1.854		0.41

1.907		0.41

1.960		0.41

Lithium Z=3

Reference (21)

E(keV)  	SE yield

0.0500  	0.5000

0.1000  	0.5550

0.1500  	0.5400

0.2000  	0.5210

0.2500  	0.4860

0.3000  	0.4690

0.4000  	0.4170

0.5000  	0.3810

0.6000  	0.3470

Data Set #2       Reference (26)

E(keV)  	SE yield

0.14    		0.35

Data Set #3     Reference (70)

E(keV)  	SE yield

0.085   	 0.5

Beryllium Z=4

Reference (2)

E(keV)  	SE yield

1       		1.690

3       		0.77

5       		0.551

10     		0.245

20      		0.152

30     	 	0.079

Data Set  #2     Reference (5)

E(keV)  	SE yield

1       		1.745

2       		0.863

3       		0.596

4      		0.4706

5      		 0.392

6       		0.334

7       		0.298

8       		0.2666

9       		0.235

10     		0.196

Data Set  (3)    Reference 21

E(keV)  	SE yield

0.05    		0.386

0.1     		0.483

0.15    		0.617

0.2     		0.528

0.3     		0.5

0.4     		0.46

0.5     		0.42

0.6     		0.386

0.7     		0.353

0.8    		0.324

Data set  #4     Reference (26)

E(keV)  	SE yield

0.2     		0.6

Data set  #5     Reference (47)

E(keV)   	SE yield

0.02    		0.204

0.04    		0.814

0.06    		1.204

0.096   	1.74

0.14   		2.37

0.2     		2.89

0.3     		3.67

0.4     		4.07

0.5    		4.25

0.6     		4.31

Data Set  #6     Reference (70)

E(keV)  	SE yield

0.2     		0.5

Data Set #7      Reference (106)

E(keV)		SE yield

  - 0.44

  - 0.444

  - 0.447

  - 0.406

  - 0.348

  - 0.305

  - 0.263

  - 0.213

- 0.175

- 0.118

- 0.098

- 0.085

Boron  Z=5

Reference (9)

E(keV)    	SE yield

0.4000    	1.0000

0.6000    	1.0000

Data Set  #2      Reference (26)

E(keV)  	SE yield

0.301   	1.00

Data Set  #3      Reference (70)

E(keV)  	SE yield

0.05		1.00

0.15  		1.2

0.60		1.00

Data Set #4       Reference (106)

E(keV)		SE yield

  - 1.06

  - 1.10

  - 1.12

  - 1.11

  - 1.05

  - 0.95

  - 0.80

  - 0.66

  - 0.49

  - 0.40

Carbon Z=6

Reference (2)

E(keV)		SE yield

- 1.56

- 0.501

- 0.125

Data Set #2      Reference (3)

E(keV)		SE yield

  - 0.334

- 0.211

- 0.143

- 0.106

- 0.079

- 0.052

Data Set #3     Reference (4)

E(keV)		SE yield

  - 0.155

  - 1.136

- 0.990

  - 0.869

  - 0.709

  - 0.655

  - 0.595

- 0.527

  - 0.442

- 0.400

  - 0.316

- 0.316

- 0.315

Data Set #4     Reference (9)

E(keV)		SE yield

  - 1.00

Data Set #5      Reference (26)

E(keV)		SE yield

  - 0.90

Data Set #6      Reference  (68)

E(keV)		SE yield

5.0		0.177

5.0		0.164

- 0.067

- 0.05

Data Set #7     Reference (69)

E(keV)		SE yield

0.20		0.92

0.30		1.10

0.40		0.98

0.50		1.02

0.60		0.97

0.70		0.95

0.80		0.95

0.90		0.90

1.00		0.72

1.5		0.39

2.0		0.36

3.0		0.33

4.0		0.25

Data Set #8      Reference (106)

E(keV)		SE yield

0.10		0.709

0.20		0.82

0.30		0.85

0.40		0.824

0.60		0.745

0.80		0.656

1.00		0.543

2.0		0.308

3.0		0.209

Sodium  Z=11

Reference 70

E(keV)    	SE yield

0.3000    	0.8200

Magnesium  Z=12

Reference (21)

E(keV)   	SE yield

0.0250   	0.2240

0.05	   	0.5860

0.10	  	0.7930

0.20	   	0.9310

0.30	   	0.9660

0.40	   	0.9280

0.50	   	0.8280

0.60	   	0.8210

Data Set  #2      Reference  (26)

E(keV)  	SE yield

0.3     		0.80

Data set  #3       Reference (70)

E(keV)  	SE yield

0.3     		0.95

Data Set #4        Reference (106)

E(keV)		SE  yield

0.039		0.188

0.064		0.354

0.132		0.806

0.210		0.627

0.303		0.63

0.40		0.621

0.60		0.554

0.80		0.531

1.0		0.427

2.0		0.299

2.5		0.285

Aluminum Z=13

Reference (2)

E(keV)  	SE yield

1.0     		1.58

3.0     		1.00

5.0     		0.501

15.0   		0.184

20.0    		0.159

30.0    		0.096

Data set #2     Reference (3)

E(keV)  	SE yield

2.5     		0.658

5.0     		0.416

10.0    		0.264

20      		0.149

25.0    		0.137

Data set  #3     Reference (4)

E(keV)  	SE yield

0.513   	3.179

0.8     		2.44

1.0     		2.10

1.2     		1.93

1.4     		1.69

1.6     		1.613

1.8     		1.39

2.0     		1.32

2.5     		1.06

3.0     		0.959

3.5     		0.854

4.0     		0.752

5.0     		0.679

Data set  #4     Reference (5)

E(keV)  	SE yield

1.0     		1.666

2.0     		0.8823

3.0     		0.6196

4.0     		0.5059

5.0    		0.439

6.0     		0.353

7.0     		0.3137

8.0     		0.2745

9.0    		0.255

10.0    		0.2316

Data set #5      Reference (14)

E(keV)  	SE yield

2.0     		1.0

3.0     		0.73

4.0     		0.60

5.0    		0.53

6.0     		0.43

8.0     		0.37

10.0    		0.28

12.5    		0.24

15.0    		0.21

17.5    		0.18

20.0    		0.17

Data set #6      Reference (17)

E(keV)  	SE yield

10.0    		0.153

15.0    		0.265

20.0   		 0.10

25.0   		0.062

28.0    		0.0455

30.0    		0.0615

32.0    		0.0575

35.0    		0.047

40.0    		0.0395

Data set #7      Reference (7)

E(keV)  	SE yield

5.0     		0.252

Data set #8       Reference (21)

E(keV)  	SE yield

0.05    		1.0

0.1     		1.32

0.2     		1.93

0.3    		2.14

0.4    		2.17

0.5     		2.10

0.6     		1.98

Data set #9       Reference (26)

E(keV)  	SE yield

0.3     		0.9

Data set #10    Reference (68)

E(keV)  	SE yield

5.0     		0.419

30.0    		0.075

Data set #11    Reference (70)

E(keV)  	SE yield

0.3     		1.0

Data set #12     Reference (106)

E(keV)		SE yield

0.1		0.571

0.2		0.616

0.3		0.642

0.41		0.64

0.6		0.58

0.808		0.5

1.0		0.45

2.0		0.304

3.0		0.228

4.0		0.18

Data set #13	Reference (127)	99.5% pure as received

E(keV)		SE yield

0.05		1,55

0.06		1.72

0.08		2.01

0.10		2.27

0.15		2.77

0.2		3.13

0.25		3.33

0.3		3.44

0.4		3.45

0.5		3.32

0.8		2.76

1.0		2.44

1.2		2.19

1.5		1.89

1.95		1.58

Silicon Z=14

Reference (2)

E(keV)  	SE yield

1.0     		1.594

3.0    		0.769

5.0     		0.49

10.0    		0.3431

20.0    		0.216

30.0    		0.138

Data set #2        Reference (10)

E(keV)  	SE yield

0.22    		0.39

0.33    		0.59

0.55    		0.98

0.77    		0.95

1.10    		0.89

1.32    		0.84

1.65    		0.79

Data set #3      Reference (17)

E(keV)  	SE yield

10.0    		0.215

15.0    		0.136

20.0    		0.104

25.0    		0.081

30.0    		0.075

35.0    		0.072

40.0    		0.0584

Data set #4      Reference (25)

E(keV)  	SE yield

0.05    		0.604

0.1     		0.854

0.15    		1.01

0.2     		1.125

0.25    		1.146

0.3     		1.167

0.4     		1.167

0.5     		1.117

0.6     		1.083

0.7     		1.04

0.8     		1.00

0.9     		0.98

1.0     		0.937

Data set #5       Reference (26)

E(keV)  	SE yield

0.3     		0.85

Data set #6      Reference (68)

E(keV)  	SE yield

5.0     		0.326

5.0     		0.246

30.0    		0.097

30.0    		0.08

Data set #7      Reference (69)

E(keV)  	SE yield

0.2     		0.90

0.3     		0.69

0.5     		0.87

0.6     		0.72

0.7     		0.68

0.8     		0.66

0.9     		0.66

1.0     		0.6

1.1    		0.54

1.2     		0.56

1.3     		0.56

1.4     		0.52

1.5     		0.51

1.6     		0.4

1.7     		0.52

1.8     		0.28

1.9     		0.35

2.0     		0.43

2.2     		0.48

2.4     		0.31

2.6     		0.38

2.8     		0.29

3.0     		0.31

3.2     		0.29

3.4     		0.28

3.6     		0.28

3.8     		0.25

4.0     		0.25

4.5     		0.26

5.0     		0.24

Data set #8      Reference (70)

E(keV)  	SE yield

0.125   	1.0

0.25    		1.1

0.5     		1.0

Data set #9       Reference (106)

E(keV)		SE yield

0.2		0.748

0.3		0.740

0.4		0.735

0.6		0.607

0.8		0.523

1.0		0.44

2.0		0.273

3.0		0.194

4.0		0.15

Data Set #10	Reference (132)

E(keV)		SE yield

20		   0.14

Silicon (Z=14)  amorphous

Reference (86)

E(keV)  	SE yield

10.000  	0.185

7.000   	0.310

5.000   	0.367

4.000   	0.440

3.000   	0.530

2.000   	0.640

1.500   	0.790

1.000   	0.980

0.700   	1.220

0.500   	1.420

Phosphorus Z=15

Reference (70)

E(keV)   	SE yield

0.2000   	0.7000

Potassium (Z=19)

Reference (70)

E(keV)		SE yield

0.2		0.70

Data set #2       Reference (106)

E(keV)		SE yield

0.04		0.076

0.06		0.15

0.1		0.237

0.163		0.235

0.398		0.233

0.601		0.209

0.805		0.19

1.02		0.173

1.196		0.152

1.597		0.125

2.0		0.106

Calcium (Z=20)

Reference (106)

E(keV)		SE yield

0.05		0.214

0.1		0.32

0.15		0.376

0.2		0.36

0.3		0.34

0.4		0.257

0.6		0.216

0.8		0.19

1.2		0.154

2.0		0.132

Scandium Z=21

Reference (9)

E(keV)   	SE yield

0.3000   	0.7510

Data set #2      Reference (26)

E(keV)  	SE yield

0.3000  	0.7500

Data set #3      Reference (106)

E(keV)		SE yield

0.085		0.57

0.193		0.59

0.307		0.57

0.4		0.552

0.5		0.54

0.6		0.531

0.8		0.475

1.0		0.446

1.55		0.396

2		0.351

2.5		0.31

Titanium Z=22

Reference (68)

E(keV)    	SE yield

5.0000    	0.3420

5.0000    	0.2790

30.000    	0.1000

30.0000   	0.0870

Data set #2      Reference (70)

E(keV)  	SE yield

0.28    		1.0

Data set #3      Reference (86)

E(keV)  	SE yield

0.5     		0.768

0.8     		0.792

1.0     		0.820

1.5     		0.771

2.0     		0.645

3.0     		0.517

5.0     		0.410

7.0     		0.34

10.0    		0.29

25.0    		0.130

Data set #4      Reference (106)

E(keV)		SE yield

0.05		0.29

0.1		0.448

0.21		0.568

0.313		0.572

0.41		0.545

0.52		0.515

0.6		0.495

0.8		0.441

1.0		0.402

2.0		0.251

3.0		0.199

4.0		0.173

Data set #5	Reference (127)  as received

E(keV)		SE yield

0.05		1.15

0.08		1.46

0.1		1.61

0.15		1.83

0.2		1.92

0.25		1.94

0.3		1.92

0.4		1.83

0.5		1.73

0.75		1.50

1.00		1.34

1.5		1.13

1.95		0.99

Vanadium Z=23

Reference (68)

E(keV)   	SE yield

5.0000   	0.3500

3.0000   	0.2680

30.0000  	0.1040

30.000   	0.0890

Chromium Z=24

Reference (68)

E(keV)   	SE yield

5.0000   	0.3760

5.0000   	0.2960

30.0000  	0.1110

30.0000  	0.0960

Data set #2 	Reference (129)

E(keV)   	SE yield

| 8 |  | 0.42 |
| --- | --- | --- |
| 7 |  | 0.46 |
| 6 |  | 0.52 |
| 5 |  | 0.59 |
| 4 |  | 0.68 |
| 3 |  | 0.82 |
| 2 |  | 1.06 |
| 1 |  | 1.56 |
| 0.5 |  | 1.78 |
| 0.3 |  | 1.5 |
| 0.2 |  | 1.2 |
| 0.1 |  | 0.6 |

Iron Z=26

Reference (68)

E(keV)  	SE yield

5.0000   	0.3680

5.0000   	0.2710

30.0000  	0.1130

30.0000   	0.0970

Data set #2       Reference (70)

E(keV)  	SE yield

0.12    		1.0

0.4     		1.3

1.4     		1.0

Data set #3       Reference (106)

E(keV)		SE yield

0.05		0.293

0.075		0.464

0.1		0.66

0.2		0.98

0.3		1.065

0.4		1.083

0.6		0.98

0.8		0.946

1.0		0.870

1.2		0.8

1.5		0.704

Cobalt Z=27

Reference (70)

E(keV)   	SE yield

0.2000    	1.0000

0.6000    	1.2000

Nickel Z=28

Reference (11)

E(keV)  	SE yield

0.265   	0.97

0.954   	1.0

1.07    		0.92

Data set #2      Reference (26)

E(keV)  	SE yield

0.5     		1.3

Data set #3       Reference (47)

E(keV)  	SE yield

0.02    		0.970

0.038   	0.177

0.07    		0.381

0.095   	0.499

0.14    		0.672

0.2     		0.825

0.39    		1.158

0.50    		1.24

0.85    		1.33

1.08    		1.32

1.3     		1.28

1.55    		1.22

Data set #4       Reference (68)

E(keV)  	SE yield

5.0     		0.405

5.0     		0.299

30.0    		0.117

30.0    		0.106

Data set #5       Reference (70)

E(keV)  	SE yield

0.15    		1.00

0.55    		1.3

1.59   		 0.8

2.385   	0.66

3.18    		0.58

Data set #6     Reference (106)

E(keV)		SE yield

0.05		0.216

0.1		0.548

0.2		0.732

0.3		0.869

0.4		0.929

0.6		0.972

0.8		0.959

1.0		0.90

1.5		1.183

2.0		0.803

3.0		0.562

4.0		0.458

Data set #7      Reference (112)

E(keV)		SE yield

0.072		0.659

0.1		0.834

0.134		0.999

0.188		1.135

0.247		1.236

0.315		1.304

0.4		1.35

0.52		1.35

0.6		1.325

0.68		1.294

0.8		1.26

0.932		1.215

1.03		1.18

1.2		1.131

Copper Z=29

Reference (2)

E(keV)  	SE yield

1.0     		1.59

5.0     		0.69

20.0    		0.216

Data set #2      Reference (3)

E(keV)  	SE yield

2.5     		0.75

5.0     		0.478

10.0    		0.31

15.0    		0.224

20.0    		0.174

25.0   		0.161

Data set #3        Reference (4)

E(keV)  	SE yield

0.5     		2.11

0.8     		1.869

1.0     		1.723

1.2     		1.469

1.4     		1.44

1.6     		1.37

1.8     		1.194

2.0     		1.117

2.5     		1.04

3.0     		0.893

3.5     		0.813

4.0     		0.752

5.0     		0.641

Data set #4      Reference (5)

E(keV)  	SE yield

0.5     		1.009

1.0     		0.8922

1.5     		0.7255

2.0     		0.5882

3.0     		0.4216

4.0     		0.3255

5.0     		0.2745

6.0     		0.245

7.0     		0.2157

8.0     		0.1961

9.0     		0.1804

10.0    		0.1666

Data set #5      Reference (21)

E(keV)  	SE yield

0.05    		0.368

0.1     		0.701

0.2     		1.00

0.4     		1.23

0.6     		1.26

0.8     		1.276

1.0     		1.23

Data set #6       Reference (23)

E(keV)  	SE yield

0.5     		1.41

1.0     		1.328

2.0    		0.992

3.0    		0.813

4.0    		0.724

5.0    		0.649

6.0     		0.604

7.0     		0.567

8.0  		0.537

9.0   		0.522

10.0    		0.5

Data set #7      Reference (26)

E(keV)  	SE yield

0.55    		1.4

Data set #8      Reference (68)

E(keV)  	SE yield

5.0     		0.39

5.0     		0.291

30.0    		0.119

30.0   		0.105

Data set #9       Reference (70)

E(keV)  	SE yield

0.2     		1.0

0.6     		1.3

1.5     		1.0

Data set #10     Reference (81)

E(keV)    	SE yield

0.02      	1.118

0.06      	1.265

0.1       	1.442

0.175     	1.554

0.25      	1.573

0.3       	1.561

0.4       	1.492

0.5       	1.404

0.7       	1.277

1.0       	1.097

1.5       	0.925

2.0       	0.859

Data set #11     Reference (61)

E(keV)		SE yield

0.00015	0.09

0.0003		0.08

0.00078	0.071

0.0013		0.067

0.00226	0.063

0.003		0.066

0.004		0.075

0.005		0.082

0.006		0.089

0.007		0.105

0.008		0.129

0.009		0.167

0.01		0.215

Data set #12    Reference (106)

E(keV)		SE yield

0.1		0.564

0.19		0.716

0.3		0.846

0.4		0.933

0.6		1.024

0.8		1.034

1.02		0.993

1.5		0.881

2.02		0.771

2.5		0.702

3.0		0.61

4.0		0.498

Data set #13	Reference (127)	OFHC as received

E(keV)		SE yield

0.05		1.13

0.08		1.42

0.125		1.71

0.175		1.91

0.25		2.054

0.3		2.10

0.45		2.11

0.5		2.08

0.6		2.04

0.8		1.92

1.0		1.80

1.2		1.69

1.5		1.55

1.95		1.39

Data set #14	Reference (127)	heat treated 80 degrees C and below

E(keV)		SE yield

0.05		1.15

0.06		1.25

0.07		1.34

0.08		1.43

0.1		1.59

0.15		1.84

0.2		1.99

0.25		2.07

0.3		2.11

0.4		2.11

0.5		2.08

0.7		1.96

1.0		1.77

1.5		1.53

1.95		1.37

2.55		1.21

3.0		1.12

Zinc (Z=30)

Reference (106)

E(keV)		SE yield

0.108		0.591

0.131		0.647

0.166		0.670

0.2		0.690

0.3		0.854

0.4		0.923

0.6		1.003

0.8		1.023

1.0		1.001

1.462		0.913

2.0		0.821

3.0		0.743

4.0		0.52

Gallium  Z=31

Reference (70)

E(keV)  	SE yield

0.0750  	1.0000

0.5000  	1.5500

Data set #2      Reference (106)

E(keV)		SE yield

0.042		0.269

0.075		0.377

0.1		0.479

0.2		0.681

0.4		0.716

0.6		0.71

0.8		0.683

1.0		0.636

1.51		0.55

2.0		0.49

3.0		0.383

4.0		0.308

Germanium  Z=32

Reference (2)

E(keV)  	SE yield

1.0     		1.62

5.0    		 0.649

20.0   		0.228

Data set #2      Reference (24)

E(keV)  	SE yield

0.1000  	0.6800

0.2000  	0.9700

0.3000  	1.1000

0.4000 	1.1200

0.5000  	1.1420

0.6000  	1.0900

1.0000  	0.9560

1.2500  	0.8700

1.5000  	0.8000

1.7500  	0.7600

2.0000  	0.6960

2.5000  	0.5400

3.0000  	0.5300

3.5000  	0.4900

4.0000  	0.4500

4.5000  	0.4200

5.0000  	0.4200

Data set #3     Reference (26)

E(keV)  	SE yield

0.5     		1.3

Data set #4       Reference (70)

E(keV) 	 SE yield

0.15    		1.00

0.5     		1.15

0.9     		1.0

Data set #5       Reference (106)

E(keV)		SE yield

0.05		0.29

0.1		0.473

0.15		0.631

0.20		0.715

0.4		0.743

0.6		0.699

0.8		0.668

1.0		0.608

1.5		0.471

2.0		0.398

3.0		0.312

4.0		0.264

Selenium (Z=34)

Reference (106)

E(keV)		SE yield

0.048		0.59

0.073		0.692

0.102		0.798

0.159		0.834

0.214		0.862

0.316		0.849

0.409		0.798

0.611		0.728

0.808		0.686

1.0		0.647

1.532		0.545

2.0		0.489

3.0		0.427

4.0		0.385

Rubidium (Z=37)

Reference #70

E(keV)     	SE yield

0.3500     	0.9000

Strontium (Z=38)

Reference (9)

E(keV)   	SE yield

0.2500    	0.7500

Data set  #2      Reference (26)

E(keV)  	E yield

0.2500  	0.7500

Data set #3        Reference (106)

E(keV)		SE yield

0.044		0.2

0.07		0.38

0.15		0.467

0.20		0.482

0.3		0.474

0.4		0.434

0.6		0.402

0.8		0.351

1.0		0.327

1.5		0.264

2.0		0.21

3.0		0.156

4.0		0.126

Yttrium (Z=39)

Reference (106)

E(keV)		SE yield

0.2		0.594

0.282		0.621

0.357		0.657

0.404		0.643

0.5		0.613

0.6		0.582

0.8		0.525

1.0		0.473

1.52		0.413

2.0		0.36

3.0		0.278

Zirconium (Z=40)

Reference (9)

E(keV)   	SE yield

0.3500    	1.0000

Data set #2   Reference (26)

E(keV)  	SE yield

0.3500  	0.9000

0.36    		1.10

Data set  #3     Reference (68)

E(keV)  	SE yield

5.0000  	0.5110

Data set  #4     Reference  (70)

E(keV)  	SE yield

5.0000  	0.2980

30.0000 	0.1680

30.0000 	0.1200

Data set #5      Reference (106)

E(keV)		SE yield

0.02		0.302

0.04		0.498

0.09		0.398

0.141		0.721

0.21		0.785

0.32		0.79

0.4		0.735

0.48		0.684

0.56		0.617

Niobium (Z=41)

Reference (9)

E(keV)  	SE yield

0.5500    	1.1510

1.0500    	1.0000

Data set  #2     Reference (26)

E(keV)  	SE yield

0.37    		1.10

Data set  #3     Reference (70)

E(keV)  	SE yield

0.15    		1.00

0.375   	1.30

Data set  #4     Reference  (81)

E(keV)    	SE yield

0.048     	1.153

0.068     	1.258

0.099     	1.37

0.157     	1.45

0.261     	1.436

0.35      	1.36

0.443     	1.31

0.535     	1.243

0.7       	1.142

1.0       	1.015

1.38      	0.941

1.864     	0.902

Data set #5      Reference (106)

E(keV)		SE yield

0.048		0.294

0.057		0.389

0.1		0.591

0.172		0.79

0.237		0.87

0.425		0.888

0.459		0.845

0.684		0.785

0.916		0.709

1.14		0.672

1.378		0.618

1.6		0.6

1.72		0.58

Molybdenum (Z=42)

Reference (2)

E(keV)  	SE yield

1.0000  	1.6000

3.0000  	0.8910

5.0000  	0.5920

10.0000 	0.3760

20.0000 	0.2550

30.0000 	0.1740

Data set  #2    Reference (4)

E(keV)  	SE yield

2.5     		0.894

5.0     		0.606

10.0    		0.381

15.0    		0.285

20.0    		0.236

25.0    		0.214

Data set  #3    Reference (9)

E(keV)  	SE yield

0.4     		1.15

Data set  #4     Reference (70)

E(keV)  	SE yield

0.15    		1.0

0.375   	1.15

1.2     		1.0

Data set #5      Reference (106)

E(keV)		SE yield

0.048		0.49

0.073		0.57

0.19		0.717

0.3		0.83

0.4		0.877

0.5		0.915

0.6		0.906

0.8		0.873

1.0		0.821

2.0		0.705

3.0		0.601

4.0		0.474

Data set #6      Reference (129)

E(keV)		SE yield

| 8 |  | 0.5 |
| --- | --- | --- |
| 7 |  | 0.52 |
| 6 |  | 0.56 |
| 5 |  | 0.63 |
| 4 |  | 0.71 |
| 3 |  | 0.84 |
| 2 |  | 1.04 |
| 1 |  | 1.41 |
| 0.5 |  | 1.54 |
| 0.3 |  | 1.24 |
| 0.2 |  | 1 |
| 0.1 |  | 0.55 |

Palladium (Z=46)

Reference (9)

E(keV)  	SE yield

0.6500   	1.3000

Data set  #2     Reference  (26)

E(keV)  	SE yield

0.6510  	1.5010

Data set #3      Reference (106)

E(keV)		SE yield

0.12		0.85

0.20		1.07

0.3		1.246

0.4		1.37

0.5		1.41

0.6		1.4

0.8		1.37

1.0		1.3

1.5		1.1

2.0		0.97

2.5		0.84

Data set #4      Reference (129)

E(keV)		SE yield

| 8 |  | 0.47 |
| --- | --- | --- |
| 7 |  | 0.52 |
| 6 |  | 0.57 |
| 5 |  | 0.67 |
| 4 |  | 0.74 |
| 3 |  | 0.92 |
| 2 |  | 1.18 |
| 1 |  | 1.67 |
| 0.5 |  | 1.97 |
| 0.3 |  | 1.34 |
| 0.1 |  | 0.6 |

Silver (Z=47)

Reference (2)

E(keV)  	SE yield

1.0     		1.615

3.0     		0.90

5.0     		0.626

10.0    		0.358

20.0    		0.264

30.0    		0.157

Data set  #2     Reference (3)

E(keV)  	SE yield

2.5     		0.932

5.0     		0.636

10.0    		0.41

15.0    		0.285

20.0    		0.236

25.0    		0.214

Data set  #3    Reference (5)

E(keV)  	SE yield

0.5     		1.2157

1.0     		1.2118

1.5     		1.0392

2.0     		0.8824

3.0     		0.6863

4.0     		0.5588

5.0     		0.4666

6.0     		0.4012

7.0     		0.353

8.0     		0.3137

9.0     		0.2941

10.0    		0.265

Data set  #4      Reference (9)

E(keV)  	SE yield

0.7     		1.30

Data set  #5    Reference (21)

E(keV)  	SE yield

0.05    		0.532

0.1     		0.862

0.2     		1.17

0.4     		1.48

0.6     		1.56

0.8     		1.56

1.0     		1.56

Data set #6      Reference (26)

E(keV)  	SE yield

0.7     		1.50

Data set  #7      Reference (68)

E(keV)  	SE yield

5.0     		0.50

5.0     		0.296

30.0    		0.152

30.0    		0.123

Data set  #8    Reference (70)

E(keV)  	SE yield

0.2     		1.0

0.8     		1.5

Data set #9      Reference (61)

E(keV)		SE yield

0.00073	0.107

0.0012		0.097

0.0018		0.0865

0.00267	0.07584

0.0037		0.0742

0.0047		0.0916

0.0057		0.1243

0.0062		0.148

0.0071		0.1848

0.008		0.232

0.009		0.262

0.01		0.282

0.011		0.287

Data set #10    Reference (106)

E(keV)		SE yield

0.02		0.48

0.1		0.704

0.15		0.861

0.2		0.958

0.3		1.135

0.4		1.239

0.6		1.332

0.8		1.346

1.0		1.326

2.0		0.875

3.0		0.655

4.0		0.508

Cadmium (Z=48)

Reference (9)

E(keV)  	SE yield

0.4760    	1.0010

0.4750    	1.0000

0.7000    	1.0000

Data set  #2      Reference (26)

E(keV)  	SE yield

0.5     		1.20

Data set #3      Reference (70)

E(keV)  	SE yield

0.3     		1.0

0.45    		1.1

Data set #4     Reference (106)

E(keV)		SE yield

0.053		0.106

0.1		0.386

0.2		0.779

0.3		0.951

0.4		1.075

0.5		1.115

0.61		1.16

0.81		1.119

1.0		1.183

2.00		0.895

3.0		0.637

4.0		0.447

Indium (Z=49)

Reference (2)

E(keV)  	SE yield

1.0000  	1.6400

3.0000  	0.8920

5.0000  	0.6560

10.0000 	0.3750

20.0000 	0.2850

30.0000 	0.1740

Data set  #2    Reference (9)

E(keV)  	SE yield

0.5     		1.35

Data set #3     Reference (80)

E(keV)    	SE yield

0.2       	0.944

0.28      	1.11

0.4       	1.195

0.5       	1.239

0.6       	1.236

0.8       	1.162

0.9       	1.149

1.0       	1.082

1.1       	1.071

1.2       	1.047

1.3       	0.984

1.4      		 0.977

1.5       	0.960

Data set #4     Reference (106)

E(keV)		SE yield

0.05		0.6

0.073		0.704

0.1		0.769

0.2		0.989

0.3		1.051

0.4		1.056

0.5		1.065

0.6		1.041

0.8		0.991

1.0		0.916

1.567		0.794

2.0		0.694

3.0		0.543

4.0		0.445

Tin (Z=50)

Reference (2)

E(keV)  	SE yield

1.0000    	1.6510

3.0000    	0.8910

5.0000    	0.6420

10.0000   	0.3770

20.0000   	0.3070

30.0000   	0.1740

Data set #2      Reference (9)

E(keV)  	SE yield

0.50    		1.221

Data set #3     Reference (26)

E(keV)  	SE yield

0.5     		1.20

Data set #4       Reference (70)

E(keV)  	SE yield

0.5     		1.35

Data set #5      Reference (106)

E(keV)		SE yield

0.056		0.47

0.086		0.536

0.14		0.8

0.21		0.956

0.3		1.025

0.41		1.06

0.6		1.063

0.8		1.037

1.0		0.999

1.5		0.829

2.0		0.713

3.0		0.57

4.0		0.459

Antimony (Z=51)

Reference (2)

E(keV)  	SE yield

1.0000    	1.6400

3.0000    	0.8920

5.0000    	0.6630

10.0000   	0.3750

20.0000   	0.3040

30.0000   	0.1760

Data set  #2      Reference (9)

E(keV)  	SE yield

0.60    		1.25

Data set #3     Reference (26)

E(keV)  	SE yield

0.6     		1.30

Data set  #4     Reference (70)

E(keV)  	SE yield

0.25    		1.0

0.6     		1.3

2.0     		1.0

Data set #5      Reference (87)

E(keV) 	SE yield

0.084		0.353

0.185		0.684

0.285		1.015

0.393		1.158

0.484		1.30

0.541		1.32

0.64		1.36

0.739		1.38

0.88		1.351

1.0		1.303

1.23		1.215

1.5		1.144

1.75		1.116

Data set #6      Reference (106)

E(keV)		SE yield

0.095		0.341

0.146		0.484

0.197		0.6

0.3		0.786

0.4		0.79

0.6		0.825

0.8		0.82

1.0		0.76

2.0		0.66

3.0		0.58

4.0		0.532

4.5		0.5

Tellurium (Z=52)

Reference (2)

E(keV)  	SE yield

1.0000  	1.6300

3.0000  	0.8910

5.0000  	0.7060

10.0000 	0.3760

20.0000 	0.3190

30.0000 	0.1740

Data set  #2     Reference (68)

E(keV)  	SE yield

5.0    		0.42

5.0     		0.323

30.0    		0.143

Data set #3      Reference (106)

E(keV)		SE yield

0.054		0.42

0.06		0.53

0.073		0.59

0.105		0.69

0.15		0.73

0.24		0.76

0.36		0.796

0.42		0.80

0.52		0.819

0.71		0.792

0.8		0.768

1.02		0.72

1.20		0.607

1.6		0.582

2.0		0.495

2.4		0.418

Cesium (Z=55)

Reference (21)

E(keV)  	SE yield

0.0500  	0.3930

0.1000  	0.4910

0.2000  	0.6200

0.3000  	0.6980

0.4000  	0.7240

0.5000  	0.7160

0.6000  	0.7150

0.7000  	0.7100

0.8000  	0.7070

Data set #2      Reference (26)

E(keV)  	SE yield

0.3     		0.7

Data set #3      Reference (70)

E(keV)  	SE yield

0.4     		0.7

Data set #4      Reference (106)

E(keV)		SE yield

0.03		0.252

0.05		0.299

0.075		0.348

0.1		0.397

0.2		0.431

0.3		0.437

0.4		0.43

0.6		0.355

0.8		0.324

Barium (Z=56)

Reference (21)

E(keV)  	SE yield

0.0500  	0.4180

0.1000  	0.5310

0.2000  	0.7440

0.3000  	0.8140

0.4000  	0.8370

0.5000  	0.8140

0.6000  	0.7900

0.7000  	0.7900

0.8000  	0.7670

0.9000  	0.7440

1.0000  	0.7400

Data set #2      Reference (26)

E(keV)  	SE yield

0.35    		0.80

Data set #3     Reference (70)

E(keV)  	SE yield

0.4     		0.8

Data set #4     Reference (106)

E(keV) 	SE yield

0.05		0.23

0.1		0.384

0.2		0.507

0.3		0.532

0.4		0.558

0.6		0.504

0.8		0.464

1.0		0.433

2.0		0.309

3.0		0.247

4.0		0.217

Lanthanum (Z=57)

Reference (9)

E(keV)  	SE yield

0.5000    	0.8000

Data set  #2      Reference (26)

E(keV)  	SE yield

0.3500  	0.8000

Data set #3      Reference (106)

E(keV)		SE yield

0.2		0.639

0.3		0.689

0.4		0.728

0.5		0.72

0.6		0.707

0.8		0.645

1.0		0.608

1.5		0.53

2.03		0.455

3.0		0.374

Hafnium (Z=72)

Reference (9)

E(keV)  	SE yield

0.4600  	1.1000

Data set #2       Reference (26)

E(keV)  	SE yield

0.4600  	1.1510

Data set #3      Reference (106)

E(keV)		SE yield

0.17		0.47

0.2		0.6

0.3		0.87

0.4		1.123

0.5		1.353

0.607		1.45

0.7		1.5

0.8		1.356

1.0		1.16

1.2		1.05

1.4		0.978

Tantalum (Z=73)

Reference (9)

E(keV)  	SE yield

0.6000    	1.2200

Data set #2      Reference (26)

E(keV)  	SE yield

0.6000  	1.3000

Data set #3      Reference (70)

E(keV)  	SE yield

0.6000  	1.3000

Data set #4     Reference (106)

E(keV)		SE yield

0.1		0.45

0.14		0.58

0.16		0.66

0.2		0.757

0.3		0.849

0.4		0.911

0.5		0.92

0.6		0.924

0.8		0.895

1.0		0.834

1.6		0.79

2.0		0.752

Data set #5      Reference (112)

E(keV)		SE yield

0.075		0.484

0.113		0.771

0.16		0.992

0.25		1.172

0.34		1.257

0.4		1.289

0.5		1.299

0.6		1.298

0.68		1.291

0.8		1.268

0.9		1.261

1.04		1.221

1.2		1.183

Tungsten (Z=74)

Reference (2)

E(keV) 	SE yield

1.0000    	1.6400

5.000     	0.7700

10.000    	0.3930

20.000    	0.3280

30.0000   	0.2440

Data set  #2      Reference (9)

E(keV)  	SE yield

0.7     		1.221

Data set  #3       Reference  (26)

E(keV)  	SE yield

0.6     		1.30

Data set  #4       Reference (70)

E(keV)  	SE yield

0.25    		1.0

0.65    		1.4

Data set  #5      Reference (82)

E(keV)    	SE yield

0.005     	0.159

0.006     	0.2

0.008     	0.285

0.011     	0.365

0.02     	0.398

0.03      	0.469

0.04      	0.615

0.05      	0.714

0.06      	0.771

0.08      	0.848

0.1       	0.9

0.12      	0.95

0.14      	0.993

0.16      	1.032

0.18      	1.053

Data set #6      Reference (106)

E(keV)		SE yield

0.1		0.803

0.2		0.791

0.3		0.815

0.4		0.94

0.6		0.99

0.7		0.986

0.8		0.956

1.0		0.884

2.0		0.816

Rhenium (Z=75)

Reference (9)

E(keV)  	SE yield

0.9000  	1.3000

Data set #2       Reference (106)

E(keV)		SE yield

0.2		1.05

0.3		1.077

0.4		1.143

0.6		1.2

0.72		1.222

0.82		1.15

1.01		1.1

1.21		1.05

1.45		1.00

Platinum (Z=78)

Reference (9)

E(keV)  	SE yield

0.7210    	1.5210

0.7200    	1.5200

0.6000    	1.7050

0.8000    	1.7410

1.2000    	1.5290

1.6000    	1.4000

1.9000    	1.3060

2.5000    	1.2000

3.0000    	1.0940

3.6000    	1.0300

Data set #2       Reference (26)

E(keV)  	SE yield

0.7     		1.60

3.0     		1.00

Data set #3       Reference (34)

E(keV)  	SE yield

0.075   	0.788

1.411   	0.70

Data set #4      Reference (70)

E(keV)  	SE yield

0.35    		1.0

0.7     		1.8

Data set #5     Reference (106)

E(keV)		SE yield

0.1		0.71

0.14		0.84

0.2		1.033

0.4		1.288

0.6		1.368

0.8		1.391

1.0		1.354

1.564		1.246

2.0		1.176

3.0		1.136

4.0		0.926

Data set #6     Reference (112)

E(keV)		SE yield

0.072		0.785

0.08		0.902

0.11		0.996

0.132		1.188

0.17		1.335

0.24		1.49

0.327		1.643

0.4		1.733

0.5		1.795

0.58		1.811

0.7		1.80

0.80		1.751

1.0		1.666

1.2		1.56

Gold (Z=79)

Reference (2)

E(keV)  	SE yield

1.0     		1.65

3.0     		1.07

5.0     		0.793

10.0    		0.498

20.0    		0.362

30.0    		0.253

Data set  #2       Reference (3)

E)keV)  	SE yield

2.5     		1.0

5.0     		0.72

10.0    		0.472

15.0    		0.379

20.0    		0.283

25.0    		0.263

Data set #3       Reference (4)

E(keV)  	SE yield

0.5     		1.55

0.8     		1.20

1.0     		1.12

1.2     		1.104

1.4     		1.01

1.6     		0.934

1.8     		0.85

2.0     		0.709

2.5     		0.68

3.0     		0.59

3.5     		0.546

4.0     		0.498

5.0     		0.437

Data set  #4     Reference (9)

E(keV)  	SE yield

0.78    		0.80

Data set #5       Reference (26)

E(keV)  	SE yield

0.8     		1.70

Data set #6      Reference (68)

E(keV)  	SE yield

5.0     		0.55

5.0     		0.313

30.0    		0.136

Data set #7       Reference (69)

E(keV)  	SE yield

0.2     		0.95

0.3     		1.20

0.4     		1.45

0.52    		1.42

0.7     		1.54

0.8     		1.51

0.9     		1.46

1.0     		1.46

1.5     		1.10

2.0     		1.05

2.5     		0.94

3.0     		0.90

3.5     		0.8

Data set #8      Reference (70)

E(keV)  	SE yield

0.15    		1.00

0.80    		1.40

Data set #9      Reference (106)

E(keV)		SE yield

0.05		0.503

0.1		0.717

0.2		1.044

0.3		1.235

0.4		1.352

0.6		1.218

0.8		1.395

1.0		1.369

2.0		1.212

3.0		1.043

4.0		0.912

Data set #10      Reference (115)

E(keV)		SE yield

1.87		0.809

2.2		0.729

2.6		0.65

3.06		0.59

3.81		0.52

4.7		0.46

6.03		0.389

7.6		0.318

10.2		0.228

19.7		0.114

29.9		0.09

Data set #11      Reference (129)

E(keV)		SE yield

| 8 |  | 0.47 |
| --- | --- | --- |
| 7 |  | 0.52 |
| 6 |  | 0.65 |
| 5 |  | 0.78 |
| 4 |  | 0.84 |
| 3 |  | 0.97 |
| 2 |  | 1.24 |
| 1 |  | 1.7 |
| 0.5 |  | 1.77 |
| 0.3 |  | 1.38 |
| 0.1 |  | 0.67 |

Data set #12	   Reference (132)

E(keV)	   SE yield

20		        0.26

Mercury (Z=80)

Reference (9)

E(keV)  	SE yield

0.6000  	1.0500

Data set #2       Reference (26)

E(keV)  	SE yield

0.6000  	1.3000

Data set #3       Reference (70)

E(keV)  	SE yield

0.6000  	1.3000

Data set #4       Reference (106)

E(keV)		SE yield

0.075		0.5

0.1		0.598

0.2		0.839

0.3		1.042

0.4		1.134

0.6		1.232

0.8		1.238

1.22		1.107

1.61		1.017

2.0		0.94

2.4		0.888

Thallium (Z=81)

Reference (9)

E(keV)  	SE yield

0.6500  	1.4000

Data set #2     Reference (26)

E(keV)  	SE yield

0.6500  	1.4000

Data set #3     Reference (70)

E(keV)  	SE yield

0.6500  	1.7000

Data set #4      Reference (106)

E(keV)		SE yield

0.044		0.495

0.082		0.639

0.13		0.739

0.19		0.869

0.29		0.978

0.39		1.04

0.5		1.068

0.6		1.053

0.8		1.009

1.0		0.966

1.56		0.854

2.0		0.777

3.0		0.649

4.0		0.554

Lead (Z=82)

Reference (9)

E(keV)  	SE yield

0.6000    	1.1010

Data set #2      Reference (26)

E(keV)  	SE yield

0.7000  	1.5000

Data set  #3     Reference (70)

E(keV)  	SE yield

0.2500  	1.0000

0.5000  	1.1000

1.0000  	1.0000

Data set #4      Reference (106)

E(keV)		SE yield

0.2		0.869

0.312		0.992

0.4		1.045

0.6		1.056

0.8		1.028

1.0		0.965

2.04		0.758

3.04		0.609

4.0		0.505

Bismuth (Z=83)

Reference (2)

E(keV)  	SE yield

1.0000  	1.6600

3.0000  	0.8910

5.0000  	0.7950

10.0000 	0.4370

20.0000 	0.3760

30.0000 	0.3140

Data set #2       Reference (9)

E(keV)  	SE yield

0.6     		1.201

Data set #3     Reference (26)

E(keV)  	SE yield

0.7     		1.50

Data set  #4       Reference (68)

E(keV)  	SE yield

5.0     		0.448

5.0     		0.355

30.0    		0.165

Data set #5      Reference (70)

E(keV)  	SE yield

0.55    		1.20

Data set #6         Reference (106)

E(keV)		SE yield

0.1		0.54

0.192		0.7

0.3		0.79

0.4		0.8

0.6		0.89

0.8		0.9

1.0		0.89

2.05		0.729

3.0		0.59

4.0		0.57

Thorium (Z=90)

Reference (9)

E(keV)  	SE yield

0.7000    	1.1010

Data set  #2          Reference (26)

E(keV)  	SE yield

0.6000  	1.3000

Data set #3           Reference (70)

E(keV)  	SE yield

0.8000  	1.1000

Aclar (polymer)

Reference (28)

E(keV)  	SE yield

0.1000    	1.2500

0.2500    	2.0000

0.5000    	1.6900

0.7500    	1.4400

1.0000    	1.1900

1.2500    	1.0900

1.5000    	1.0300

Alumina - Al2O3  (sintered  block )

Reference (20)

E(keV)  	SE yield

0.1000    	3.1500

0.3200    	5.2600

0.5300    	6.2300

0.6500    	6.2300

0.7500    	6.2000

0.9000    	6.0200

1.0000    	6.0000

1.1000    	5.6500

1.2500    	5.1200

2.0000    	3.8300

3.0000    	2.4400

Aluminum Beryllium AlBe

Reference (79)

E(keV)  	SE yield

0.200   	2.219

0.300   	3.155

0.400   	3.985

0.500   	4.268

0.600   	4.483

0.710   	3.691

0.810   	2.852

0.900   	2.100

1.000  		2.010

1.100   	1.981

Ammonia Ice (frozen NH3)

Reference (115)

E(keV) 	SE yield

2.0		0.717

2.5		0.615

3.00		0.538

3.5		0.407

5.0		0.353

6.1		0.247

8.2		0.179

10.1		0.145

12.0		0.165

14.2		0.140

15.9		0.131

17.9		0.111

20.4		0.107

22.0		0.111

23.2		0.111

25.9		0.092

27.7		0.092

29.0		0.092

Boron Nitride BN

Reference (20)

E(keV)  	SE yield

0.050   	1.000

0.600   	2.900

3.000   	1.700

Carbon dioxide (“dry”) ice

Reference (115)

E(keV) 	SE yield

2.0		0.308

3.0		0.272

4.1		0.309

5.0		0.258

7.0		0.179

8.0		0.259

10.0		0.165

12.2		0.172

14.7		0.143

16.6		0.148

20.0		0.134

22.6		0.141

24.4		0.122

26.7		0.107

29.1		0.108

COAT725 (wafer coat)

Reference (86)

E(keV)  	SE yield

0.500   	2.150

0.700   	1.625

1.000   	1.350

1.500   	1.040

2.000   	0.895

3.000   	0.727

4.000   	0.610

5.000   	0.570

7.000   	0.497

10.000  	0.405

Chromium dioxide Cr2O3

Reference (72)

E(keV)  	SE yield

0.072   	0.100

0.100   	0.400

0.200   	0.650

0.300   	0.780

0.500   	0.920

0.650   	0.980

0.750   	0.970

1.000   	0.900

1.500   	0.700

Copper dioxide Cu2O

Reference (72)

E(keV)  	SE yield

0.020   	0.200

0.100   	0.740

0.200   	1.000

0.300   	1.130

0.500   	1.230

0.650   	1.230

0.750   	1.210

1.000   	1.180

1.500   	1.080

Diamond (CVD diamond activated with CsI)

Reference (111)

E(keV) 	SE yield

0.09		5.37

0.138		4.68

0.18		8.39

0.25		18.48

0.35		25.5

0.45		30.2

0.59		35.2

0.73		39.95

0.95		46.6

1.14		53.3

1.34		59.4

1.55		64.37

1.76		69.0

1.96		73.0

2.17		76.7

2.37		80.7

2.54		83.7

27.3		86.3

2.93		89.0

3.0		90.3

Fosterite

Reference (20)

E(keV)  	SE yield

0.015   	0.900

0.020   	1.060

0.025   	1.250

0.030   	1.400

0.045   	1.700

0.050   	2.000

0.075   	2.530

0.100   	3.100

0.300   	4.100

0.400   	4.500

0.500   	4.600

0.600   	4.600

0.700   	4.450

1.000   	4.050

1.400   	3.650

2.000   	3.100

2.400   	2.900

3.000   	2.500

Ice (H2O)

Reference (115)

E(keV) 	SE yield

2.0		1.154

3.0		0.80

4.0		0.954

5.0		0.75

6.0		0.613

8.0		0.552

10.0		0.454

12.0		0.356

13.7		0.306

17.7		0.227

23.5		0.186

Liquid water

Reference 122

E(keV)		SE yield

0.45		0.103

0.64		0.49

0.88		1.13

1.08		1.52

1.26		1.58

1.45		1.56

1.67		1.47

1.85		1.40

2.07		1.31

2.25		1.26

2.5		1.21

3.6		1.11

4.06		1.04

5.1		0.98

10.1		0.67

15.1		0.45

20.1		0.362

Liquid water (200 monolayers on copper)

Reference 127

E(keV)		SE yield

0.049		1.38

0.060		1.52

0.070		1.61

0.08		1.70

0.1		1.87

0.15		2.12

0.2		2.24

0.25		2.38

0.3		2.27

0.4		2.16

0.5		2.02

0.7		1.76

0.1		1.55

0.15		1.39

1.95		1.29

Indium tin oxide (ITO)

Reference: (131)

E(keV)		SE yield

0.5		2.52

0.7		2.37

1.0		2.12

1.5		1.71

2		1.55

3		1.31

5		1.03

7		0.72

10		0.72

Indium Zinc Oxide

Reference: (131)

E(keV)		SE yield

0.5		2.67

0.7		2.5

1.0		2.2

1.5		1.78

2		1.61

3		1.31

5		1.02

7		0.86

10		0.72

Interconnect line aluminum

Reference (86)

E(keV)  	SE yield

10.000  	0.215

7.000   	0.320

5.000   	0.380

4.000   	0.550

3.000   	0.630

2.000   	0.790

1.500   	0.840

1.000   	0.910

0.700   	1.020

0.500  		1.050

Kapton (polymer sheet)

Reference (27)

E(keV)  	SE yield

1.45    		0.50

1.9     		0.4

2.5     		0.37

3.0     		0.31

3.8     		0.28

4.5     		0.23

5.2     		0.14

Data set #2       Reference (32)

E(keV)  	SE yield

0.1     		1.90

0.15    		1.92

0.25    		1.90

0.35    		1.15

0.6     		0.82

0.8     		0.50

0.9     		0.425

1.0     		0.25

1.25    		0.19

1.5     		0.09

2.0     		0.085

2.5     		0.08

Data set #3       Reference (33)

E(keV) 	SE yield

9.0     		0.14

25      		0.06

45      		0.04

65      		0.033

80      		0.025

Data set #4      Reference (28)

E(keV)  	SE yield

0.1     		1.52

0.2     		1.81

0.3     		1.68

0.4     		1.51

0.5     		1.355

0.6     		1.23

0.7     		1.13

0.8     		1.06

0.95    		1.0

KCl (Potassium Bromide)

Reference (19)

E(keV)  	SE yield

0.2000  	6.5000

0.3000  	7.5000

0.4000  	8.4700

0.6000  	10.1200

0.9000  	11.7600

1.2000  	12.3500

1.5000  	13.3000

1.8000  	13.4000

2.4000  	13.3500

3.0000  	13.0500

4.2000  	12.0000

5.1000  	11.0000

KBr (Potassium Bromide)

Reference (19)

E(keV)  	SE yield

0.2000  	6.5000

0.3000  	7.5000

0.4000  	8.4700

0.6000  	10.1200

0.9000  	11.7600

1.2000  	12.3500

1.5000  	13.3000

1.8000  	13.4000

2.4000  	13.3500

3.0000  	13.0500

4.2000  	12.0000

5.1000  	11.0000

KI (Potassium Iodide)

Reference (19)

E(keV)  	SE yield

0.0800  	2.3400

0.1500  	3.4000

0.2000  	5.8400

0.4000  	6.8000

0.6000  	8.9700

0.7500  	9.3600

1.0000  	10.4000

1.2000  	10.4000

1.5000  	10.7700

1.8000  	10.6400

2.1000  	10.5000

2.5000  	10.2500

3.0000  	9.4000

3.5000  	8.8500

4.0000  	8.0800

4.5000  	7.9500

5.0000  	7.1800

5.5000  	7.3100

Data set #2      Reference (70)

E(keV) 	SE yield

1.60    		10.0

KTCNQ (organic conductor)

Reference (29)

E(keV)  	SE yield

0.0500  	1.0600

0.1000  	1.4000

0.1500  	1.4840

0.2000  	1.5700

0.3000  	1.4900

0.4000  	1.3500

0.5000  	1.2300

0.6000  	1.1200

0.8000  	0.9400

1.0000  	0.8300

1.2000  	0.7400

1.4000  	0.6900

0.0200  	0.5300

0.0100  	0.2900

Lucite (polymer sheet)

Reference (30)

E(keV)  	SE yield

0.2200  	2.4000

0.2600  	2.5000

0.3500  	2.5000

0.4000  	2.2000

0.5000  	2.0000

0.7000  	1.5000

1.0000  	1.1000

1.5000  	0.8000

1.8000  	0.7000

2.0000  	0.6000

2.5000  	0.5500

Data set #2      Reference (31)

E(keV)  	SE yield

8.0     		0.29

10.0    		0.20

15.0    		0.15

20.0    		0.12

25.0    		0.09

Magnesium Oxide MgO

Reference (18)

E(keV)  	SE yield

0.0800  	5.0000

0.2000  	9.0000

0.2600  	12.8000

0.3600  	16.2000

0.5000  	19.2000

0.7000  	21.6000

0.8000  	21.6000

0.9000  	22.5000

1.0000  	23.0000

1.1000  	23.6000

1.2000  	24.2000

1.3000  	24.3000

1.4000  	24.0000

1.5000  	23.3000

1.6000  	23.2000

1.8000  	22.4000

2.0000  	21.8000

2.4000  	20.2000

2.8000  	18.2000

3.2000  	17.5000

3.6000  	16.2000

4.0000  	15.0000

Data Set #2	Reference (130)

E(keV)  	SE yield	(MgO deposited by EBE on to a heated silicon substrate)

0.5		   3.2

0.75		   3.3

1.0		   3.25

1.25		   3.1

1.5		  2.75

1.75		  2.5

2.0		  2.25

2.5		  2.0

3.0		  1.6

3.5		  1.3

4.0		  1.3

Data Set #3	Reference (130)

E(keV)  	SE yield	(MgO deposited by EBE on to a cold silicon substrate)

0.5		  3.15

0.75		  3.35

1.0		  3.45

1.25		  3.6

1.5		  3.4

1.75		  3.0

2.0		  2.85

2.5		  2.5

3.0		 2.25

3.5		 2.05

4.0		 1.75

Data Set #4	Reference (130)

E(keV)  	SE yield	(MgO deposited by RF sputtering)

0.5		   2.0

0.75		   2.0

1.0		   1.8

1.25		   1.6

1.50		   1.5

1.75		   1.25

2.0		   1.1

2.5		   0.8

3.0		   0.7

3.5		   0.55

4.0		   0.5

Methanol ice (CH3OH)

Reference (115)

E(keV) 	SE yield

2.0		0.37

2.5		0.339

3.0		0.322

4.1		0.32

6.2		0.257

8.4		0.212

10.6		0.166

12.4		0.169

14.7		0.123

17.4		0.109

21.2		0.121

23.5		0.676

Mylar (polymer sheet)

Reference (32)

E(keV)  	SE yield

0.2     		3.10

0.3     		3.1

0.4     		2.6

0.5     		2.2

0.6     		2.0

0.9     		1.5

1.0     		1.2

1.3     		0.83

1.5     		0.8

2.0     		0.70

2.5     		0.62

Data set #2      Reference (33)

E(keV)  	SE yield

9.0     		0.175

25.0    		0.075

45.0   		0.056

60.0    		0.044

80.0    		0.04

Data set #3      Reference (28)

E(keV)  	SE yield

0.1     		1.54

0.22    		1.8

0.33    		1.62

0.44    		1.47

0.55    		1.32

0.66    		1.19

0.77    		1.13

0.88    		1.06

1.03    		1.00

Sodium Bromide NaBr

Reference (19)

E(keV)  	SE yield

0.1000  	2.6000

0.2000  	4.5000

0.4000  	12.0000

0.6000  	16.7000

0.8000  	19.5000

1.0000  	20.8500

1.2000  	21.6500

1.5000  	22.5000

1.8000  	22.1000

2.1000  	21.3000

2.4000  	20.5000

2.7000  	20.4000

3.0000  	20.2000

4.0000  	18.4500

4.5000  	17.6000

5.0000  	17.5000

Data set #2     Reference (70)

E(keV)  	SE yield

1.8     		24.0

Nickel chromide NiCr

Reference (79)

E(keV)		 SE yield

0.212   	1.787

0.310   	2.574

0.400   	3.435

0.500   	3.744

0.600   	3.373

0.710   	2.597

0.800   	2.226

0.900   	1.966

1.000   	1.944

1.100   	1.850

Nylon (polymer solid)

Reference (29)

E(keV)  	SE yield

0.1500  	2.2900

0.2000  	2.5400

0.3000  	2.4800

0.4000  	2.2300

0.5000  	1.9800

0.6000  	1.8000

0.8000  	1.4600

1.0000  	1.2300

1.2000  	1.0300

1.4000  	0.9500

Polyethylene (polymer solid)

Reference (3)

E(keV)  	SE yield

0.2000  	2.8000

0.2500  	2.9000

0.3000  	2.9000

0.4500  	2.5000

0.5000  	2.5000

0.6000  	2.4000

0.9000  	1.9000

1.0000  	1.5000

1.5000  	1.0500

2.0000  	0.8000

Data set #2      Reference (33)

E(keV)  	SE yield

8.0     		0.3

25.0    		0.15

40.0    		0.10

60.0    		0.07

80.0    		0.06

Polyimide (polymer solid)

Reference (29)

E(keV)  	SE yield

0.0500  	1.0000

0.1000  	1.3200

0.1500  	1.4600

0.2000  	1.4600

0.3000  	1.3700

0.4000  	1.2900

0.5000  	1.1500

0.6000  	1.0000

0.8000  	0.8300

1.0000  	0.7230

1.2000  	0.6610

1.4000  	0.6000

Polyeurethane    (polymer solid)

Reference (29)

E(keV)  	SE yield

0.1500  	2.3000

0.2000  	2.4300

0.3000  	2.4500

0.4000  	2.2800

0.5000  	2.0600

0.6000  	1.8100

0.8000  	1.4600

1.0000  	1.2300

1.2000  	1.0300

1.4000  	0.9500

PETEOS (organic)

Reference (86)

E(keV)  	SE yield

10.000  	0.255

7.000   	0.340

5.000   	0.427

3.000   	0.662

2.000   	0.788

1.500   	0.975

1.000   	1.205

0.700   	1.345

0.500   	1.613

Resist (electron beam – PMMA)

Reference (86)

E(keV)  	SE yield

10.000  	0.600

7.000   	0.690

5.000   	0.915

4.000   	0.960

3.000   	1.145

2.000   	1.440

1.500   	1.850

1.000   	2.160

0.700   	2.330

0.500   	2.315

Silicon dioxide SiO2   (steam formed)

Reference (25)

E(keV)  	SE yield

0.050   	1.0200

0.1     		1.3120

0.15    		1.4380

0.20    		1.5000

0.25    		1.4830

0.30    		1.4580

0.4     		1.3960

0.5     		1.3120

0.6     		1.2710

0.70    		1.1870

0.8     		1.1040

0.9     		1.0830

1.0     		1.0200

Data set  #2      Reference (70)

E(keV)  	SE yield

0.4     		2.10

Data set #3     Reference (86)

E(keV) 	SE yield

0.5     		1.35

0.7     		1.274

1.0    		1.18

1.5     		1.0

2.0     		0.85

3.0    		0.765

4.0     		0.710

5.0     		0.582

7.0     		0.427

10.     		0.314

Stainless Steel

Reference 127

E(KeV)	SE  yield

0.05		1.15

0.08		1.40

0.1		1.55

0.15		1.8

0.2		1.94

0.25		1.99

0.3		2.02

0.4		1.99

0.5		1.92

0.7		1.75

1.0		1.53

1.5		1.28

1.95		1.13

Tantalum Carbide TaC

Reference (112)

E(keV) 	SE yield

0.087		0.245

0.098		0.404

0.109		0.504

0.128		0.672

0.156		0.801

0.2		0.865

0.29		0.872

0.386		0.823

0.507		0.760

0.592		0.703

0.701		0.656

0.792		0.623

0.94		0.595

1.03		0.576

1.2		0.553

TCNQ (organic conductor)

Reference (29)

E(keV)  	SE yield

0.0500  	0.6900

0.1000  	0.8460

0.1500  	1.0000

0.2000  	1.0300

0.3000  	1.0300

0.4000  	1.0000

0.5000  	0.9500

0.6000  	0.9070

0.8000  	0.8300

1.0000  	0.7850

1.2000  	0.7380

1.4000  	0.6930

Teflon (polymer solid)

Reference (27)

E(keV)  	SE yield

0.5000  	2.3000

0.7000  	1.8000

1.4500  	1.2000

1.5000  	1.000

1.9500  	0.9300

2.0000  	0.9000

2.1000  	0.8600

2.2000  	0.8200

2.7000  	0.7800

3.0000  	0.7200

3.8000  	0.5600

Data set #2      Reference (28)

E(keV)  	SE yield

0.1     		1.217

0.25    		1.94

0.5     		1.62

0.75    		1.25

1.0     		1.0

1.25    		1.04

1.5     		1.015

Titanium Carbide TiC

Reference (112)

E(keV) 	SE yield

0.09		0.58

0.14		0.724

0.2		0.869

0.33		1.0

0.4		1.02

0.53		1.01

0.62		0.997

0.73		0.974

0.8		0.944

0.92		0.895

1.0		0.865

1.2		0.812

Titanium Nitride (TiN)

Reference 127

E(keV)		SE yield

0.06		0.79

0.07		0.84

0.08		0.90

0.1		0.98

0.15		1.16

0.2		1.28

0.25		1.38

0.3		1.49

0.4		1.56

0.5		1.57

0.6		1.58

0.75		1.56

1.0		1.49

1.5		1.37

2.0		1.25

3.0		1.05

Vanadium Pentoxide V2O5

Reference (83)

E(keV)  	SE yield

0.087   	0.887

0.156   	1.000

0.200   	1.117

0.270   	1.210

0.404   	1.216

0.542   	1.135

0.653   	1.088

0.778   	1.027

0.889   	1.001

1.013   	0.947

1.210   	0.894

1.433   	0.849

1.705   	0.776

2.010   	0.718

2.540   	0.669

3.044   	0.578

3.572   	0.530

4.034   	0.487

5.056   	0.389

5.571   	0.347

Xylene (organic solid)

Reference (29)

E(keV)  	SE yield

0.0500  	1.3300

0.1500  	1.7500

0.2000  	1.7700

0.2500  	1.7400

0.3000  	1.6300

0.4000  	1.4900

0.5000  	1.3500

0.6000  	1.2100

0.8000  	1.0000

1.0000  	0.8900

1.2000  	0.7700

1.4000  	0.6700

Zirconium Carbide ZrC

Reference (112)

E(keV) 	SE yield

0.095		0.817

0.14		1.01

0.21		1.178

0.3		1.252

0.4		1.242

0.5		1.199

0.64		1.118

0.8		1.044

0.93		0.976

1.06		0.921

1.2		0.873

SECTION TWO

Backscattered Electron Yield Data

(a) for elements, arranged in ascending atomic number

(b) for compounds, arranged in alpha-numeric order

Beryllium (Z=4)

Reference (2)

E(keV)  	BS yield

1.0     		0.127

3.0     		0.0885

5.0     		0.07

10.0    		0.0558

20      		0.05

25      		0.0462

30      		0.0460

Data set #2        Reference (5)

E(keV)  	BS yield

1.0     		0.226

2.0     		0.086

3.0     		0.0636

5.0     		0.0496

10.0    		0.0418

Data set #3      Reference (7)

E(keV)  	BS yield

4.5     		0.064

11.0    		0.04

28.0    		0.023

Data set #4       Reference (13)

E(keV)  	BS yield

15.0    		0.039

20.0    		0.036

30      		0.033

40      		0.031

50      		0.029

60      		0.028

Data set #5      Reference (15)

E(keV)  	BS yield

9.3     		0.05

17.3    		0.05

25.2    		0.045

41.5    		0.04

62.1    		0.04

81.8    		0.04

102.2   	0.035

Data set #6        Reference (106)

E(keV)		BS yield

0.1		0.095

0.2		0.109

0.3		0.112

0.4		0.112

0.6		0.103

0.8		0.092

1.0		0.081

2.0		0.065

3.0		0.055

4.0		0.049

Boron (Z=5)

Reference (1)

E(keV)  	BS yield

3.93    		0.0410

5.0     		0.0740

7.50    		0.0570

10.00   	0.0550

15.20   	0.0530

20.20   	0.0410

31.00   	0.0430

41.0    		0.0440

Carbon (Z=6)

Reference (1)

E(keV)  	BS yield

3.9     		0.083

5.0     		0.082

7.5     		0.071

10.0    		0.066

15.2    		0.057

20.2    		0.049

31.0    		0.051

41.0    		0.049

Data set #2       Reference (6)

E(keV)  	BS yield

5.0     		0.085

10.0    		0.072

20.0    		0.061

30.0    		0.06

Data set #3        Reference (7)

E(keV)  	BS yield

4.5     		0.083

11.0    		0.059

28.0    		0.052

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.069

20.0    		0.06

30.0    		0.052

40.0    		0.054

49.0    		0.052

Data set #5      Reference (13)

E(keV)  	BS yield

15.0    		0.068

20.0    		0.064

30.0    		0.06

40.0    		0.056

50.0    		0.055

Data set #6       Reference (34)

E(keV)  	BS yield

0.2     		0.076

0.4     		0.081

0.8     		0.074

1.2     		0.0714

1.4     		0.071

1.65    		0.066

2.05    		0.066

2.25    		0.066

Data set #7      Reference (35)

E(keV)  	BS yield

2.0     		0.0771

3.0     		0.0857

4.0    		0.0886

5.0     		0.0857

6.0     		0.0834

8.0     		0.08

10.0    		0.0743

12.0    		0.071

14.0    		0.0685

16.0    		0.0674

Data set #8       Reference (68)

E(keV)  	BS yield

5.0     		0.082

30.0    		0.05

Data set #9       Reference (106)

E(keV)		BS yield

0.288		0.149

0.4		0.153

0.5		0.15

0.6		0.147

0.8		0.14

1.0		0.133

2.0		0.107

3.0		0.088

Data set #10    Reference (107)

E(keV)		BS yield

1.0		0.076

1.5		0.071

2.0		0.071

2.5		0.064

3.0		0.063

3.5		0.063

4.0		0.058

4.5		0.058

5.0		0.058

Magnesium (Z=12)

Reference (1)

E(keV)  	BS yield

3.93    		0.1740

5.0     		0.1640

7.50    		0.1560

10.0    		0.1520

15.2    		0.1430

20.2    		0.1400

31.0    		0.1350

41.0    		0.1260

Data set #2       Reference (8)

E(keV)  	BS yield

10.0    		0.145

20.0    		0.14

30.0    		0.136

40.0    		0.132

49.0    		0.13

Data set #3      Reference (106)

E(keV)		BS yield

0.20		0.238

0.4		0.241

0.6		0.238

0.8		0.221

1.0		0.207

2.0		0.184

3.0		0.156

Aluminum (Z=13)

Reference (2)

E(keV) 	BS yield

1.0     		0.192

3.0     		0.161

5.0     		0.153

10.0    		0.15

15.0    		0.15

20.0    		0.148

25.0    		0.148

30.0    		0.144

Data set #2      Reference (4)

E(keV)  	BS yield

0.8     		0.198

1.0     		0.195

1.2     		0.189

1.4     		0.182

1.6     		0.179

1.8     		0.175

2.0    		0.17

2.5     		0.168

3.0     		0.157

3.5     		0.152

4.0     		0.151

5.0     		0.148

Data set #3       Reference (5)

E(keV)  	BS yield

1.0     		0.2346

3.0     		0.2132

5.0     		0.20

10.0    		0.1875

Data set #4     Reference (6)

E(keV)  	BS yield

5.0     		0.186

10.0    		0.177

30.0    		0.15

Data set #5     Reference (7)

E(keV)  	BS yield

4.5     		0.181

11.0    		0.133

28.0    		0.130

Data set #6      Reference (8)

E(keV)  	BS yield

30.0    		0.149

Data set #7      Reference (13)

E(keV)  	BS yield

15.0    		0.171

20.0    		0.164

30.0    		0.155

40.0    		0.151

50.0    		0.147

60.0    		0.146

Data set #8      Reference (14)

E(keV)  	BS yield

2.0     		0.14

2.5     		0.133

3.0     		0.132

4.0    		0.131

5.0     		0.135

6.0     		0.137

8.0     		0.142

10.0    		0.14

12.5    		0.14

15.0    		0.137

17.5    		0.139

20.0    		0.139

Data set #9      Reference (15)

E(keV)  	BS yield

9.3     		0.175

17.3    		0.159

25.2    		0.151

41.5    		0.155

62.1   		0.137

81.8    		0.135

102.2   	0.133

Data set #10     Reference (22)

E(keV)  	BS yield

20.0    		0.14

45.0    		0.15

Data set  #11    Reference (35)

E(keV)  	BS yield

1.0     		0.134

2.0     		0.146

3.0     		0.154

5.0     		0.158

7.5     		0.153

10.0    		0.149

12.5    		0.151

15.0    		0.149

17.5    		0.151

Data set #12     Reference (68)

E(keV)  	BS yield

5.0     		0.168

30.0    		0.135

Data set #13     Reference (106)

E(keV)		BS yield

0.1		0.19

0.2		0.224

0.3		0.235

0.4		0.237

0.6		0.234

0.8		0.226

1.0		0.217

2.0		0.20

3.0		0.191

4.0		0.185

Data set #14     Reference (107)

E(keV)		BS yield

0.5		0.216

1.0		0.212

1.5		0.206

2.0		0.203

2.5		0.202

3.0		0.197

3.5		0.195

4.0		0.191

4.5		0.188

5.0		0.185

6.0		0.180

Silicon (Z=14)

Reference (1)

E(keV)  	BS yield

3.93    		0.204

5.0     		0.188

7.5     		0.182

10.0    		0.174

15.2    		0.163

20.0    		0.159

31.0    		0.152

41.0    		0.144

Data set #2      Reference (2)

E(keV)  	BS yield

1.0     		0.235

3.0     		0.212

5.0     		0.206

10.0    		0.2

15.0    		0.197

20.0   		0.194

25.0    		0.192

30.0    		0.19

Data set #3      Reference (6)

E(keV) 	BS yield

5.0     		0.197

10.0    		0.186

20.0    		0.169

30.0    		0.162

Data set #4        Reference (8)

E(keV) 	BS yield

10.0    		0.174

20.0    		0.164

30.0   		0.159

40.0    		0.153

49.0    		0.15

Data set #5      Reference (15)

E(keV)  	BS yield

9.3     		0.183

17.3    		0.178

25.2    		0.165

41.5    		0.155

62.1    		0.149

81.8    		0.145

102.2   	0.145

Data set #6      Reference (68)

E(keV)  	BS yield

5.0     		0.184

30.0    		0.145

Data set #7      Reference (106)

E(keV)		BS yield

0.2		0.252

0.3		0.263

0.4		0.255

0.6		0.241

0.8		0.231

1.0		0.228

2.0		0.204

3.0		0.192

4.0		0.189

Data set #8	Reference (132)

E(keV)	BS yield

20		  0.18

Silicon (Z=14) Amorphous

Reference (86)

E(keV)  	BS yield

10.000  	0.190

7.0000  	0.200

5.000   	0.200

4.00    		0.200

3.000   	0.200

2.000   	0.210

1.500   	0.210

1.000   	0.210

0.700   	0.210

0.500   	0.210

Potassium (Z=19)

Reference (106)

E(keV)		BS yield

0.1		0.256

0.22		0.255

0.4		0.254

0.6		0.249

0.8		0.242

1.2		0.232

1.6		0.223

2.0		0.214

Calcium (Z=20)

Reference (35)

E(keV)  	BS yield

2.0     		0.2030

3.0     		0.2130

4.00    		0.2260

6.0     		0.2290

9.0     		0.2290

11.0    		0.2290

13.0    		0.2310

15.0    		0.2310

Data set #2      Reference (106)

E(keV)		BS yield

0.15		0.159

0.2		0.187

0.4		0.251

0.6		0.255

0.8		0.255

1.2		0.248

1.6		0.245

2.0		0.24

Scandium (Z=21)

Reference (106)

E(keV)		BS yield

0.130		0.218

0.200		0.246

0.31		0.271

0.4		0.27

0.6		0.269

0.8		0.268

1.0		0.263

2.0		0.263

4.0		0.262

Titanium (Z=22)

Reference (1)

E(keV)  	BS yield

3.93    		0.258

5.0     		0.26

7.5     		0.257

10.0    		0.256

15.2    		0.249

20.2    		0.248

31.0    		0.246

41.0    		0.238

Data set #2       Reference (6)

E(keV)  	BS yield

5.0     		0.27

10.0    		0.268

20.0    		0.266

30.0    		0.254

Data set #3     Reference (7)

E(keV)  	BS yield

4.5     		0.262

11.0    		0.236

28.0    		0.214

Data set #4       Reference (8)

E(keV)  	BS yield

10.0    		0.262

20.0    		0.253

30.0    		0.243

40.0    		0.245

49.0    		0.243

Data set #5      Reference (13)

E(keV)  	BS yield

15.0    		0.268

20.0    		0.263

30.0    		0.258

40.0    		0.252

50.0    		0.248

60.0    		0.246

Data set #6      Reference (68)

E(keV)  	BS yield

5.0     		0.246

30.0    		0.23

Data set #7      Reference (106)

E(keV)		BS yield

0.1		0.12

0.21		0.234

0.31		0.27

0.41		0.283

0.6		0.293

0.8		0.299

1.0		0.294

2.0		0.291

3.0		0.287

4.0		0.283

Vanadium (Z=23)

Reference (1)

E(keV)  	BS yield

3.93    		0.2740

5.0     		0.2750

7.50    		0.2670

10.0    		0.2640

15.2    		0.2610

20.20   	0.2530

31.0    		0.2510

41.0    		0.2460

Data set #2       Reference (8)

E(keV)  	BS yield

30.0    		0.268

Data set #3

Reference (68)

E(keV)  	BS yield

5.0     		0.255

30.0    		0.238

Chromium (Z=24)

Reference (1)

E(keV)  	BS yield

3.93    		0.273

5.0     		0.273

7.50   		0.27

10.0    		0.267

15.2    		0.264

20.2    		0.259

31.0    		0.257

41.0    		0.248

Data set #2      Reference (6)

E(keV)  	BS yield

5.0     		0.285

10.0    		0.283

30.0    		0.276

Data set #3       Reference (8)

E(keV)  	BS yield

10.0    		0.273

20.0    		0.268

30.0    		0.265

40.0    		0.259

49.0    		0.256

Data set #4     Reference (68)

E(keV)  	BS yield

5.0     		0.255

30.0    		0.245

Manganese (Z=25)

Reference (8)

E(keV)  	BS yield

10.0    		0.2920

20.0    		0.2860

30.0    		0.2840

40.0    		0.2770

49.0    		0.2760

Iron (Z=26)

Reference (1)

E(keV)  	BS yield

3.93    		0.294

5.0     		0.284

7.5     		0.287

10.0    		0.285

15.2    		0.278

20.2    		0.276

31.0    		0.277

41.0    		0.266

Data Set #2     Reference (6)

E(keV)  	BS yield

5.0     		0.3

10.0    		0.296

30.0    		0.288

Data set #3      Reference (7)

E(keV)  	BS yield

4.5     		0.307

11.0    		0.266

28.0   		0.251

Data set #4       Reference (8)

E(keV)  	BS yield

10.0    		0.289

20.0    		0.287

30.0    		0.275

40.0    		0.276

49.0    		0.282

Data set #5       Reference (13)

E(keV)  	BS yield

15.0    		0.298

20.0    		0.294

30.0    		0.288

40.0    		0.284

50.0    		0.281

60.0    		0.279

Data set #6      Reference (34)

E(keV)  	BS yield

0.25    		0.219

0.4     		0.219

0.65    		0.23

0.825   	0.22

1.05    		0.22

1.225   	0.22

1.65    		0.223

3.825   	0.248

Data set #7      Reference (35)

E(keV)  	BS yield

1.0     		0.237

1.5     		0.263

2.0     		0.27

3.0     		0.277

4.0     		0.288

5.0     		0.285

6.0     		0.286

9.0     		0.289

10.0    		0.289

11.0    		0.291

12.0    		0.291

13.0    		0.291

14.0    		0.291

16.0    		0.29

Data set #8       Reference (68)

E(keV)  	BS yield

5.0     		0.275

30.0    		0.26

Cobalt (Z=27)

Reference (1)

E(keV) 	BS yield

3.93    		0.3110

5.0     		0.3100

7.5     		0.3060

10.0    		0.3030

15.20   	0.2980

20.20   	0.2960

31.00   	0.2890

41.0    		0.2830

Data set #2      Reference (7)

E(keV)  	BS yield

4.5     		0.316

11.0    		0.28

28.0    		0.261

Data set #3      Reference (8)

E(keV)  	BS yield

10.0    		0.309

20.0    		0.302

30.0    		0.302

40.0    		0.297

49.0    		0.292

Nickel (Z=28)

Reference (1)

E(keV)  	BS yield

3.93    		0.318

5.0     		0.312

7.5     		0.309

10.0    		0.308

15.2    		0.301

20.2    		0.30

31.0    		0.293

41.0    		0.29

Data set #2      Reference (6)

E(keV)  	BS yield

5.0     		0.333

10.0    		0.323

30.0    		0.308

Data set #3       Reference (7)

E(keV)  	BS yield

4.5     		0.347

11.0    		0.30

28.0    		0.283

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.307

20.0    		0.301

30.0    		0.298

40.0    		0.289

49.0    		0.286

Data set #5      Reference (16)

E(keV)  	BS yield

2.0     		0.46

3.0     		0.471

5.0     		0.477

8.0     		0.44

10.0    		0.4

Data set #6      Reference (35)

E(keV)  	BS yield

2.0     		0.297

3.0     		0.306

4.0     		0.306

5.0     		0.307

6.0         	0.311

15.0    		0.312

16.5    		0.312

Data set #7       Reference (68)

E(keV)  	BS yield

5.0     		0.282

30.0    		0.28

Data set #8       Reference (106)

E(keV)		BS yield

0.1		0.108

0.2		0.268

0.3		0.329

0.4		0.353

0.6		0.374

0.8		0.378

1.0		0.383

2.0		0.371

3.0		0.359

4.0		0.338

Data set #9       Reference (112)

E(keV)		BS yield

0.08		0.05

0.142		0.013

0.19		0.195

0.265		0.256

0.334		0.283

0.403		0.304

0.54		0.304

0.7		0.306

0.8		0.306

1.0		0.321

1.2		0.32

Copper (Z=29)

Reference (1)

E(keV) 	BS yield

3.93    		0.329

5.0     		0.323

7.5     		0.317

10.0    		0.316

15.2    		0.31

20.2    		0.306

31.0    		0.301

41.0    		0.295

Data set #2     Reference (2)

E(keV)  	BS yield

3.0     		0.311

5.0     		0.311

10.0    		0.311

15.0    		0.311

20.0    		0.311

25.0    		0.311

30.0    		0.311

Data set #3        Reference (3)

E(keV)  	BS yield

0.8     		0.259

1.0     		0.265

1.2     		0.268

1.4     		0.268

1.6     		0.279

2.0     		0.301

2.5     		0.306

3.0     		0.309

3.5    	 	0.313

4.0     		0.306

5.0     		0.325

Data set #4      Reference (5)

E(keV)  	BS yield

1.0     		0.4375

2.0     		0.419

3.0     		0.3989

5.0     		0.3842

10.0    		0.3566

Data set #5      Reference (6)

E(keV)  	BS yield

5.0     		0.352

10.0    		0.339

20.0    		0.339

30.0    		0.319

Data set #6      Reference (8)

E(keV)  	BS yield

10.0    		0.318

20.0    		0.309

30.0    		0.306

40.0    		0.303

49.0    		0.297

Data set #7       Reference (13)

E(keV)  	BS yield

15.00   	0.335

20.0    		0.328

30.0    		0.319

40.0    		0.316

50.0    		0.313

60.0    		0.311

Data set #8     Reference (15)

E(keV)  	BS yield

9.3     		0.313

17.3    		0.310

25.2    		0.307

41.5    		0.301

62.1    		0.299

81.8    		0.294

102.2   	0.291

Data set #9      Reference (22)

E(keV)  	BS yield

10.0    		0.29

20.0    		0.29

45.0    		0.30

Data set #10     Reference (23)

E(keV)  	BS yield

0.5     		0.40

1.0     		0.43

2.0     		0.406

3.0     		0.406

5.0     		0.398

6.0     		0.381

7.0     		0.366

8.0     		0.368

9.0     		0.358

10.0    		0.356

Data set #11     Reference (34)

E(keV)  	BS yield

0.4     		0.268

0.65    		0.269

0.825   	0.276

1.05    		0.276

1.45    		0.275

1.65    		0.281

1.92    		0.281

Data set #12     Reference (68)

E(keV)  	BS yield

5.0     		0.298

30.0   		 0.291

Data set #13      Reference (106)

E(keV)		BS yield

0.1		0.146

0.2		0.284

0.3		0.339

0.4		0.356

0.6		0.375

0.8		0.384

1.0		0.381

1.5		0.384

2.0		0.379

3.0		0.361

4.0		0.34

Data set  #14     Reference (107)

E(keV)		BS yield

0.61		0.275

0.718		0.29

0.785		0.307

0.9		0.308

1.0		0.31

1.5		0.317

2.0		0.322

2.5		0.321

3.0		0.321

3.0		0.321

4.0		0.321

4.5		0.323

5.0		0.319

6.0		0.321

Zinc (Z=30)

Reference (1)

E(keV)  	BS yield

3.93    		0.3340

5.0     		0.3310

7.50    		0.3230

10.0    		0.3250

15.2    		0.3120

20.2    		0.3160

31.0    		0.3100

41.0    		0.3040

Data set #2     Reference (6)

E(keV)  	BS yield

5.00    		0.352

10.0    		0.342

30.0    		0.33

Data set #3      Reference (106)

E(keV)		BS yield

0.091		0.139

0.106		0.192

0.15		0.248

0.2		0.286

0.3		0.338

0.4		0.372

0.6		0.386

0.8		0.386

1.0		0.382

1.5		0.373

2.0		0.376

3.0		0.368

4.0		0.351

Gallium (Z=31)

Reference (106)

E(keV)		BS yield

0.1		0.146

0.2		0.241

0.4		0.334

0.6		0.366

0.8		0.371

1.0		0.376

2.0		0.369

3.0		0.364

4.0		0.35

Germanium (Z=32)

Reference (1)

E(keV)  	BS yield

3.93    		0.351

5.0     		0.34

7.5     		0.339

10.0    		0.331

15.2    		0.325

20.2    		0.319

31.0    		0.319

41.0    		0.317

Data set #2      Reference (2)

E(keV)  	BS yield

1.0    	 	0.34

3.0     		0.342

5.0     		0.339

10.0   		0.338

15.0    		0.337

20.0    		0.332

25.0    		0.335

30.0    		0.335

Data set #3       Reference (6)

E(keV)  	BS yield

5.0     		0.362

10.00   	0.349

30.0    		0.334

Data set #5      Reference (7)

E(keV)  	BS yield

28.0    		0.306

Data set #6      Reference (15)

E(keV)  	BS yield

9.3     		0.336

17.3    		0.327

25.2    		0.327

41.5    		0.317

62.1    		0.319

81.8    		0.315

102.2   	0.313

Data set #7      Reference (106)

E(keV)		BS yield

0.11		0.14

0.2		0.252

0.4		0.34

0.6		0.351

0.8		0.363

1.0		0.353

2.0		0.348

3.0		0.331

4.0		0.318

Arsenic (Z=33)

Reference (7)

E(keV)  	BS yield

4.50    		0.3800

11.00   	0.3170

28.0    		0.3080

Selenium (Z=34)

Reference (106)

E(keV)		BS yield

0.11		0.108

0.164		0.204

0.21		0.242

0.3		0.307

0.4		0.337

0.6		0.358

0.8		0.355

1.0		0.353

2.0		0.35

3.0		0.344

4.0		0.337

Strontium (Z=38)

Reference (106)

E(keV)		BS yield

0.116		0.09

0.16		0.133

0.2		0.173

0.3		0.239

0.4		0.282

0.5		0.297

0.6		0.307

0.8		0.325

1.0		0.33

2.0		0.344

3.0		0.348

4.0		0.352

Yttrium (Z=39)

Reference (106)

E(keV)		BS yield

0.2		0.253

0.3		0.277

0.4		0.296

0.5		0.310

0.6		0.323

0.8		0.339

1.0		0.349

2.0		0.352

3.0		0.352

Zirconium (Z=40)

Reference (1)

E(keV)  	BS yield

3.93    		0.3690

5.0     		0.3680

7.5     		0.3670

10.0    		0.3660

15.20   	0.3640

20.2    		0.3640

31.0    		0.3680

41.0    		0.3630

Data set #2      Reference (8)

E(keV)  	BS yield

10.0    		0.376

20.0    		0.379

30.0    		0.379

40.0    		0.381

49.0    		0.376

Data set #3      reference (68)

E(keV)  	BS yield

5.0     		0.346

30.0    		0.355

Niobium (Z=41)

reference (13)

E(keV)  	BS yield

15.0    		0.3850

20.0    		0.3870

30.0    		0.3870

40.0    		0.3870

50.0    		0.3860

60.0    		0.3840

Data set #2       Reference (7)

E(keV)  	BS yield

4.5     		0.393

11.0    		0.347

28.0    		0.333

Molybdenum (Z=42)

Reference (2)

E(keV)  	BS yield

3.0     		0.363

5.0     		0.379

10.0    		0.387

15.0    		0.387

20.0    		0.387

25.0    		0.387

30.0    		0.387

Data set #2       Reference (6)

E(keV)  	BS yield

5.0     		0.367

10.0    		0.381

30.0    		0.385

Data set #3      Reference (7)

E(keV)  	BS yield

28.0    		0.3327

Data set #4     Reference (8)

E(keV)  	BS yield

10.0    		0.384

20.0    		0.382

30.0    		0.386

40.0    		0.384

49.0    		0.377

Data set #6      Reference (34)

E(keV)  	BS yield

0.15    		0.138

0.5     		0.179

0.75    		0.204

1.0     		0.22

1.2     		0.236

1.5     		0.249

1.9     		0.266

Data set #7       Reference (35)

E(keV)  	BS yield

3.0     		0.329

4.0     		0.346

6.0     		0.357

8.0     		0.369

9.5     		0.376

12.5    		0.382

15.0    		0.381

17.0    		0.389

Data set #8     Reference (106)

E(keV)		BS yield

0.2		0.249

0.4		0.313

0.6		0.338

0.8		0.352

1.0		0.359

2.0		0.369

3.0		0.372

4.00		0.381

Palladium (Z=46)

Reference (8)

E(keV)  	BS yield

10.0   		0.4030

20.0    		0.4050

30.0    		0.3970

40.0    		0.4020

49.0    		0.3980

Silver (Z=47)

Reference (1)

E(keV)  	BS yield

3.93    		0.394

5.0     		0.393

7.5     		0.395

10.0    		0.394

15.2    		0.394

20.2    		0.398

31.0    		0.396

41.0    		0.395

Data set #2      Reference (2)

E(keV)  	BS yield

3.0     		0.371

5.0     		0.392

10.0    		0.411

15.0    		0.415

20.0    		0.415

30.0    		0.415

Data set #3      Reference (4)

E(keV)  	BS yield

0.8     		0.25

1.0     		0.297

1.2     		0.298

1.4     		0.318

1.6     		0.331

1.8     		0.339

2.0     		0.35

2.5     		0.359

3.0     		0.359

3.5     		0.37

4.0     		0.373

5.0     		0.372

Data set #4      Reference (5)

E(keV)  	BS yield

1.0     		0.47

3.0     		0.4614

5.0     		0.454

10.0    		0.4449

Data set #5      Reference (6)

E(keV)  	BS yield

5.0     		0.418

10.0    		0.42

20.0    		0.419

30.0    		0.42

Data set #6       Reference (7)

E(keV)  	BS yield

4.5     		0.42

11.0    		0.365

28.0    		0.361

Data set #7       Reference (8)

E(keV)  	BS yield

10.0    		0.397

20.0    		0.408

30.0    		0.407

40.0    		0.403

49.0    		0.402

Data set  #8       Reference (13)

E(keV)  	BS yield

15.0    		0.423

20.0    		0.422

30.0    		0.42

40.0    		0.419

50.0    		0.418

60.0    		0.417

Data set #9     Reference (15)

E(keV)  	BS yield

9.3     		0.407

17.3    		0.406

25.2    		0.403

41.5    		0.405

62.1    		0.399

81.8    		0.402

102.2   	0.399

Data set #10      Reference (22)

E(keV)  	BS yield

5.0     		0.38

20.0    		0.40

45.0    		0.41

Data set #11      Reference (35)

E(keV)  	BS yield

3.0     		0.357

5.0     		0.383

6.0     		0.383

7.0     		0.391

9.0     		0.41

11.0    		0.406

13.0    		0.407

15.0    		0.409

Data set #12       Reference (68)

E(keV)  	BS yield

5.0     		0.361

30.0    		0.388

Data set #13      Reference (106)

E(keV)		BS yield

0.1		0.134

0.2		0.224

0.4		0.314

0.6		0.354

0.8		0.372

1.0		0.366

2.0		0.396

3.0		0.410

4.0		0.415

Data set #14     Reference (107)

E(keV)		BS yield

0.6		0.348

0.9		0.374

1.0		0.378

1.5		0.382

2.0		0.389

2.5		0.389

3.0		0.389

4.0		0.392

4.5		0.393

5.0		0.394

4.0		0.402

Cadmium (Z=48)

Reference (1)

E(keV)  	BS yield

3.93    		0.3970

5.00    		0.4010

7.50    		0.4060

10.0    		0.4030

15.2    		0.4000

20.20   	0.3990

31.00   	0.4030

41.00   	0.4020

Data set #2       Reference (106)

E(keV)		BS yield

0.1		0.128

0.2		0.219

0.3		0.279

0.4		0.321

0.5		0.351

0.6		0.366

0.8		0.377

1.0		0.377

2.0		0.385

3.0		0.393

4.0		0.393

Indium (Z=49)

Reference (2)

E(keV)  	BS yield

3.0     		0.3840

5.0     		0.4080

10.0    		0.4190

15.0    		0.4190

20.0    		0.4190

30.0    		0.4190

Data set #2        Reference (106)

E(keV)		BS yield

0.116		0.154

0.2		0.235

0.4		0.330

0.6		0.365

0.8		0.381

1.0		0.392

2.0		0.4

3.0		0.406

4.0		0.416

Tin (Z=50)

Reference (1)

E(keV)  	BS yield

3.93    		0.399

5.0     		0.4

7.5    		0.406

10.0    		0.407

15.2    		0.404

20.2   		0.41

31.0    		0.411

41.0    		0.409

Data set #2      Reference (2)

E(keV)  	BS yield

3.0     		0.39

5.0     		0.417

10.0    		0.429

15.0    		0.429

20.0    		0.429

30.0    		0.429

Data set #3      Reference (8)

E(keV)  	BS yield

20.0    		0.394

30.0    		0.416

40.0    		0.417

49.0    		0.415

Data set #4       Reference (7)

E(keV)  	BS yield

4.5     		0.425

11.0    		0.37

28.0   		0.38

Data set #5      Reference (106)

E(keV)		BS yield

0.1		0.135

0.2		0.240

0.3		0.293

0.4		0.338

0.6		0.364

0.8		0.371

1.0		0.371

2.0		0.394

3.0		0.401

4.0		0.405

Antimony (Z=51)

Reference  (1)

E(keV)  	BS yield

3.93    		0.399

5.0     		0.407

7.5     		0.408

10.0    		0.413

20.2    		0.412

31.0    		0.413

41.0    		0.408

Data set #2      Reference (2)

E(keV)  	BS yield

3.0     		0.394

5.0     		0.417

10.0    		0.435

15.0    		0.436

20.0    		0.436

30.0    		0.436

Data set #3     Reference (8)

E(keV)  	BS yield

10.0    		0.42

20.0    		0.423

30.0    		0.423

40.0    		0.426

49.0    		0.427

Tellurium (Z=52)

Reference (1)

E(keV)  	BS yield

3.93    		0.408

5.0     		0.416

7.5     		0.416

10.0    		0.415

15.2    		0.413

20.2    		0.418

31.0    		0.418

41.0    		0.416

Data set #2      Reference (2)

E(keV)  	BS yield

3.0     		0.39

5.0     		0.419

10.0    		0.444

15.0    		0.447

20.0    		0.447

30.0    		0.447

Data set #3      Reference (7)

E(keV)  	BS yield

28.0    		0.3765

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.425

20.0    		0.427

30.0    		0.427

40.0    		0.426

49.0    		0.431

Data set #5        Reference (52)

E(keV)  	BS yield

5.0     		0.389

30.0    		0.408

Barium (Z=56)

Reference (106)

E(keV)		BS yield

0.1		0.095

0.2		0.19

0.4		0.295

0.6		0.345

0.8		0.363

1.0		0.373

2.0		0.398

3.0		0.405

4.0		0.405

Lanthanum (Z=57)

Reference (106)

E(keV)		BS yield

0.2		0.229

0.4		0.282

0.6		0.319

0.8		0.342

1.0		0.354

2.0		0.368

3.0		0.376

Samarium (Z=62)

Reference (1)

E(keV)  	BS yield

3.93    		0.4280

5.0     		0.4380

7.5     		0.4310

10.0    		0.4410

15.2    		0.4410

20.2    		0.4500

31.0    		0.4540

41.0    		0.4570

Hafnium (Z=72)

Reference (1)

E(keV)	 	BS yield

3.93    		0.4390

5.0     		0.4500

7.5     		0.4560

10.0    		0.4630

15.2    		0.4660

20.2    		0.4730

31.0    		0.4760

41.0    		0.4770

Tantalum (Z=73)

Reference (1)

E(keV)  	BS yield

3.93    		0.443

5.0     		0.451

7.5     		0.454

10.0    		0.46

15.2    		0.467

20.2    		0.468

31.0    		0.472

41.0    		0.473

Data set #2       Reference (7)

E(keV)  	BS yield

28.0    		0.432

Data set #3      Reference (8)

E(keV)  	BS yield

10.0    		0.481

20.0    		0.491

30.0    		0.487

40.0    		0.501

49.0    		0.503

Data set #4       Reference (13)

E(keV)  	BS yield

15.0    		0.49

20.0    		0.496

30.0    		0.5

40.0    		0.503

50.0    		0.504

60.0    		0.5

Data set #5      Reference (16)

E(keV)  	BS yield

2.0     		0.567

3.0     		0.571

5.0     		0.586

8.0     		0.58

10.0    		0.563

Data set #6      Reference (34)

E(keV)  	BS yield

0.4     		0.149

0.8     		0.186

1.2     		0.255

1.65    		0.3

2.0     		0.319

2.75    		0.371

3.2     		0.381

3.8     		0.39

Data set #7       Reference (106)

E(keV)		BS yield

0.2		0.144

0.3		0.241

0.4		0.289

0.5		0.340

0.6		0.373

0.8		0.409

1.0		0.421

2.0		0.421

5.0		0.420

Data set #8      Reference (112)

E(keV)		BS yield

0.078		0.205

0.113		0.293

0.21		0.407

0.32		0.457

0.4		0.467

0.48		0.487

0.57		0.503

0.65		0.518

0.73		0.516

0.8		0.519

0.93		0.518

1.03		0.511

1.123		0.51

1.20		0.513

Tungsten (Z=74)

Reference (1)

E(keV)  	BS yield

3.93    		0.438

5.0     		0.449

7.5     		0.457

10.0    		0.46

15.2    		0.467

20.2    		0.469

31.0    		0.478

41.0    		0.477

Data set #2       Reference (2)

E(keV)  	BS yield

3.0     		0.413

5.0     		0.436

10.0    		0.471

15.0    		0.482

20.0    		0.482

30.0    		0.482

Data set #3     Reference (6)

E(keV)  	BS yield

5.0     		0.472

10.0    		0.483

30.0    		0.501

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.482

20.0    		0.494

30.0    		0.489

40.0    		0.499

49.0    		0.506

Data set #5      Reference (35)

E(keV)  	BS yield

1.5     		0.336

2.0     		0.354

3.0     		0.387

4.0     		0.406

6.0     		0.431

8.0     		0.451

10.0    		0.457

12.0    		0.466

14.0    		0.469

16.0    		0.459

Data set #6      Reference (7)

E(keV)  	BS yield

4.5     		0.473

11.0    		0.433

28.0    		0.434

Data set #7       Reference (106)

E(keV)		BS yield

0.2		0.169

0.4		0.311

0.6		0.391

0.8		0.436

1.0		0.459

2.0		0.461

Iridium (Z=77)

Reference (8)

E(keV)  	BS yield

30.0    		0.4987

Platinum (Z=78)

Reference (1)

E(keV)  	BS yield

3.93    		0.457

5.0     		0.463

7.5     		0.467

10.0    		0.475

15.2    		0.478

20.2    		0.49

31.0    		0.492

41.0    		0.491

Data set #2       Reference (6)

E(keV)  	BS yield

5.0     		0.486

10.0    		0.503

20.0    		0.511

30.0    		0.516

Data set #3       Reference (8)

E(keV)  	BS yield

10.0    		0.486

20.0    		0.504

30.0    		0.499

40.0    		0.503

49.0    		0.51

Data set #4      Reference (34)

E(keV)  	BS yield

0.25    		0.176

0.6     		0.223

0.8     		0.247

1.2     		0.289

1.6     		0.317

1.9     		0.329

2.5     		0.376

3.0     		0.376

3.6     		0.388

Data set #5       Reference (35)

E(KeV)  	BS yield

2.0     		0.365

3.0     		0.406

4.0     		0.417

5.0     		0.431

6.0     		0.44

8.0     		0.461

10.0    		0.467

12.0    		0.477

14.0    		0.479

Data set #6       Reference (106)

E(keV)		BS yield

0.2		0.165

0.3		0.232

0.4		0.278

0.6		0.355

0.8		0.402

1.0		0.435

1.55		0.461

2.0		0.46

3.0		0.469

4.0		0.466

Data set #7       Reference (112)

E(keV)		BS yield

0.08		0.102

0.114		0.156

0.16		0.204

0.23		0.23

0.3		0.269

0.4		0.301

0.55		0.36

0.66		0.394

0.8		0.423

0.88		0.438

1.0		0.449

1.2		0.475

Gold (Z=79)

Reference (1)

E(keV)  	BS yield

3.93    		0.45

5.0     		0.469

7.5     		0.465

10.0    		0.476

15.2    		0.484

20.2    		0.485

31.0    		0.49

41.0    		0.494

Data set #2       Reference (2)

E(keV)  	BS yield

3.0     		0.415

5.0     		0.448

10.0    		0.471

15.0    		0.482

20.0    		0.482

30.0    		0.482

Data set #3       Reference (4)

E(keV)  	BS yield

0.8     		0.245

1.0     		0.289

1.2     		0.325

1.4     		0.339

1.6     		0.349

1.8     		0.376

2.0     		0.373

2.5     		0.386

3.0     		0.414

3.5     		0.428

4.0     		0.443

5.0     		0.459

Data set #4      Reference (6)

E(keV)  	BS yield

5.0     		0.489

10.0    		0.501

30.0    		0.521

Data set #5      Reference (8)

E(keV)  	BS yield

10.0    		0.483

20.0    		0.506

30.0    		0.512

40.0    		0.51

49.0    		0.511

Data set #6     Reference (13)

E(keV)  	BS yield

15.0    		0.514

20.0    		0.516

30.0    		0.519

40.0    		0.521

50.0    		0.523

60.0    		0.525

Data set #7      Reference (15)

E(keV)  	BS yield

9.3     		0.478

17.3    		0.492

25.2    		0.501

41.5    		0.507

62.1    		0.513

81.8    		0.51

102.2   	0.513

Data set #8     Reference (22)

E(keV)  	BS yield

5.0     		0.43

10.0    		0.47

20.0    		0.48

45.0    		0.5

Data set #9      Reference (68)

E(keV)  	BS yield

5.0     		0.432

30.0    		0.481

Data set #10      Reference (106)

E(keV)		BS yield

0.1		0.082

0.2		0.14

0.3		0.20

0.4		0.256

0.6		0.357

0.8		0.407

1.0		0.419

2.0		0.45

3.0		0.464

4.0		0.461

Data set #11     Reference (107)

E(keV)		BS yield

0.61		0.367

0.9		0.387

1.0		0.395

1.51		0.411

2.0		0.428

2.5		0.444

3.0		0.451

3.5		0.455

4.0		0.459

4.5		0.458

5.0		0.461

6.0		0.471

Data set #12	  Reference (132)

E(keV)	BS Yield

20		  0.51

Mercury (Z=80)

Reference (106)

E(keV)		BS yield

0.21		0.112

0.42		0.246

0.6		0.32

0.8		0.369

1.2		0.42

1.6		0.438

2.0		0.443

2.4		0.448

Thallium (Z=81)

Reference (106)

E(keV)		BS yield

0.09		0.057

0.15		0.102

0.2		0.131

0.3		0.197

0.4		0.248

0.6		0.332

0.8		0.397

1.0		0.414

2.0		0.445

3.0		0.462

4.0		0.461

Lead (Z=82)

Reference (106)

E(keV)		BS yield

0.2		0.151

0.3		0.208

0.4		0.255

0.6		0.334

0.8		0.377

1.0		0.41

2.0		0.441

3.0		0.451

4.00		0.453

Bismuth (Z=83)

Reference (1)

E(keV)  	BS yield

3.93    		0.453

5.0     		0.47

7.5     		0.475

10.0    		0.488

15.2    		0.492

20.2    		0.493

31.0    		0.50

41.0    		0.493

Data set #2      Reference (2)

E(keV)  	BS yield

3.0     		0.43

5.0     		0.477

10.0    		0.509

15.0    		0.515

20.0    		0.517

30.0    		0.521

Data set #3      Reference (7)

E(keV)  	BS yield

4.5     		0.48

11.0    		0.448

28.0    		0.4442

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.498

20.0    		0.513

30.0    		0.516

40.0    		0.519

49.0    		0.521

Data set  #5      Reference (68)

E(keV)  	BS yield

5.0     		0.447

30.0    		0.489

Uranium (Z=92)

Reference (1)

E(keV)  	BS yield

3.93    		0.468

5.0     		0.476

7.5     		0.481

10.0    		0.481

15.2    		0.496

20.2    		0.504

31.0    		0.51

41.0   		0.511

Data set #2      Reference (2)

E(keV)  	BS yield

5.0     		0.495

10.0    		0.513

20.0    		0.526

30.0    		0.534

Data set #3      Reference (7)

E(keV)  	BS yield

4.5     		0.483

11.0    		0.455

28.0    		0.46

Data set #4      Reference (8)

E(keV)  	BS yield

10.0    		0.495

20.0    		0.52

30.0    		0.527

40.0    		0.527

49.0    		0.53

Data set #5      Reference (13)

E(keV)  	BS yield

15.0    		0.426

20.0    		0.531

30.0    		0.537

40.0    		0.542

50.0    		0.545

60.0   		0.548

Data set #6       Reference (15)

E(keV)  	BS yield

9.3     		0.498

17.3    		0.516

25.2    		0.527

41.5    		0.524

62.1    		0.541

81.8   		0.542

102.2   	0.562

COAT725 (wafer coat)

Reference (86)

E(keV)  	BS yield

0.500  		0.130

0.700   	0.125

1.000   	0.130

1.500   	0.130

2.000   	0.125

3.000   	0.128

4.000   	0.125

5.000   	0.125

7.000   	0.123

10.000  	0.125

Indium Tin Oxide (ITO)

Reference (131)

E(keV)		BS yield

0.5		0.16

1		0.17

1.5		0.18

2		0.19

3		0.2

5		0.21

7		0.25

10		0.26

Indium Zinc Oxide (IZO)

Reference (131)

E(keV)		BS yield

0.15		0.16

1.5		0.21

5		0.21

7		0.26

10		0.27

Interconnect line Aluminum

Reference (86)

E(keV)  	BS yield

10.000  	0.150

7.000   	0.155

5.000   	0.155

4.000   	0.160

3.000   	0.170

2.000   	0.175

1.500   	0.180

1.000   	0.180

0.700   	0.190

0.500   	0.187

PETEOS

Reference (86)

E(keV)  	BS yield

10.000  	0.080

7.0000  	0.080

5.000   	0.083

4.000   	0.080

3.000   	0.078

2.000   	0.082

1.500   	0.085

1.000   	0.085

0.700   	0.085

0.500   	0.087

Resist (e-beam –PMMA) )

Reference (86)

E(keV)  	BS yield

10.000  	0.060

7.000   	0.060

5.000   	0.065

4.000   	0.070

3.000   	0.065

2.000   	0.070

1.500   	0.070

1.000   	0.080

0.700   	0.090

0.500   	0.105

Silicon (amorphous)

Reference (86)

E(keV) 	BS yield

0.5		0.21

0.7		0.21

1.0		0.21

1.5		0.21

2.0		0.21

3.0		0.2

4.0		0.2

5.0		0.2

7.0		0.2

10.0		0.19

Silicon Dioxide SiO2 (steam formed)

Reference (86)

E(keV)  	BS yield

10.000  	0.213

7.000   	0.233

5.000   	0.238

4.000   	0.235

3.000   	0.245

2.000   	0.255

1.000   	0.250

0.700   	0.246

0.500   	0.246

Tantalum Carbide TaC

Reference (112)

E(keV) 	BS yield

0.096		0.07

0.13		0.119

0.193		0.163

0.295		0.181

0.4		0.198

0.5		0.202

0.61		0.205

0.8		0.212

0.92		0.218

1.06		0.222

1.2		0.223

Titanium Carbide TiC

Reference (112)

E(keV) 	BS yield

0.137		0.049

0.182		0.135

0.25		0.188

0.34		0.223

0.4		0.237

0.52		0.246

0.63		0.262

0.8		0.259

0.93		0.249

1.09		0.25

1.2		0.261

U-V Resist

Reference (86)

E(keV) 	BS yield

0.5		0.082

0.7		0.082

1.0		0.082

1.5		0.08

2.0		0.081

3.0		0.08

4.0		0.08

5.0		0.08

7.0		0.082

10.0		0.08

Vanadium Pentoxide V2O5

Reference (83)

E(keV)  	BS yield

0.079   	0.118

0.137   	0.153

0.211   	0.126

0.320   	0.107

0.380   	0.095

0.488   	0.103

0.705   	0.106

0.981   	0.104

1.400   	0.110

1.800   	0.102

2.000   	0.112

2.520   	0.113

3.000   	0.113

4.000   	0.107

5.000   	0.109

Zirconium Carbide ZrC

Reference (112)

E(keV) 	BS yield

0.106		0.114

0.18		0.174

0.252		0.196

0.35		0.205

0.4		0.206

0.53		0.201

0.68		0.207

0.8		0.204

0.96		0.195

1.2		0.195

SECTION Three

Electron Stopping Power Data

(a) for elements, arranged in ascending atomic number

(b) for compounds, sorted in alpha-numeric order

Carbon (Z=6)

Reference (54)

E(keV)		SP(eV/A)

0.01		0.016

0.02		0.065

0.03		3.162

0.04		5.23

0.05		6.49

0.06		6.98

0.08		7.61

0.1		7.5

0.2		5.87

0.3		4.53

0.5		3.65

0.7		3.16

1.0		2.55

2.0		1.56

Data set #2     Reference (89)

E(keV)		SP(eV/A)

0.001		0.005

0.003		0.053

0.005		0.157

0.007		0.307

0.01		0.529

0.015		0.984

0.02		1.79

0.03		4.459

0.04		6.43

0.05		7.45

0.06		7.94

0.07		8.144

0.08		8.176

0.1		7.99

0.15		7.19

0.2		6.463

0.3		5.33

0.5		4.076

0.7		3.36

1.0		2.7

1.5		2.07

2.0		1.7

3.0		1.27

3.5		1.14

Aluminum (Z=13)

Reference (46)

E(keV)		SP(eV/A)

0.65		1.54

1.0		1.24

1.15		1.15

2.0		0.916

2.7		0.75

4.25		0.657

Data set #2       Reference (74)

E(keV)		SP(eV/A)

0.53		1.628

1.45		1.29

2.04		0.895

3.33		0.811

4.42		0.74

5.54		0.654

6.63		0.51

7.7		0.421

8.71		0.408

9.73		0.39

Data set #3      Reference (75)

E(keV)		SP(eV/A)

2.0		1.144

3.0		0.682

5.0		0.484

7.0		0.308

8.5		0.242

10.0		0.207

Data set #4      Reference (76)

E(keV)		SP(eV/A)

0.42		2.86

0.45		2.31

0.5		3.08

0.6		3.08

0.65		3.04

0.75		3.26

0.85		2.93

0.95		3.19

Data set #5      Reference (78)

E(keV)		SP(eV/A)

20.0		0.22

30.0		0.163

40.0		0.132

Data set #6      Reference (89)

E(keV)		SP(eV/A)

0.01		0.398

0.015		0.85

0.02		3.089

0.025		4.013

0.03		4.517

0.04		4.867

0.05		4.856

0.06		4.783

0.07		4.65

0.08		4.496

0.09		4.421

0.1		4.365

0.15		4.241

0.2		4.114

0.3		3.732

0.4		3.366

0.5		3.095

0.6		2.844

0.8		2.458

0.9		2.303

1.0		2.148

1.55		1.589

1.6		1.467

2.0		1.269

3.0		0.964

4.0		0.787

5.0		0.670

6.0		0.586

7.0		0.523

8.0		0.473

9.0		0.432

Silicon (Z=14)

Reference (47)

E(keV)		SP(eV/A)

0.002		0.003

0.003		0.084

0.005		0.265

0.007		0.303

0.01		0.54

0.02		3.02

0.03		4.71

0.05		4.71

0.07		4.70

0.1		4.47

0.2		3.61

0.3		3.16

0.5		2.42

1.0		1.78

2.0		1.2

3.0		1.0

5.0		0.702

7.0		0.514

10.0		0.39

Chromium (Z=24)

Reference (77)

E(keV)		SP(eV/A)

0.001		0.0001

0.002		0.0013

0.003		0.0098

0.005		0.059

0.007		0.12

0.01		0.265

0.02		1.42

0.03		3.16

0.05		5.38

0.07		5.87

0.1		6.09

0.2		5.67

0.3		4.92

0.5		4.5

0.7		4.12

1.0		3.78

2.0		2.89

3.0		2.10

5.0		1.7

7.0		1.3

10.0		1.0

Nickel (Z=28)

Reference (74)

E(keV)		SP(eV/A)

1.08		4.69

2.09		3.825

3.45		3.044

4.57		2.585

5.62		2.55

6.44		2.19

7.55		1.86

8.57		1.83

9.64		1.57

Copper (Z=29)

Reference (47)

E(keV)		SP(eV/A)

0.01		0.43

0.02		1.44

0.04		2.41

0.05		5.21

0.06		5.82

0.08		6.15

0.1		6.72

0.15		7.13

0.325		7.24

0.5		5.67

1.0		5.17

2.0		3.74

6.0		1.7

10.0		1.14

Data set #2       Reference (74)

E(keV)		SP(eV/A)

1.22		3.81

1.59		3.21

3.15		2.792

4.45		2.19

5.51		2.12

6.67		1.56

7.7		1.47

8.73		1.38

9.75		1.28

Data set #3      Reference (89)

E(keV)		SP(eV/A)

0.001		0.000

0.003		0.016

0.005		0.088

0.007		0.184

0.01		0.453

0.015		1.023

0.02		1.777

0.03		3.34

0.04		4.504

0.05		5.3

0.06		5.88

0.07		6.31

0.08		6.654

0.1		7.19

0.2		7.6

0.3		7.02

0.4		6.44

0.5		5.93

0.6		5.485

0.7		5.105

0.8		4.779

0.9		4.494

1.0		4.259

1.5		3.446

3,0		2.29

4.0		1.92

8.0		1.21

9.0		1.11

10.0		1.03

Germanium (Z=32)

Reference (77)

E(keV)		SP(eV/A)

0.001		0.007

0.002		0.017

0.003		0.050

0.005		0.119

0.007		0.210

0.01		0.35

0.02		4.13

0.03		6.43

0.05		6.35

0.07		6.51

0.1		5.64

0.2		4.44

0.3		3.85

0.5		3.11

0.7		2.66

1.0		2.30

2.0		1.71

3.0		1.32

5.0		1.02

7.0		0.78

10.0		0.60

Palladium (Z=46)

Reference (77)

E(keV)		SP(eV/A)

0.001		0.005

0.002		0.013

0.003		0.031

0.005		0.111

0.007		0.278

0.01		0.514

0.02		1.36

0.03		2.59

0.05		5.14

0.07		5.93

0.1		6.99

0.2		7.74

0.3		7.36

0.5		6.31

0.7		5.58

1.0		4.64

2.0		3.41

3.0		2.75

5.0		1.94

7.0		1.58

10.0		1.24

Silver (Z=47)

Reference (74)

E(keV)		SP(eV/A)

1.90		3.074

1.99		2.373

3.67		2.12

5.01		2.04

6.27		1.77

7.4		1.606

8.45		1.60

9.57		1.33

Platinum (Z=78)

Reference (77)

E(keV)		SP(eV/A)

0.001		0.001

0.002		0.004

0.003		0.01

0.005		0.046

0.007		0.147

0.01		0.316

0.02		1.12

0.03		2.02

0.05		5.99

0.07		8.80

0.1		11.36

0.2		13.08

0.3		12.27

0.5		11.07

0.7		10.1

1.0		7.86

2.0		5.84

3,0		3.6

5.0		3.16

7.0		2.51

10.0		2.02

Data set #2       Reference (89)

E(keV)		SP(eV/A)

0.001		0.001

0.005		0.065

0.010		0.352

0.015		0.75

0.02		1.286

0.03		3.084

0.04		5.44

0.053		7.606

0.072		9.478

0.1		10.51

0.2		10.187

0.3		9.34

0.4		8.70

0.5		8.20

0.61		7.74

0.90		6.78

1.0		6.47

1.53		5.40

2.0		4.72

3.0		3.79

4.0		3.23

5.0		2.83

7.0		2.30

10.0		1.83

Gold (Z=79)

Reference (47)

E(keV)		SP(eV/A)

0.003		0.01

0.005		0.05

0.007		0.14

0.01		0.30

0.02		1.28

0.03		2.50

0.05		5.10

0.07		6.81

0.10		8.25

0.2		8.3

0.3		7.5

0.5		6.81

0.7		6.19

1.0		5.11

2.0		3.83

3.0		3.01

5.0		2.37

7.0		1.96

10.0		1.56

Data set #2       Reference (74)

E(keV)		SP(eV/A)

2.02		2.61

2.11		2.86

2.12		2.64

2.53		2.91

2.83		2.83

3.43		2.82

3.52		2.86

3.66		2.76

4.24		2.7

4.41		2.66

5.01		2.45

5.10		2.34

5.12		2.46

5.76		2.30

5.91		2.23

7.27		2.23

8.67		2.00

Lead (Z=82)

Reference (47)

E(keV)		SP(eV/A)

0.01		0.474

0.02		2.10

0.03		3.62

0.05		4.94

0.07		4.92

0.1		4.91

0.2		4.32

0.3		3.87

0.5		3.16

0.7		2.58

1.0		2.41

2.0		1.84

3.0		1.40

5.0		1.16

10.0		0.873

Alumina (sapphire) Al2O3

Reference (77)

E(keV)		SP(eV/A)

0.01		0.004

0.02		0.332

0.03		2.23

0.05		5.22

0.07		6.06

0.1		6.44

0.2		6.06

0.3		5.43

0.5		4.27

0.7		3.86

1.0		3.32

2.0		2.01

3.0		1.65

5.0		1.22

7.0		0.9

10.0		0.672

Data set #2        Reference (89)

E(keV)		SP(eV/A)

0.001		0.013

0.015		0.185

0.02		0.66

0.03		2.66

0.04		4.40

0.05		5.48

0.07		6.43

0.1		6.75

0.2		6.075

0.3		5.23

0.4		4.58

0.5		4.077

0.7		3.37

1.0		2.712

1.5		2.08

2.0		1.71

3.0		1.28

5.0		0.878

7.0		0.677

Bismuth High Tc superconductor

Reference (47)

E(keV)		SP(eV/A)

0.01		0.18

0.02		0.87

0.03		1.84

0.05		3.62

0.1		4.75

0.2		4.43

0.3		3.87

0.5		2.87

1.0		1.84

2.0		1.00

3.0		0.77

5.0		0.58

10.0		0.38

CuAu (50:50) alloy

Reference (47)

E(keV)		SP(eV/A)

0.001		0.001

0.002		0.003

0.003		0.011

0.005		0.061

0.007		0.166

0.01		0.349

0.02		1.389

0.03		3.11

0.05		5.71

0.07		6.634

0.1		6.988

0.2		6.332

0.3		5.715

0.5		4.92

0.7		4.42

1.0		3.925

2.0		3.059

3.0		2.592

5.0		2.01

7.0		1.665

10.0		1.314

GaAs

Reference (47)

E(keV)		SP(eV/A)

0.01		0.513

0.02		2.32

0.03		3.79

0.04		4.33

0.05		4.83

0.06		5.42

0.07		5.50

0.08		5.45

0.1		5.45

0.2		4.28

0.3		3.70

0.5		3.16

0.7		2.91

1.0		2.48

2.0		1.88

3.0		1.53

5.0		1.26

7.0		1.07

10.0		0.79

GaSb

Reference (77)

E(keV)		SP(eV/A)

0.002		0.003

0.003		0.007

0.005		0.041

0.007		0.103

0.01		0.256

0.02		3.113

0.03		4.33

0.05		4.95

0.07		4.47

0.1		4.29

0.2		3.75

0.3		3.28

0.5		2.67

0.7		2.40

1.0		2.06

2.0		1.48

3.0		1.27

5.0		1.09

7.00		0.83

10.0		0.61

Guanine

Reference (77)

E(keV)		SP(eV/A)

0.003		0.002

0.005		0.018

0.007		0.10

0.01		0.238

0.02		1.205

0.03		3.14

0.05		5.37

0.07		5.57

0.10		5.71

0.2		4.45

0.3		3.6

0.5		2.88

0.7		2.36

1.0		1.86

2.0		1.21

3.0		0.88

5.0		0.64

7.0		0.435

10.0		0.337

Ice (pure water as vitreous ice)

Reference (47)

E(keV)		SP(eV/A)

0.01		0.3

0.03		1.95

0.04		2.44

0.07		2.93

0.1		3.00

0.2		2.55

0.3		2.12

0.5		1.92

0.7		1.4

1.0		1.2

2.0		0.74

3.0		0.6

5.0		0.37

10.0		0.3

Data set #2       Reference (73)

E(keV)		SP(eV/A)

0.007		0.004

0.008		0.006

0.009		0.018

0.01		0.032

0.02		0.7

0.03		1.92

0.04		2.78

0.05		3,27

0.06		3.53

0.07		3.66

0.08		3.68

0.09		3.67

0.10		3.64

0.2		3.00

0.3		2.51

0.4		2.16

0.5		1.90

0.7		1.55

1.0		1.24

2.0		0.76

3.0		0.57

5.0		0.38

7.0		0.29

10.0		0.22

InSb

Reference (77)

E(keV)		SP(eV/A)

0.001		0.002

0.002		0.007

0.003		0.017

0.005		0.053

0.007		0.0127

0.010		0.357

0.02		2.98

0.03		3.90

0.05		4.217

0.07		4.215

0.1		4.12

0.2		3.39

0.3		3.20

0.5		2.69

0.7		2.40

1.0		1.89

2.0		1.45

3.0		1.26

5.0		0.63

7.0		0.50

10.0		0.43

MgO

Reference (77)

E(keV)		SP(eV/A)

0.01		0.056

0.02		1.08

0.03		3.83

0.05		5.97

0.07		6.47

0.10		6.17

0.2		5.26

0.3		4.87

0.5		4.155

0.7		3.69

1.0		3.15

2.0		2.04

3.0		1.607

5.0		1.17

7.0		0.723

10.0		0.548

MoS2

Reference (77)

E(keV)		SP(eV/A)

0.005		0.02

0.007		0.066

0.01		0.146

0.02		0.668

0.03		1.58

0.05		3.35

0.07		4.07

0.1		4.57

0.2		4.57

0.3		4.12

0.5		3.39

0.7		2.98

1.0		2.66

2.0		1.78

3.0		1.41

5.0		1.03

7.0		0.794

10.0		0.623

SiC

Reference (47)

E(keV)		SP(eV/A)

0.005		0.033

0.007		0.07

0.01		0.10

0.02		1.05

0.03		4.92

0.05		7.02

0.07		7.33

0.1		7.3

0.2		6.42

0.3		5.15

0.5		3.77

0.7		3.45

1.0		2.90

2.0		2.32

3.0		1.94

5.0		1.08

7.0		0.84

10.0		0.64

SiO2 (as quartz)

Reference (77)

E(keV)		SP(eV/A)

0.03		0.823

0.05		3.89

0.07		4.70

0.1		4.44

0.2		3.81

0.3		3.48

0.5		2.87

0.7		2.57

1.0		2.15

2.0		1.43

3.0		1.149

5.0		0.779

7.0		0.59

10.0		0.447

Data set #2      Reference (89)

E(keV)		SP(eV/A)

0.01		0.003

0.015		0.245

0.02		0.81

0.03		2.575

0.04		3.613

0.052		4.264

0.069		4.67

0.1		4.71

0.151		4.388

0.2		4.065

0.3		3.49

0.4		3.05

0.5		2.73

0.6		2.50

0.8		2.11

1.0		1.834

2.0		1.18

3.0		0.89

4.0		0.723

5.0		0.612

6.0		0.534

7.0		0.475

8.6		0.404

ZnS

Reference (89)

E(keV)		SP(eV/A)

0.01		0.02

0.015		0.8

0.02		1.82

0.025		2.88

0.053		4.44

0.1		4.45

0.13		4.24

0.15		4.08

0.2		3.75

0.4		2.87

0.5		2.60

0.61		2.36

0.71		2.18

0.82		2.01

0.9		1.90

1.0		1.77

1.1		1.69

1.3		1.53

1.5		1.398

2.0		1.16

2.5		1.0

3.0		0.89

4.0		0.731

5.0		0.625

6.0		0.55

7.0		0.49

8.0		0.445

9.0		0.408

10.0		0.378

ZnSe

Reference (89)

E(keV)		SP(eV/A)

0.003		0.013

0.01		0.549

0.015		1.518

0.02		2.20

0.03		2.92

0.05		3.17

0.06		3.17

0.07		3.164

0.1		3.169

0.15		3.18

0.2		3.22

0.3		3.119

0.53		2.727

0.62		2.57

0.76		2.37

0.99		2.10

1.61		1.64

2.0		1.467

3.0		1.168

4.0		0.987

5.0		0.852

6.0		0.755

7.0		0.68

8.0		0.62

9.0		0.57

ZnTe

Reference (89)

E(keV)		SP(eV/A)

0.005		0.037

0.01		0.43

0.015		0.984

0.02		1.655

0.037		2.640

0.05		3.057

0.06		3.322

0.07		3.56

0.08		3.787

0.1		4.236

0.136		4.60

0.20		4.51

0.31		4.08

0.413		3.68

0.53		3.31

0.62		3.09

0.76		2.824

0.82		2.74

1.03		2.448

1.6		1.96

2.0		1.74

3.0		1.38

4.0		1.152

5.0		0.997

6.0		0.884

7.0		0.797

8.0		0.727

9.0		0.67

10.0		0.622

SECTION FOUR

Experimental X-ray Ionization Cross-sections

for elements, arranged in ascending atomic number/line type

Carbon (Z=6) K line

Reference (37)

E(keV)		sigma (barns)

0.29		69100

0.3		94400

0.35		146000

0.4		194000

0.5		250000

0.6		293000

0.7		303000

0.8		327000

0.9		326000

1.0		328000

1.25		326000

1.5		321000

1.75		305000

2.0		289000

3.0		242000

4.0		211000

5.0		183000

6.0		165000

8.5		133000

10.6		117000

12.6		102000

14.7		91800

16.8		85500

Data set #2      Reference (38)

E(keV)		sigma (barns)

2.0		453000

3.0		338000

4.0		278000

5.0		226000

7.0		177000

10.0		129000

15.0		90700

20.0		72100

25.0		59900

30.0		52400

Data set #3      Reference (39)

E(keV)		sigma (barns)

25.0		75000

Data set #4       Reference (40)

E(keV)		sigma (barns)

75.0		6000

Data set #5        Reference (41)

E(keV)		sigma (barns)

80.0		37000

Data set #6     Reference (108)

E(keV)		sigma (barns)

80.0		29170

Nitrogen (Z=7) K line

Reference (37)

E(keV)		sigma (barns)

0.45		56200

0.5		75700

0.6		109000

0.7		136000

0.8		153000

0.9		159000

1.0		172000

1.25		178000

1.5		176000

1.75		179000

2.0		169000

3.0		148000

4.0		135000

6.0		104000

8.5		87500

10.6		76500

12.6		66000

14.7		57500

16.8		55200

Data set #2       Reference (42)

E(keV)		sigma (barns)

0.5		88300

0.65		106000

0.9		142000

1.0		156000

1.1		165000

1.21		172000

1.41		176000

1.51		176000

1.61		176000

1.71		175000

1.81		176000

2.01		172000

2.41		166000

2.81		160000

3.22		153000

3.62		146000

4.02		139000

4.82		128000

5.63		120000

6.43		110000

7.24		103000

8.04		96900

8.84		91100

9.65		85800

10.5		81100

Data set #3        Reference (39)

E(keV)		sigma (barns)

25.0		53000

Data set #4       Reference (108)

E(keV)		sigma (barns)

80.0		19520

Oxygen (Z=8) K line

Reference (42)

E(keV)		sigma (barns)

1.0		64300

1.2		76500

1.4		85300

1.6		90500

1.8		93200

2.0		94200

2.2		95200

2.4		95200

2.6		94000

2.8		92800

3.0		90800

3.2		90100

3.5		87600

3.8		85700

4.1		83600

4.4		81300

4.5		80700

4.7		79300

5.0		76100

5.5		73200

6.0		70200

7.0		65300

8.0		61200

9.0		57200

10.0		53900

11.0		50900

12.0		48300

13.0		45500

Data set #2        Reference (37)

E(keV)		sigma (barns)

1.0		75800

2.0		94100

3.0		93600

4.0		89600

5.0		78100

6.0		68200

8.5		56000

10.6		46800

12.6		41900

16.8		34300

Data set #3        Reference (45)

E(keV)		sigma (barns)

1.24		89000

2.08		94000

3.11		91000

Data set #4       Reference (39)

E(keV)		sigma (barns)

25.0		40000

Neon (Z=10) K line

Reference (37)

E(keV)		sigma (barns)

0.95		6000

1.0		9160

1.25		20700

1.5		28800

1.75		33500

2.0		37400

2.5		36800

3.0		38200

3.5		39400

4.0		40100

6.0		35000

8.5		31400

10.6		26800

12.6		23500

14.6		22300

Data set #2      Reference (45)

E(keV)		sigma (barns)

1.26		15600

1.54		29500

2.04		40500

3.32		41100

4.08		35400

5.04		32500

Data set #3      Reference (42)

E(keV)		sigma (barns)

1.31		19800

1.74		28300

2.18		32600

2.61		35200

3.05		36000

3.26		36200

3.48		36200

3.7		36200

3.92		36200

4.13		35700

4.35		35500

5.22		34100

6.09		32500

6.96		31100

7.83		29400

8.7		28200

10.0		26100

10.4		25400

Aluminum (Z=13) K line

Reference (53)

E(keV)		sigma (barns)

2.58		11800

3.68		14600

5.06		15300

6.54		14600

8.79		13400

11.0		12800

13.8		11400

17.2		10000

21.8		8880

25.8		8000

29.7		7280

Data set #2       Reference (93)

E(keV)		sigma (barns)

100		1527

Data set #3        Reference (108)

E(keV)		sigma (barns)

80		3650

Silicon (Z=14) K line

Reference (45)

E(keV)		sigma (barns)

2.99		8800

5.13		8500

5.69		8600

6.62		9500

7.95		9600

Silicon L23 line

Reference (55)

E(keV)		sigma (barns)

0.2		463000

0.4		620000

0.6		589000

0.8		540000

1.0		493000

1.2		445000

1.4		406000

1.6		378000

1.8		347000

Phosphorus  (Z=15)  L23 line

Reference (55)

E(keV)		sigma (barns)

0.26		299000

0.5		400000

0.75		380000

1.0		349000

1.3		318000

1.5		287000

1.8		264000

2.1		246000

2.3		225000

Sulfur (Z=16) L23 line

Reference (55)

E(keV)		sigma (barns)

0.33		205000

0.65		275000

1.0		261000

1.3		240000

1.6		218000

2.0		197000

2.3		181000

2.6		169000

Chlorine (Z=17) L23 line

Reference (55)

E(keV)		sigma (barns)

0.609		196500

0.71		196000

0.812		206300

0.913		207770

1.015		208500

1.131		200000

1.29		199000

1.53		193000

1.8		178000

2.03		167000

2.286		162500

2.54		156000

Argon (Z=18)	K line

Reference (56)

E(keV)		sigma (barns)

3.37		328

3.59		780

3.85		1090

4.03		1270

4.32		1490

4.56		1670

5.46		2170

6.42		2680

7.27		2710

8.11		2920

9.18		2980

10.0		2870

11.0		2900

12.0		2870

Data set #2      Reference (45)

E(keV)		sigma (barns)

3.64		820

3.99		1350

4.54		1660

5.05		2260

5.97		2760

6.99		2760

8.0		3370

8.9		3460

9.74		2960

Data set #3     Reference (37)

E(keV)		sigma (barns)

1.136		1370

1.246		1900

1.417		2380

1.577		2910

1.864		2910

2.182		2950

2.498		2890

2.779		2780

3.041		2730

Data set #4      Reference (57)

E(keV)		sigma (barns)

4.19		1440

5.11		1790

6.1		2270

7.68		2670

8.2		3120

  - 3080

Scandiun (Z=21) K line

E(KeV)	sigma (barns)

  - 76

  - 832

  - 1140

- 1233

  - 1228

15.1		1304

  - 1312

- 1272

- 1177

- 1188

- 1081

  - 1059

- 977

- 907

Titanium (Z=22) K line

Reference (58)

E(keV)		sigma (barns)

5.91		499

6.46		658

7.45		909

8.44		1070

9.44		1200

9.98		1260

10.4		1130

11.5		1350

12.5		1380

13.4		1400

14.9		1420

18.0		1420

23.0		1360

33.0		1220

38.0		1150

43.0		1090

47.0		1050

50.0		1030

Data set #2       Reference (93)

E(keV)		sigma (barns)

- 258

Data set #3	Reference (120)

E(keV)		sigma (barns)

5.5		36

6.0		102

7.0		364

9.0		515

10.0		649

12.0		880

14.0		885

16.0		1128

20.0		1205

25.0		1128

29.0		1064

Titanium (Z=22) L23 line

Reference (55)

E(keV)		sigma (barns)

0.9		43300

1.85		58000

2.75		55100

Vanadium (Z=23)  K line

Reference (125)

E (keV)	sigma (barns)

  - 34

  - 455

  - 764

  - 905

- 991

  - 1083

- 1105

- 1044

- 988

- 977

  - 850

  - 817

- 794

Chromium (Z=24) K line

Reference (119)

E(keV)		sigma (barns)

6.0		32

6.25		91

6.5		168

7.0		199

8.0		425

10.0		666

12.0		854

14.0		969

16.0		994

20.0		1020

23.0		964

25.0		907

Data set #2	Reference (120)

E(keV)		sigma (barns)

6.0		23

6.25		64

6.5		119

7.0		141

8.0		300

10.0		471

12.0		604

14.0		685

16.0		703

20.0		721

23.0		682

- 641

Data set #3	Reference (123)

E (keV)	sigma (barns)

  - 143

7.0		283

7.5		393

8.0		485

9.0		606

- 721

- 796

- 856

- 880

- 913

- 920

- 946

- 953

- 970

- 967

- 967

- 970

- 966

- 970

- 965

- 940

- 958

- 938

- 952

- 932

- 922

- 918

- 911

- 896

- 897

- 899

- 874

38.0		848

- 832

Manganese (Z=25) K line

Reference (59)

E(keV)		sigma (barns)

6.71		26

6.9		68

7.4		149

8.0		240

9.0		352

11.0		518

15.0		654

20.0		677

Data set #2      Reference (104)

E(keV)		sigma (barns)

50.0		600

Data set #3	Reference (118)

E(keV)		sigma (barns)

7.5		132.1

9.49		470.1

11.51		615.3

13.54		671.3

15.64		699.0

17.82		691.1

19.90		746.8

21.71		748.3

23.65		765.3

  - 728.2

Data set #4	Reference (126)

E(keV)		sigma (barns)

- 101

  - 222

- 317

  - 405

- 476

  - 542

- 574

- 662

- 713

- 755

- 806

- 820

- 854

- 852

- 871

- 853

- 869

- 857

- 848

- 865

- 899

- 843

- 857

- 836

- 857

- 836

- 833

- 829

- 820

- 815

- 799

- 794

- 781

- 804

- 765

- 750

- 745

Iron (Z=26) K line

Reference (113)

E(keV)		sigma (barns)

7.5		66

8.0		99.5

9.0		230.4

10.0		360.5

11.0		405.8

12.0		577.1

14.0		765.3

16.0		812.6

18.0		855.6

20.0		886.6

22.0		850.0

25.0		877.4

28.0		868.9

Data set #2	Reference (118)

E(keV)		sigma (barns)

7.93		105.9

10.0		362.5

12.05		482.4

14.23		612.5

16.26		679.6

18.36		689.9

20.38		683.2

22.33		706.8

  - 697.5

Data set #3	Reference (126)

E(keV)		sigma (barns)

  - 47

- 136

  - 216

- 274

  - 330

- 368

- 442

- 500

- 541

- 573

- 600

- 616

- 626

- 639

- 651

- 650

- 663

- 652

- 673

- 667

- 665

- 660

- 664

- 661

- 651

- 647

- 646

- 639

- 632

- 635

- 629

- 619

- 621

- 608

- 604

- 614

Cobalt (Z=27) K line

Reference (117)

E(keV)		sigma (barns)

8.50		86

10.57		314

12.67		454

14.78		502

16.73		526

18.67		575

20.85		568

22.80		547

24.90		525

Nickel (Z=28) K line

Reference (58)

E(keV)		sigma (barns)

8.91		105

9.83		193

12.3		351

14.7		446

19.7		528

24.7		552

29.8		553

34.8		540

39.7		526

44.7		512

49.7		498

Data set #2      Reference (60)

E(keV)		sigma (barns)

14.8		316

24.8		389

35.7		382

46.2		363

55.6		337

75.3		298

95.1		275

Data set #3      Reference (67)

E(keV)		sigma (barns)

70		338

Data set #4	Reference (119)

E(keV)		sigma (barns)

9.0		80

10.0		105

12.0		350

16.0		480

20.0		512

25.0		547

30.0		537

34.0		517

Data set#5	Reference (120)

E(keV)		sigma (barns)

9.0		57

10.0		74

12.0		247

16.0		339

20.0		362

25.0		387

30.0		380

34.0		366

42.0		341

46.0		308

Data set #4	Reference (123)

E (keV)	sigma (barns)

- 77

  - 115

9.5		134

  - 156

- 181

  - 220

- 262

  - 284

- 313

- 357

- 396

- 427

- 452

- 472

- 482

- 497

- 504

- 507

- 511

- 523

- 520

- 532

- 530

- 531

- 526

- 528

- 533

- 526

- 526

- 526

- 528

- 526

- 523

38		518

- 514

Copper (Z=29) K line

Reference (43)

E(keV)		sigma (barns)

9.12		15.9

10.0		86

15.0		294

20.0		380

25.0		397

Data set #2      Reference (59)

E(keV)		sigma (barns)

9.27		10.8

9.5		32.6

10.0		67.2

11.0		120

12.0		186

15.0		294

20.0		402

25.0		397

Data set #3     Reference (62)

E(keV)		sigma (barns)

81		269

114		249

Data set #4       Reference (44)

E(keV)		sigma (barns)

25		450

30		477

40		445

60		428

80		391

100		325

135		299

Data set #5      Reference (93)

E(keV)		sigma (barns)

100		185

Data set #6        Reference (104)

E(keV)		sigma (barns)

50		104

Data set #7	 Reference (117)

E(keV)		sigma (barns)

9.40		20

11.60		155

13.64		257

15.60		303

17.65		375

19.69		381

21.74		412

23.94		398

25.90		397

Data set #8	Reference (120)

E(keV)		sigma (barns)

9.0		10

9.5		20

10.5		50

12.0		151

15.0		291

17.5		339

20.0		373

22.5		395

25.0		410

- 406

Data set #9	Reference (123)

E (keV)	sigma (barns)

9.5		52

  - 144

- 182

- 244

- 294

- 332

- 362

- 382

- 405

- 420

- 438

- 448

- 453

- 460

- 465

- 474

- 487

- 484

- 493

- 493

- 488

- 494

- 492

- 491

- 490

- 484

- 484

- 486

- 479

- 483

40		482

Germanium (Z=32) K line

Reference (43)

E(keV)		sigma (barns)

11.2		4.76

12.0		37.3

15.0		136.0

20.0		210

- 237

Selenium (Z=34) K line

Reference (63)

E(keV)		sigma (barns)

60.0		206

100.0		180

200		145

Zirconium (Z=40) K line

Reference (93)

E(keV)		sigma (barns)

100		79.25

Niobium (Z=41) K line

Reference (121)

E(keV)		sigma (barns)

20.0		10.6

22.0		19.1

24.0		24.1

26.0		31.4

28.0		42.0

30.0		53.1

32.0		58.5

34.0		65.3

Molybdenum (Z=42) K line

Reference (113)

E(keV)		sigma (barns)

21.0		15.5

22		27.8

24		37.9

26		49.8

28		60.9

30		70.7

32		76.7

34		87.0

36		94.3

38		107.4

40		129.9

Silver (Z=47) K line

Reference (36)

E(keV)		sigma (barns)

29.88		15.5

37.35		29.6

49.8		38.9

62.25		44.8

74.7		46.3

87.15		46.37

99.6		46.07

124.5		44.81

149.4		43.3

174.3		42.1

Data set #2      Reference (43)

E(keV)		sigma (barns)

26		1.9

27		6.2

28		9.11

29		12.5

30		16.4

Data set #3       Reference (44)

E(keV)		sigma (barns)

30		25.7

40		49.9

50		63.2

60		68

80		67.9

100		67.9

120		67.7

140		65.4

Data set #4       Reference (93)

E(keV)		sigma (barns)

100		48.7

Data set #5       Reference (66)

E(keV)		sigma (barns)

108		42.4

114		34.2

129		40.6

133		36.5

162		49.2

223		58.6

285		58.1

289		55.6

352		55.9

360		58.3

423		56.7

431		54.4

Data set #6       Reference (104)

E(keV)		sigma (barns)

- 44

Data set #7	Reference (124)

E(keV)		sigma (barns)

- 11

32		18

- 23

40		40

- 45

- 50

- 46

- 49

- 50

65		53

Tin (Z=50) K line

Reference (94)

E(keV)		sigma (barns)

50		40

100		51

200		46

500		41

Data set #2       Reference (66)

E(keV)		sigma (barns)

103.4		25.33

108.5		30.23

123.0		30.0

125.0		35.0

155.0		45.4

160.0		51.2

213.0		43.2

217.0		58.0

275.0		47.5

278.0		57.4

337.0		59.2

343.0		51.7

405.0		54.4

410.0		60.0

Data set #3      Reference (104)

E(keV)		sigma (barns)

50		33.0

Antimony (Z = 51) K line

Reference (63)

E(keV)		sigma (barns)

60		34.0

100		40.1

200		41.1

Data set #2       Reference (93)

E(keV)		sigma (barns)

100		38.6

Barium (Z=56) K line

Reference (93)

E(keV)		sigma (barns)

100		25.6

Lanthanum (Z=57) K line

Reference (93)

E(keV)		sigma (barns)

100		23.7

Praesodymium (Z=59) K line

Reference (93)

E(keV)		sigma (barns)

100		20.3

Tungsten (Z=74) K line

Reference (66)

E(keV)		sigma (barns)

210		5

217		14.8

244		6.6

267		11.4

274		17.9

336		16.9

343		23.4

405		22.4

472		19.7

546		26.0

553		30.0

Tungsten L line

Reference (128)

E(keV)		sigma (barns)

12		68

13		91

14		108

15		125

16		137

17		147

18		155

19		162

20		168

22		176

24		181

26		186

28		186

30		187

Platinum (Z=78) L line

Reference (128)

E(keV)		sigma (barns)

13		52

14		75

15		93

16		106

17		118

18		124

19		136

20		148

22		155

24		160

26		166

28		167

30		174

Gold (Z=79) K line

Reference (44)

E(keV)		sigma (barns)

90		2.46

100		4.43

120		5.91

140		6.5

200		8.57

Data set #2      Reference (94)

E(keV)		sigma (barns)

100		5.6

200		9.5

500		13.2

Data set #3       Reference (66)

E(keV)		sigma (barns)

236		9.25

270		15

277		20.8

301		11.56

310		21.5

341		13.94

400		17.1

408		27.1

466		19.4

556		19.1

564		24.9

Gold (Z=79) L2  lines

Reference (64)

E(keV)		sigma (barns)

14.832		10.7

15.656		25.7

16.892		38.8

18.128		47.8

20.462		61.2

21.973		74.6

24.307		86.9

27.466		100.0

29.251		108

34.333		111

41.199		119

Data set #2       Reference (65)

E(keV)		sigma (barns)

16.34		25.4

20.599		65.7

24.582		96.4

29.938		122.1

34.333		125

41.199		123.9

Data set #3       Reference (71)

E(keV)		sigma (barns)

17.17		111.0

19.64		154

23.35		207

34.33		260

41.2		245

Data set #4	Reference (128)

E(keV)		sigma (barns)

13		39

14		69

15		89

16		105

17		120

18		128

19		138

20		146

22		155

24		161

26		163

28		165

30		167

Gold (Z=79) L3 line

Reference (64)

E(keV)		sigma (barns)

13.468		44.2

14.422		111.9

15.018		126.9

17.879		174.6

20.858		203.3

22.408		229.2

25.387		288.0

27.652		300

30.632		349.0

36.949		383.6

41.24		382.0

Data set #2      Reference (65)

E(keV)		sigma (barns)

13.468		51.6

14.78		114.9

17.759		164.2

23.838		252.0

29.797		282

35.757		295

41.717		273

Data set #3     Reference (44)

E(keV)		sigma (barns)

20		702

25		690

30		706

40		695

60		643

80		552

100		509

120		460

140		450

Data set #4      Reference (71)

E(keV)		sigma (barns)

14.89		253

17.88		373

24.4		550

29.8		598

35.25		625

  - 591

Data set #5	Reference (124)

E(keV)		sigma (barns)

12		180

- 310

16		410

- 490

- 510

- 520

- 510

32		490

- 500

- 450

- 420

55		400

75		310

Lead (Z=82) K line

Reference (66)

E(keV)		sigma (barns)

262		19.2

303		10.3

311		17.5

334		22.2

396		13.2

405		19.6

476		18.6

550		29.7

563		23.1

# Section 5

Xray fluorescent yields

Arranged by shell and atomic number

#### K-shell Data

| Element Z | Name | 53 | 34 | 58 | 61,62 | 56 | 101 | 101, 116 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 0.0009 |  |  |  |  |  |  |
| 7 |  | 0.0015 |  |  |  |  |  |  |
| 8 |  | 0.0022 |  |  |  |  |  |  |
| 9 |  |  |  |  |  |  |  |  |
| 10 |  | 0.0081 |  | 0.043 |  |  |  |  |
| 11 |  |  |  |  |  |  |  |  |
| 12 |  | 0.013 |  |  | 0.028 |  |  |  |
| 13 |  |  |  | 0.008 | 0.0381 |  |  | 0.038 |
| 14 |  | 0.038 |  |  |  |  |  | 0.043 |
| 15 |  |  |  |  |  |  |  | 0.06 |
| 16 |  | 0.083 |  |  |  |  |  | 0.082 |
| 17 |  | 0.108 |  |  |  |  | 0.093 | 0.0955 |
| 18 |  | 0.123 |  |  |  |  | 0.081 | 0.122 |
| 19 |  |  |  |  |  |  |  |  |
| 20 |  | 0.15 | 0.207 |  |  |  |  |  |
| 21 |  |  |  |  |  |  |  | 0.19 |
| 22 |  |  |  |  |  |  | 0.18 | 0.221 |
| 23 |  |  |  | 0.305 | 0.23 |  | 0.24 | 0.253 |
| 24 |  | 0.264 |  |  |  |  | 0.285 | 0.283 |
| 25 |  |  |  | 0.308 | 0.27 |  |  | 0.313 |
| 26 |  | 0.33 | 0.343 |  |  |  | 0.375 | 0.342 |
| 27 |  |  |  |  | 0.31 |  |  | 0.366 |
| 28 |  | 0.38 | 0.436 |  |  |  | 0.366 |  |
| 29 |  | 0.419 |  |  | 0.42 |  | 0.4 | 0.443 |
| 30 |  | 0.44 | 0.476 |  |  |  | 0.446 |  |
| 31 |  |  |  |  | 0.47 |  | 0.53 | 0.528 |
| 32 |  |  |  |  |  |  |  | 0.554 |
| 33 |  | 0.53 |  |  |  |  |  | 0.588 |
| 34 |  | 0.562 | 0.585 |  |  |  | 0.575 |  |
| 35 |  | 0.623 |  |  |  |  | 0.565 |  |
| 36 |  | 0.67 |  |  |  |  | 0.62 | 0.66 |
| 37 |  |  |  |  |  |  |  | 0.669 |
| 38 |  | 0.644 |  |  |  |  | 0.64 | 0.702 |
| 39 |  |  |  |  |  |  |  |  |
| 40 |  |  |  |  |  | 0.645 | 0.7 |  |
| 41 |  |  |  |  |  | 0.713 | 0.73 |  |
| 42 |  | 0.785 |  |  |  | 0.714 | 0.73 |  |
| 43 |  |  | 0.7 |  |  |  | 0.697 |  |
| 44 |  |  |  |  |  |  |  |  |
| 45 |  | 0.801 |  |  |  | 0.779 | 0.786 |  |
| 46 |  | 0.835 |  |  |  | 0.781 | 0.79 |  |
| 47 |  | 0.84 |  |  |  | 0.813 | 0.821 | 0.834 |
| 48 |  | 0.773 |  |  |  | 0.819 | 0.827 |  |
| 49 |  |  |  |  |  |  | 0.87 |  |
| 50 |  | 0.855 |  |  |  | 0.84 | 0.846 |  |
| 51 |  | 0.862 |  |  |  |  |  |  |
| 52 |  | 0.872 |  |  |  |  |  | 0.857 |
| 53 |  | 0.88 |  |  |  |  | 0.91 |  |
| 54 |  | 0.81 |  |  |  |  | 0.88 | 0.894 |
| 55 |  | 0.89 |  |  |  | 0.898 | 0.873 | 0.889 |
| 56 |  | 0.87 |  |  |  | 0.85 |  |  |
| 57 |  |  |  |  |  | 0.94 | 0.88 |  |
| 58 |  |  |  |  |  | 0.9 |  |  |
| 59 |  | 0.88 |  |  |  | 0.9 |  |  |
| 60 |  |  |  |  |  |  |  |  |
| 61 |  |  |  |  |  |  |  |  |
| 62 |  |  |  |  |  |  |  | 0.923 |
| 63 |  |  |  |  |  |  | 0.908 | 0.925 |
| 64 |  |  |  |  |  |  | 0.925 | 0.940 |
| 65 |  |  |  |  |  |  |  |  |
| 66 |  |  |  |  |  | 0.943 |  | 0.941 |
| 67 |  |  |  |  |  |  |  |  |
| 68 |  |  |  |  |  |  | 0.955 |  |
| 69 |  |  |  |  |  |  |  |  |
| 70 |  |  |  |  |  | 0.936 |  |  |
| 71 |  |  |  |  |  |  |  |  |
| 72 |  |  |  |  |  |  |  |  |
| 73 |  |  |  |  |  |  |  | 0.954 |
| 74 |  |  |  |  |  |  |  | 0.961 |
| 75 |  |  |  |  |  |  |  |  |
| 76 |  |  |  |  |  |  |  |  |
| 77 |  |  |  |  |  |  |  |  |
| 78 |  | 0.942 |  |  |  |  |  | 0.967 |
| 79 |  |  |  |  |  |  |  | 0.954 |
| 80 |  | 0.946 |  |  |  |  | 0.952 | 0.958 |
| 81 |  |  |  |  |  |  |  |  |
| 82 |  |  |  |  |  | 0.96 |  | 0.972 |
| 83 |  | 0.95 |  |  |  | 0.96 | 0.976 |  |
| 84 |  | 0.894 |  |  |  | 0.944 |  |  |
| 85 |  |  |  |  |  |  |  |  |
| 86 |  |  |  |  |  |  |  |  |
| 87 |  |  |  |  |  |  |  |  |
| 88 |  |  |  |  |  |  |  |  |
| 89 |  |  |  |  |  |  |  |  |
| 90 |  |  |  |  |  |  |  |  |
| 91 |  |  |  |  |  |  |  |  |
| 92 |  |  |  |  |  | 0.967 |  | 0.97 |
| 93 |  |  |  |  |  | 0.938 |  |  |

L-shell data

| Z | Name | Ref 98 | Ref 102 | Ref 100 | Ref 101 | Ref 101 | Ref 101 | Ref 101 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23 | V | 0.00235 |  |  |  |  |  |  |
| 24 | Cr |  |  |  |  |  |  |  |
| 25 | Mn | 0.00295 |  |  |  |  |  |  |
| 26 | Fe |  |  |  |  |  |  |  |
| 27 | Co |  |  |  |  |  |  |  |
| 28 | Ni |  |  |  |  |  |  |  |
| 29 | Cu | 0.0056 |  |  |  |  |  |  |
| 30 | Zn |  |  |  |  |  |  |  |
| 31 | Ga | 0.0064 |  |  |  |  |  |  |
| 32 | Ge |  |  |  |  |  |  |  |
| 33 | As |  |  |  |  |  |  |  |
| 34 | Se |  |  |  |  |  |  |  |
| 35 | Br |  |  |  |  |  |  |  |
| 36 | Kr |  |  |  |  |  | 0.013 | 0.075 |
| 37 | Rb |  |  | 0.13 | 0.075 | 0.011 |  |  |
| 38 | Sr |  |  | 0.011 |  |  |  |  |
| 39 | Y |  |  | 0.0315 |  |  |  |  |
| 40 | Zr |  | 0.034 | 0.057 |  |  |  |  |
| 41 | Nb |  | 0.036 | 0.022 |  |  |  |  |
| 42 | Mo |  | 0.047 | 0.067 |  |  |  |  |
| 43 | Tc |  |  |  |  |  |  |  |
| 44 | Ru |  |  |  |  |  |  |  |
| 45 | Rh |  |  |  |  |  |  |  |
| 46 | Pd |  |  |  |  |  |  |  |
| 47 | Ag |  | 0.054 | 0.1 | 0.029 | 0.047 |  |  |
| 48 | Cd |  | 0.055 |  |  |  |  |  |
| 49 | In |  | 0.065 |  |  |  |  |  |
| 50 | Sn |  | 0.064 |  |  |  |  |  |
| 51 | Sb |  | 0.07 | 0.119 |  |  |  |  |
| 52 | Te |  |  | 0.122 | 0.073 |  |  |  |
| 53 | I |  |  |  |  |  |  |  |
| 54 | Xe |  |  | 0.25 | 0.103 | 0.11 | 0.21 |  |
| 55 | Cs |  |  | 0.089 |  |  |  |  |
| 56 | Ba |  |  | 0.148 | 0.093 |  |  |  |
| 57 | La |  | 0.15 | 0.158 | 0.11 | 0.092 |  |  |
| 58 | Ce |  | 0.16 | 0.163 |  |  |  |  |
| 59 | Pr |  | 0.16 | 0.123 | 0.167 | 0.09 |  |  |
| 60 | Nd |  | 0.16 | 0.17 |  |  |  |  |
| 61 | Pm | 0.185 |  |  |  |  |  |  |
| 62 | Sm |  | 0.17 | 0.188 |  |  |  |  |
| 63 | Eu |  | 0.17 | 0.17 |  |  |  |  |
| 64 | Gd |  | 0.18 | 0.198 |  |  |  |  |
| 65 | Tb | 0.195 | 0.19 | 0.19 |  |  |  |  |
| 66 | Dy |  | 0.21 | 0.14 |  |  |  |  |
| 67 | Ho |  | 0.22 | 0.17 |  |  |  |  |
| 68 | Er |  | 0.21 |  |  |  | 0.228 |  |
| 69 | Tm |  | 0.23 |  |  |  |  |  |
| 70 | Yb |  | 0.25 | 0.2 |  |  | 0.2 |  |
| 71 | Lu |  | 0.26 | 0.29 |  |  |  |  |
| 72 | Hf |  | 0.29 | 0.26 | 0.17 | 0.24 |  |  |
| 73 | Ta |  | 0.29 | 0.225 |  |  | 0.28 |  |
| 74 | W |  | 0.31 | 0.298 |  |  |  |  |
| 75 | Re |  | 0.3 |  |  |  |  |  |
| 76 | Os |  | 0.32 | 0.348 |  |  |  |  |
| 77 | Ir |  | 0.31 | 0.3 |  |  |  |  |
| 78 | Pt |  | 0.32 | 0.348 |  |  |  |  |
| 79 | Au |  | 0.374 | 0.365 | 0.43 |  |  |  |
| 80 | Hg |  | 0.41 | 0.24 | 0.37 | 0.34 | 0.43 | 0.4 |
| 81 | Tl |  | 0.44 | 0.5 | 0.48 | 0.34 | 0.32 | 0.39 |
| 82 | Pb |  | 0.36 | 0.398 | 0.39 | 0.297 |  |  |
| 83 | Bi |  | 0.414 | 0.402 | 0.51 | 0.38 |  |  |
| 84 | Po |  |  |  |  |  |  |  |
| 85 |  |  |  |  |  |  |  |  |
| 86 |  |  |  |  |  |  |  |  |
| 87 |  |  |  |  |  |  |  |  |
| 88 | Ra |  |  | 0.48 | 0.4 | 0.52 |  |  |
| 89 |  |  |  |  |  |  |  |  |
| 90 | Th |  |  | 0.488 |  |  |  |  |
| 91 | Pa |  |  | 0.52 | 0.5 |  |  |  |
| 92 | U |  |  | 0.478 | 0.603 | 0.57 |  |  |
| 93 | Np |  |  | 0.66 | 0.49 |  |  |  |
| 94 | Pu |  |  | 0.54 | 0.73 | 0.566 |  |  |
| 95 |  |  |  |  |  |  |  |  |
| 96 | Cm |  |  | 0.531 |  |  |  |  |

M-shell

| Z | Name | Ref 102 | Ref 98 | Ref 101 |
| --- | --- | --- | --- | --- |
| 76 | Os | 0.013 |  |  |
| 77 | Ir |  |  |  |
| 78 | Pt |  |  |  |
| 79 | Au | 0.024 | 0.023 |  |
| 80 | Hg |  |  |  |
| 81 | Tl |  |  |  |
| 82 | Pb | 0.026 | 0.029 |  |
| 83 | Bi | 0.03 | 0.035 | 0.037 |
| 84 | Po |  |  |  |
| 85 |  |  |  |  |
| 86 |  |  |  |  |
| 87 |  |  |  |  |
| 88 | Ra |  |  |  |
| 89 |  |  |  |  |
| 90 | Th |  |  |  |
| 91 | Pa |  |  |  |
| 92 | U |  |  | 0.06 |

End of Data

316