## Slide 1: Investigation of Fundamental Limits to Beam Brightness Available From Photoinjectors
Ivan Bazarov
Cornell University

## Slide 2
Project Significance
Goals & Status
Accomplishments
National and International Impact
Future Steps
Outline

## Slide 3
Project Significance
What is Physical Limit to Beam Brightness?
electrons
Photocathode
-Ez
electron beam
Lab scale ultrafast electron diffraction
Big linear accelerators
LCLS-II
Laser
Coherence length
Beam brightness
EIC
Small MTE has big impact on accelerators

## Slide 4
Goals
Understand fundamental physics and technology limits to high brightness beam production in photoinjectors;
Cathode research:
  Photoemission physics modeling & measurements of intrinsic mean transverse energy (MTE), response time, and quantum efficiency (QE) of non-metal photocathodes (QE  5%);
  Explore and engineer novel photocathode materials in real-life accelerator conditions of a high average current photoinjector
Beam dynamics:
  Realization of the brightness limit from the photoinjector as set by space charge and the photocathode mean transverse energy spread
  Among the physics issues being tackled: adaptive laser shaping for lowest emittance

## Slide 5
Project Status
Project start/end: Apr 2010/2015
Output: 19 journal papers, 12 conference proceedings, 2 book chapters
All milestones/goals met
Enabled many advances: e.g. world-record brightness photoinjector, smallest emittance cathodes to date, longest lifetime @ high currents, etc.

## Slide 6
Some of the Highlights
Photocathode physics modeling
Ultralow emittance cathode diagnostics
High performance photocathodes
Laser shaping for low emittance production
Cornell Photoinjector Record Beam Performance

## Slide 7
(1) Cathode modeling of III-V’s
VBM
CBM
Vacuum level
GaAs – Vacuum interface
Fermi level
Band Gap = 1.42 eV
0.5 eV
Surface
barrier
VBM
CBM
Vacuum level
GaAs – Vacuum interface
Fermi level
Band Gap = 1.42 eV
0.5 eV
4-5 eV
Ga
As
Cs
Best known photocathode
Source of spin-polarized electrons
Well studied material –
best for low energy photoemission studies
7
Easy to grow layered structures
Why III-V’s?

## Slide 8
Monte-Carlo Photocathode Code
Matlab based – also Python version now available
Developed in collaboration with Tech-X
>10k lines of vectorized code
Few days on a normal PC
Few hours on a cluster
Lots of bench-marking!!!
J. App. Phys. 113 (10), 104904 (2013)

## Slide 9
Physics Toolkit Approach
Ability to model various materials, include different scattering processes;
Excellent agreement to experiment (Cs:GaAs) in wide rage of photon energies.
Extension to layered structures;

## Slide 10
Engineering Photocathodes
Surface Layers have different doping and different material (GaAs/AlGaAs…)
Easy to grow
using MBE
Change in material causes change in band-gap
Change in doping causes bands to bend
Γ-valley min
Valance Band Max
Band profiles can be calculated
using a Schrodinger-Poisson
solver
valley heights
X-valley min
We can tune –
light absorption
electric fields
scattering
Can we tune structure to improve photoemission?
Light
e-

## Slide 11
Layered Photocathodes
p-GaAs
Layered structure
Layered structure
p-GaAs
Simulation
Experiment
Simulation
Experiment
QE
MTE
PRL 112 (9), 097601 (2014)
Layered structure
p-GaAs

## Slide 12
(2) Surface Effect on Photoemission
Amorphous Cs
adsorption
Random Cs
adsorption
J. Kim, M.C. Gallagher and R.F. Willis, Appl. Surf. Sci., 67, 286 (1993)
Top
Views
GaAs(100)
Ga
As
Cs
Raised Ga Dimer Reconstruction
~1 nm Surface Roughness
~100 meV Workfunction Varia-tion: Cause for a Larger MTE?
PRB, 91, 035408 (2015)
What Does the Surface Look Like?

## Slide 13
Ultra-low emittance diagnostics
Resolving ≤ 10 meV of low energy (≪ eV) photo-electrons tricky;
Need for reliable diagnostics capable of diagnosing cathodes in-situ;
Must be connected to other surface analysis techniques to “debug” the physics, operate in UHV without interruptions

## Slide 14
2D Energy Analyzer at Cornell
MARK1
MARK2
B field
CATHODE
2-D distribution
from K2CsSb
3x Resolution (5 meV)
50x Signal to noise ratio
Compact size
First Marking Electrode
Varying Magnetic Field
Second Marking Electrode
Beam Current Detector
Rev. Sci. Instr. 86, 033301 (2015)
Improvements over its predecessor:

## Slide 15
Essential Cathode Capabilities
dedicated MBE system
over in Wilson Lab
actual injector
Phillips
Newman
Wilson
over in Newman Lab
Photocathode growth & analysis chamber
over in Phillips Hall
Cornell University campus
Vacuum Suitcase
Photocathode Growth, Diagnostics, Beam Testing at Cornell

## Slide 16: Cornell Injector Overview
NaKSb: MTE = 140 meV, QE roughly 5%
Superconducting
RF Cavities
395 kV DC Gun +
Bunching/Focusing
Short SRF Linac
5 – 15 MeV
6 Dimensional Phase Space Diagnostics + High Power Beam Dump + Chicane (Compton Scattering)
Viewscreen
Emittance Measurement System
1st Scanner
Magnet Pair
2nd Scanner
Magnet Pair
1st Slit
2nd Slit
Deflecting Cavity
Faraday Cup
+ Viewscreen
Faraday Cup
395 kV DC Gun
50 MHz,
520 nm

## Slide 17
High Performance Cathodes
Active area is offset from the center
Ion damage limited to the central area
photocathode after use
Lifetime good enough with the existing laser to operate for a week without interruption at ~70 mA
Learned how to minimize halo/manufacture robust cathodes
NaKSb Lifetime at 65 mA
Appl. Phys. Lett. 102 (2013) 034105
Appl. Phys. Lett. 103 (2013) 103504
0.1 Amp avg current from photoinjectors with good lifetime no longer a dream
1.3 GHz laser

## Slide 18
Laser Shaping
Transversely: clip Gaussian laser profile at a given intensity
fraction (typically 50%)
Longitudinally: Birefringent Crystals for pulse stacking:

## Slide 19: Effects of the Laser Shape
Ideal Shape
Measured Shape
Emittance at 10 MeV

## Slide 20: Now able to compensate for QE changes!
Phys. Rev. ST Accel. Beams 18, 023401 (2015)
Appl. Phys. Lett. 105 (2014) 171109
A new shaping method using liquid crystal spatial light modulator (SLM)
Tested with the actual e- beam
Increase emittance performance
Adaptively fix spatial QE irregularities; obtain more optimal shape

## Slide 21: LCLS-II Injector Tests at Cornell
CU Injector as possible injector for high rep. rate FEL (LCLS-II)
Funded by SLAC to perform beam tests
10 MeV operation with low current (<1 mA)
Bunch charge | Peak current | Emittance (95%)
20 pC | 5 A | 0.25 mm
100 pC | 10 A | 0.4 mm
300 pC | 30 A | 0.6 mm

## Slide 22: LCLS-II Specs Met…
Q (pC) | Ipeak Target (A) | Ipeak (A) | εn Target (95%, mm) | εn (95%, mm) | εn,th /εn
20 | 5 | 5 | 0.25 | H: 0.18, V: 0.19 | >60%
100 | 10 | 11.5 | 0.40 | H: 0.32, V: 0.30 | >80%
300 | 30 | 32 | 0.60 | H: 0.62, V: 0.60 | >70%
First injector to demonstrate LCLS-II beam requirements
Appl. Phys. Lett. 106 (2015) 094101
@10 MeV kinetic energy

## Slide 23: Nanocoulomb Operation for EIC
CU Injector as a demonstration of Electron-Ion Collider technology (funded by DOE NP)
Operate at higher bunch charges (up to 2 nC)
More relaxed emittance requirements
More relaxed bunch length
High current (up to 50 mA @ 50 MHz repetition rate, 1 nC)
  Requires running off center on cathode

## Slide 24: 1 & 2nC Results
1 nC: 1.6 μm, 2 nC: 4.4 μm (95%)
1 nC: 1.6 μm, 2 nC: 4.0 μm (95%)
submitted to PRSTAB (2015)

## Slide 25: Emittance growth vs. charge
Q (pC) | Peak current (A) | Emittance (95%, mm)
20 | 5 | H: 0.18 V: 0.19
100 | 11.5 | H: 0.32 V: 0.30
300 | 32 | H: 0.62 V: 0.60
1000 | 50 | H: 1.6 V: 1.6
2000 | 56 | H: 4.4 V: 4.0
The trend starts out as q1/2, and becomes more linear around 300 pC…

## Slide 26
Next Steps
Emittance of well-designed photoinjectors is dominated by photocathodes (e.g. ~90% for Cornell)
  Plenty of room for further increase of brightness;
  Key direction to pursue: MTE = 1-2 meV photocathodes (limit due to Disorder-Induced-Heating);
Exciting directions:
  Cryogenic cathodes (MTE limited by the lattice temperature)
  Surface engineering (avoid Cs layer or its scattering)
New approaches for improving cathode longevity
  Thin protective layers

## Slide 27
Big Impact
x100 Brightness Improvement in View
Huge Impact: e.g. this would enable
  Compact xFELs (100’s of MeV)
  Extend fs electron diffraction to proteins

## Slide 28
Training for future
PhD students
>10 undergrads who participated in the research over 5 years

## Slide 29
Cornell High Brightness Sources Group
Cornell High-Brightness Beam Group:

## Slide 30
Backup Slides

## Slide 31
Find materials with the room temperature MTE and cool them!
Trading QE for lower MTE (still worth doing so for many apps);
Try materials with higher density of states;
Get MTE’s similar to ionized ultracold (MOT) atoms.
T. Vecchione, P3 Cornell workshop (2012)
MTE = 25 meV
oxidized antimony @ RT
U. Weigel, PhD thesis (2003)
GaAs
Ultracold (cryo) photocathodes

## Slide 32
K. Uchida et al., IPAC’14 (2014) 664
GaAs
Cs2Te
thin layer
Sensitive to 900 nm!
What happens to lifetime?
What happens to the polarization?
Protective layers?
Notes: Masao Kuriki