## Slide 1: High brightness electron source using cryo-DC HV photogun
Ivan Bazarov (Cornell University)

## Slide 2: Acknowledgements
Hyeri Lee (PhD student)
Xianghong Liu
Luca Cultrera
Val Kastroun
Bruce Dunham
Colwyn Gulliford
Adam Bartnik
Funding by the NSF Grant No. PHY-1416318
And the DOE DE-SC0014338 and DE-SC0011643

## Slide 3: Outline
Drivers for high brightness
Experimental evidence in favor of cooling cathodes
Cryo-cooled HV DC gun concept
Simulated performance
Gun construction & first beam

## Slide 4: Brightness, Emittance and Disordered Cathodes
0
electrons
Ez (sets maximum electron density)
electron beam
Laser
Photocathode
All photoinjectors use cathodes with disordered surfaces (e.g. alkali-antimonides, polycrystalline metals, Cs:GaAs)
Energy
Vacuum Level
Fermi Level
Temperature, surface roughness, and work function variations eventually limit MTE
Appl. Phys. Lett. 107, 134101 (2015)
Phys. Rev. Applied 4, 024015 (2015)
J. Appl. Phys. 121, 044904 (2017)

## Slide 5: Cornell’s Center for Bright Beams
x100 brighter electron beams through better photocathodes, guns, beam dynamics, etc.

## Slide 6: Ultrafast electron diffraction
light sensitive
protein rhodopsin
Coherence length ≥ protein unit cell (~few nm)
Time resolution ~100fs (ultrafast scale)
Number of electrons (for signal) ≥ 105
Toward a molecular movie for biological processes with electrons…
State-of-the art 100 fs electron source
With 100x more brightness

## Slide 7: Coherence length scaling
Phys. Rev. Acc. Beams 19, 093402 (2016)
reduced Compton wavelength
cathode emittance preservation ratio ∊ (0, 1]
final spot size
cathode field
(“pancake”)
(“cigar”)

## Slide 8: Points of impact
emittance preservation
cathode field
initial beam temperature
genetic algorithms & beamline optimization
breakdown (DC vs RF; field vs voltage)
≥10 MV/m DC field doable
cold atoms, single-crystal cathodes, cooling disordered cathodes

## Slide 9: Cooling alkali antimonides to 90K

## Slide 10: Cooling alkali antimonides to 90K
~25 meV at 300 K
~8 meV at 90 K
~0.3 mm mrad
~0.17 mm mrad
What happens if we cool the cathode to cryogenic temperature?
As T lowers from 300 K to 90 K, MTE should lower from 25 to 8 meV
actual MTE ~14 meV or 160 K equiv. temp.

## Slide 11: Cooling even further?
We suspect that the cathode roughness manifests itself here
Active research ongoing that promises much smoother surface
Our Monte-Carlo modeling of the bulk scattering suggests cryo-cooling can bring MTE further down
~2 meV is predicted @ 20K
J. Appl. Phys 121 (2017) 215702

## Slide 12: Transmission cathodes
Appl. Phys. Lett. 108, 124105 (2016)

## Slide 13: Best configuration for tight laser focusing

## Slide 14: Cryo-cooled photogun concept
1) HV DC photoemission gun
- Voltage: >200kV
- Cathode E-field: >10MV/m
2) Cathode cryo-T (20K)
3) Compact design

## Slide 15: Simulated performance
Phys. Rev. Acc. Beams 19, 093402 (2016)

## Slide 16: 105 electrons (MTE = 5 meV)
Phys. Rev. Acc. Beams 19, 093402 (2016)
MTE accounts for ≤1/2 final emittance

## Slide 17: Gun construction

## Slide 18: Cryo-tests
At the cathode
43±1K
Cryopump
(~6W at 15K)

## Slide 19: HV processing

## Slide 20: Puck transfer
Interface jacket to the old Cornell puck

## Slide 21: First beam!
Made first beam at ~200 kV (10MV/m) at both RT and cryo-T (40K)
The gun is now being relocated to its permanent home, more results soon!